Victorian Stucco

Editor: Miles Lewis

Published by the Heritage Council 
of Victoria, Melbourne

References throughout to the heritage website or Heritage 
Victoria website refer to: www.heritage.vic.gov.au which 
includes the searchable Victorian Heritage Database.

Published by the Heritage Council of Victoria, Melbourne, 
March 2013. Also published at www.heritage.vic.gov.au

© State of Victoria, Heritage Council of Victoria 2011.

This publication is copyright. No part may be reproduced 
by any process except in accordance with the provisions 
of the Copyright Act 1968.

ISBN 978-1-921607-97-4 (online)

Disclaimer

This publication may be of assistance to you but the State of Victoria and its employees do not guarantee that the publication is without flaw of any kind or is wholly appropriate for your particular purposes and therefore disclaims all liability for any error, loss or other consequence which may arise from you relying on any information in this publication.

Heritage Victoria/Heritage Council of Victoria,
Level 4, 55 Collins St, Melbourne 3000

GPO Box 2392, Melbourne, Victoria 3001

Phone: (03) 9208 3333
Fax: (03) 9208 3147

Email: heritage.council@dpcd.vic.gov.au
Web: www.heritage.vic.gov.au

Donald Ellsmore: further editing and coordination

Sue Balderstone: Index

Cover images: From left ( back cover) to right

Photographs by Donald Ellsmore:
Detail of weathered stucco on St Patrick’s Hall, Ballarat
Detail of incised decoration on house Gore Street, Fitzroy
Detail on facade of Smith Street, Fitzroy

Contents

Introduction	6

Origins of Stucco	7

Miles Lewis	7

Stucco: Materials and Finishes	13

Donald Ellsmore	13

Stucco layering	18

Surface textures and finishes	19

Stucco materials	19

Natural and applied colour	20

Australian Stucco	24

Miles Lewis	24

Materials and Techniques  of External Stucco	36

Barrie Cooper	36

External Renders: Materials,  Properties and Conservation Issues	42

David Young	42

Non-hydraulic lime	43

Lime putty versus dry hydrated lime powder	44

Hydraulic limes	44

Mineralogy and colour	46

Impurities	47

Grain shape	47

Size grading	47

Clays and fine silts	47

Void ratio	47

Significance	48

Compatibility	48

Application of significance and compatibility criteria	48

Testing of stucco	50

David West	50

General overview	50

Hands-on overview	50

Detailed survey	51

The Analysis and Conservation  of Stucco Surface Finishes	55

Jenny Dickens with a contribution by David Tilbrooke	55

Stucco materials	57

Stucco colourants	57

Stucco coatings	58

Maintenance coatings	59

Surface deposits	59

Documentary research	61

Sampling	61

Visual examination	62

Visual microscopy	62

Semi-micro analysis in architectural conservation investigation	63

Instrumental techniques for micro sample analysis	64

Spectroscopy	64

Chromatography	64

Electron microscopy	64

X-ray Fluorescence (XRF) and Particle Induced X-ray Emission (PIXE)	65

X-ray Diffraction (XRD)	65

Determining the architect’s or builder’s intent	65

Approach to intervention	65

Applying the results	66

Case study: ‘Benvenuta’	69

Background	69

Project	69

Results	69

Summary	70

Conclusions	71

Cleaning and Re-coating Victorian Stucco	72

Donald Ellsmore	72

Cleaning	77

Dealing with clear coatings	78

Paint removal	78

Clear finishes	79

Limewashes	79

Distempers	79

Cement paints	80

Oil paints	80

Mineral silicate paints	80

Acrylic resin paints	80

Other paint types	81

CASE STUDIES	82

Documentation: Peter Lovell	82

Mason & Bricklayer	82

Plasterer	82

Advertisements	82

Mason and Bricklayer	83

Plasterer	83

Bontharambo tower: Greg Owen	85

Render	87

Repair types	88

Mortars	88

Access	89

Repair Type R2, repair of vertical cracking in cornice, other than type R1	90

Repair Type R3, removal and replacement of poor previous OPC render repairs	90

Repair Type R4, replacement/patching of flat render	91

Repair Type R5, replacement/patching of run mouldings	91

Repair Type R6, replacement/repair of precast finials, balusters and enrichments	91

Repair Type R7, refixing flat delaminated render	92

Repair Type R8, refixing run mouldings	92

Repair Type R9, repairing eroded brickwork and joints	93

Stucco – Malmsbury Town Hall:  Michael Dempsey	94

Methods	96

A sampling of terminology	98

Glossary	100

Bibliography	109

Endnotes	117

Index	124

Introduction

This publication derives from a seminar on Victorian Stucco held at the South Melbourne Town Hall in 2007, initiated by Dr Donald Ellsmore of the Association for Preservation Technology and managed by the International Specialised Skills Institute. The sponsoring bodies were the Association for Preservation Technology International, the Design Institute of Australia, the Heritage Council of Victoria, Heritage Victoria, the International Specialised Skills Institute, and the National Trust of Australia (Victoria).

However, it has been compiled two to three years afterwards, and does not purport to be a literal record of the event. Some speakers produced no written papers, and are not included here, or produced papers subsequently. All have been given the opportunity to revise their material, and some have done this extensively, and some completely new material has been introduced in an attempt to make the document a more comprehensive and useful reference. The resulting papers provide important insights into Victorian stucco: this publication should provide a highly useful and practical reference for anyone interested in the topic.

An attempt has also been made to rationalise terminology, and a glossary is included. But the most contentious word has been ‘stucco’ itself. It is used to mean so many things that no complete agreement can be reached, and this can be a source of great confusion. The word is sometimes used, as in the title of this seminar, as a generic term to cover the whole range of plaster, lime and cement finishing. In reality, however, it has not generally been used in the last two centuries for internal plasterwork, although that was its primary meaning in Renaissance Italy. It has been used loosely in the twentieth century for various ornamental or textured finishes, but this is unhelpful, and is not recommended. In nineteenth century Australia, it was in general use for plaster, lime and hydraulic cement exterior finishes, but not usually for artificial or Portland cement, and not for castings. In the twentieth century most writers have referred to ‘cement’, ‘cementing’, ‘cement render’, ‘composition’, ‘compo’; a few refer to ‘Portland cement stucco’ or ‘cement stucco’; but very few describe a Portland cement finish simply as ‘stucco’.

We therefore recommend that any external finish be described by its material if possible, as in ‘hydraulic lime stucco’, ‘Hamelin’s mastic stucco’, ‘Roman cement stucco’. But as this information is commonly unknown for earlier work, where the word ‘stucco’ alone is used, it should be taken to mean external plastering in a material other than Portland cement. Portland cement finishes are better not called ‘stucco’ at all, but rather, ‘cement’ or ‘composition’, or possibly (where they are applied by trowel), ‘cement render’. As the matter is so controversial, we include at the end of this publication a series of brief extracts from British and Australian texts, which illustrate the use of the various terms.

The Heritage Council of Victoria has kindly taken on the funding and production of this publication.

Origins of Stucco

Miles Lewis

sources and precedents

the Renaissance

modern stucco

natural cement

artificial cement

conclusion

## Sources and precedents

Plastering is the secret craft. Until the 1890s, there was no solid textbook on the subject. Aspects like scagliola, though widely understood in general terms, were conducted according to the secret recipes and procedures of each practitioner. In terms of external rendering, I have never found any clear published description of the method of creating incised decoration before that of Barrie Cooper in this volume. It is unsurprising, therefore, that the greatest confusion has surrounded the use of the word ‘stucco’.

Many writers refer to the use of stucco in Egypt, Mycenae, classical Greece and Rome,1 and the Roman writer Vitruvius has likewise been translated as referring to stucco.2 But there is no Latin or other ancient word corresponding to ‘stucco’, and the most that can be inferred is that they are referring to some sort of plastering. The most relevant is what Vitruvius called albarium opus, a pure white lime coat to the surface of which crushed marble was added to give a marble-like external finish,3 used especially in the Achaean temples of southern Italy. Pliny also speaks of a mixture of refined lime with saffron, hard enough to be used even in floors and pavements.4 Later medieval and other recipes involve the use of carbonate of lime—generally burnt limestone or chalk—mixed with materials such as fig juice, eggs, blood, elm bark, hot barley water, and malt wort.5

There is plenty of evidence of ancient plastering: including many examples in Egypt and some in Mesopotamia. The albarium opus of the Achaean Greek temples has disappeared. In fact there is virtually no surviving plaster from the classical Greek period, but there is a great deal of Roman plasterwork surviving—varying from the delicate relief work of the underground basilica at the Porta Maggiore, Rome, to the crude interior finish of some of the tombs at Palmyra. There is then an interregnum, and very little survives in Europe until the Romanesque period, after about 1000 CE.

## The Renaissance

The word ‘stucco’ appears only after the Italian Renaissance, principally in reference to a material for internal modelling, and Papworth gives stuccatura as an Italian word embracing all sorts of interior ornament imitating carved stone.6 Bankart devotes a chapter to ‘The Stucco-Duro of the Italian Renaissance’, and this is also about decorative relief work, almost all of it internal (the exception being the Palazzo Podesta, Genoa, of 1563).7 Vasari refers to a stucco resembling that of Vitruvius, with a surface finished in marble dust.8 Various recipes survive from the Renaissance. One, used by the sculptor Jacopo de Monte San Savino, is described as ‘Admirable stucco for making and modelling figures for colouring and resisting water’:

Take of finely powdered travertine 5lb., and if you would have it fine and more delicate, take fine marble instead of travertine, and 2 lb. of slaked lime, and stir and beat them well together like a fine paste.9

The stucco known as marmorino was, similarly, given a marble effect by the addition of powdered seashells and travertine marble dust, and was pressed with a hot iron after being applied.10 It was also common in rural buildings in Italy to use intonaco or plaster stucco ruled in imitation of ashlar masonry, and this was done by Palladio in all of his country villas, the fabric of which is brick. Palladio’s walls were incised to suggest the joints of masonry, though these lines are much less perceptible today.11

Vasari credits Primataccio with executing the first stucchi in France,12 but he is referring to the artist’s elaborate interior plaster modelling at Fontainebleau, which is of no relevance to the present topic. Bankart refers to stucco as being introduced to England at Nonsuch Palace in about 1538, and this work was external relief modelling and sculpture, though not the sort of broad surface work now evoked by the term.13 It was carried out by Italians, including the brothers Luca and Bartolomeo Penni, summoned for the purpose by Henry VII.14 In 1666 Hugh May wrote of stucco still in the classical sense of a render surfaced in marble dust, or at least a good imitation of it:

If there be use of stucco, I have great hopes, from some experience already had, that there are English materials to be brought by sea at an easy rate, that will afford as good plaister as is any where to be found in the world; and that with a mixture of cheaper ingredients than marble-meal, which was the old, is now the modern way of Italy.15

Both Wren and Kent used plaster with marble dust added for internal carved decoration.16

Richard Neve, author of the first dictionary of building terms in English, or perhaps in any language,17 gives no definition of stucco, but he makes a reference to its use for sculptural work:

For figures, the last coat is made of plaster stone managed as marble or alabaster. Stuc ornaments are made of a composition neither too hard nor too soft, and then a prepared mould is pressed or struck upon it, and when removed, is cleaned by hand. – The moderns consider that plaster of lime and sand does not dry so soon as stuc for painting on, and being greyish is more proper than so white a ground for colours.18

Soon stucco, in something more like the modern sense, was to reach Britain. The Palladian revival of the eighteenth century gave rise to an interest in Palladio’s stucco surfaces, sometimes finished in colours such as ochre. At Colen Campbell’s ‘Mereworth Castle’, Kent, of 1753, both the house and the later pavilions were finished in ochre-coloured stucco in what was seen as the Italian manner. 
It is this type of Palladian stucco, covering broad surfaces, ruled to imitate masonry, and sometimes coloured with ochre or other pigment, which is the source of Australian practice. But it is ignored by British writers on plastering, who are more concerned with elaborately modelled work.

Thus, Millar and Verrall credit Robert Adam with introducing to England the use of ‘stucco externally to give brick houses the appearance of stone’.19 But Adam was later than Campbell, and I am not aware that he faced complete buildings in this way, though he certainly created frontispieces, pilasters and other elements in cement. He used some stucco in Hanover Square in about 1776 (Summerson suggests based upon Liardet’s cement). Wyatt used Higgins’s cement for stucco in 1779 as indicated above, and Nash used some sort of stucco in 1783.20 But the more extensive adoption of stucco in Britain follows the discovery of Parker’s and other hydraulic cements, and their use by architects such as John Nash and James Wyatt. Nash adopted Parker’s cement as soon as it was introduced in 1796, and used it until about 1820, when he changed to either Hamelin’s or Diehl’s mastic.21

There was also a lively vernacular tradition in Britain. Lime plaster was used externally in London in the reign of King John, and plastering or daubing over wattling and other infill materials was essential in half timbered buildings, which were the predominant type until the seventeenth century. Verrall reported that all those he had examined were three-coat work in lime plaster containing either chopped straw or, in better quality work, ox or horse hair. The surface was whitewashed, or occasionally painted.22 Such a material, based upon non-hydraulic components, depends heavily on the maintenance of a painted surface to protect it, and cannot simulate natural stone in the same way as the hydraulic limes and cements of better class work. But in Australia, as we shall see, that distinction is not so clear.

As the aim in the finishing of stucco is to simulate ashlar masonry, it was commonly ruled (either with a groove or with a line in crayon or pencil). William Atkinson had recommended as a dash coat a mixture of quicklime and sharp sand, coloured to imitate stone, which if properly done would not require new colouring but ‘improve daily with the mosses and weather stains’.23 His recommended colouring materials were yellow ochre and lamp black or ivory black, or even better ‘blue black’, prepared from charcoal (probably meaning the latter for the ruling of the ashlar joints).24 Apart from this he advocated a stucco made of slaked lime and clean sharp sand, which ‘if laid on with an uneven surface to give it the appearance of undressed stone, will produce all the desired effect, and look better than rough-cast’.25 The use of lime in these ways seems optimistic, especially in the English climate, though the mosses and weather stains should certainly have been achievable.

## Modern stucco

In England, which must be taken as largely relevant to Australia, ‘stucco’ was described in the eighteenth and the nineteenth centuries as ‘now a species of plastering, occasionally worked to resemble marble. One sort is made of lime, the other of plaster.’26 By the end of the century, it was said to be ‘a somewhat indefinite term, used loosely for various plastic mixtures in whose composition lime, plaster, or cements enter’. However, the four types which Millar described as being used in the south of England (common, rough, bastard and trowelled) were all based more or less on hydraulic lime, washed sand and/or grey lime putty.27 He distinguishes Portland cement work as something different from stucco, which had come into use in the mid-nineteenth century,28 though the examples he gives are earlier, including the Athenaeum Club, Travellers Club, and United Services Club.29

Verrall, however, uses the term ‘Portland Cement Stucco’ and devotes a brief chapter to it:30

By Portland cement stucco is meant something different from, and superior to, an ordinary mixture of cement and sand. The aim is to produce a material which will set with moderate rapidity, dry hard and give good protection, but which will be more plastic than ordinary cement mortar, and possessing reasonable retardation properties in setting, can be manipulated over a sufficiently long period to give freedom in obtaining decorative effects without interfering with ultimate or definite setting.31

An American text of the 1920s, Lowndes and Boyd, distinguishes three types of external stucco: lime, Portland cement and magnesite, though the boundaries were blurred, as the lime stucco might have a small amount 
of Portland cement, and the Portland cement stucco might contain a proportion of lime.32 Magnesite could not be mixed with either, and as it is not known to have been used in Australia (except as flooring) will not be further considered here.

## Natural cement

Major changes had taken place with the introduction of hydraulic ‘Roman’ cement, and then Portland cement. In the late eighteenth century a number of so-called cements, actually limes with pozzolanic additives, were developed in Europe. In both Britain and Australia there were some rock limes which by reason of their composition, particularly if the stone contained a proportion of clay, produced a material with some hydraulic properties. A true hydraulic lime cannot be slaked, will set even under water, and when used as stucco on the outside of a building will be able resist the weather. In Britain the best known type was the blue lias lime found in the west of England.33

The engineer John Smeaton used blue lias lime in the 1750s in the construction of the Eddystone Light, but added terra puzzulano, which was available, more or less fortuitously, from a Plymouth merchant.34 The addition of pozzolano and other materials to lime is a traditional practice, quite distinct from the manufacture of artificial cement. Such mixtures were developed to a high degree by Bryan Higgins, who published his results in 1780,35 and may conceivably have been influential in Australia. Higgins patented one recipe36 and licensed it to be used by the builder Samuel Wyatt, and the architect James Wyatt,37 only shortly before the latter was to form his partnership with James Parker in the development of natural cement. Wyatt covered a façade at 9 Conduit St, London, in Higgins’s cement in 1779.38

In 1774 Antoine-Joseph Loriot published his cement in the Mémoire sur une Découverte dans l’Art de Bâtir.39 This was followed immediately by an English edition that sold out: a success attributed by Eileen Harris to the facts that the invention was fully explained in the book but not protected by patent, and that the publication coincided with the London Building Act, 1774.40 Loriot’s ‘cement’ was in fact no more than a mixture of sand, brick dust and either quicklime or old slaked lime (according to his two recipes),41 and Higgins dismissed it entirely, apart from acknowledging that lime was at least a better ingredient than whiting.42 Higgins was promoting his 
own cement, which was at least the result of a process of experimental development, but it, in its turn, could not compete with the natural or ‘Roman’ cement discovered a few years later.

Roman cement was the invention, or more precisely the discovery, of James Parker of Northfleet in Kent, who found that septaria nodules found on the Island of Sheppey, or by extension other naturally occurring combinations of clay and limestone, would produce a hydraulic cement. Parker’s patent of 1796 provided essentially that this material should be burnt to a high temperature and ground to produce a stronger cement than any hitherto available,43 and one which could resist weathering and even had some capacity to set under water. It was manufactured and marketed by Parker in partnership with the architect James Wyatt. In France, comparable nodules were found at Boulogne, and a clay beneath this stratum was the only identified natural cement in the form of a soft deposit.44 Many other types followed. The principal British brands, according to Hurst, were Harwich, or Frost’s; Francis & Grellier’s, made at Millwall; Atkinson’s or Mulgrave, from Whitby in Yorkshire; Calderwood, from Glasgow; and Medina, from Hampshire and the Isle of Wight.45 But of these Frost’s at least is better described as an artificial cement, and is discussed in that context below.

Roman cement is in many ways the key to the Regency style. It was much used by Wyatt himself, and by his principal rival John Nash, as a way to conceal brick or other material and give it the appearance of stone, though ironically it was a failed exercise of this sort that bankrupted Nash at the outset of his career. It lent itself to the curves of bow windows and the pilasters, Greek frets and other adornments of the Regency. And it was the very material against which Pugin was to fulminate when he argued for a more ethical style:

Timbered fronts of curious and ingenious design are swept away before the resistless torrent of Roman-cement men, who buy their ornaments by the yard, and their capitals by the ton. Every linen-draper’s shop apes to be something after the palace of the Caesars ...46

## Artificial cement

The success of natural or so-called ‘Roman’ cement naturally led to experiments aimed at artificially matching or improving upon the naturally occurring proportions of clay and lime. In Britain Edgar Dobbs obtained a patent in 1810 for mixing chalk or limestone with clay, burning it, and grinding the clinker, which if done correctly in terms of proportions and temperature, could have produced an artificial or Portland cement.47 However, Dobbs specifically avoided vitrefaction.

In France L J Vicat had already succeeded in creating:

a factitious Roman cement by making bricks with a pasty mixture of 4 parts of chalk, and 1 part of dry clay, drying, burning and grinding them ... its efficiency is somewhat doubtful; though it has, for want of a better substitute, been much employed in Paris.48

According to Skempton the description of it as ‘factitious Roman cement’ is an exaggeration, for what Vicat created was an artificial hydraulic lime, though this was in itself sufficient to encourage others to experiment with artificial cements.49 Skempton may or may not be right, but certainly N E Pelouze, writing in 1829, proposed the creation of an artificial cement to reproduce the qualities of the Roman cement made by Parker. He clearly distinguished hydraulic lime [chaux hydraulique] as a different substance, and acknowledged Vicat as the pioneer in the field.50

Vicat published his Recherches Expérimentales in 1818, followed by Résumé des Connaissance Positives Actuelles sur les Qualités, &c, in 1828. The London builder James Frost went to France to study Vicat’s cement, which was now in production at Meudon,51 then took out a patent in 1822 for his ‘British cement’, which was largely inspired by Vicat.52 In 1825 Frost established a factory at Northfleet (Swanscombe) to manufacture it,53 and then in about 1830, by increasing the clay content from 15% to 30%, succeeded in producing what Skempton calls an artificial Roman cement.54 However, A C Davis was later to claim that Frost had produced what we now understand by the term ‘Portland cement’.55 These differences are impossible to resolve, given that contemporary records are limited and that Portland cement had yet to reach its canonical form. In 1833 Frost retired to the United States, and sold the factory to Francis, White & Francis, who in turn transferred it over the next four years to the control of White & Son.56 Later still the company became J Bazley White & Sons,57 then by 1853 John Bazley White & Brothers,58 whose cement was specified for Parliament House, Ottawa, in 1859,59 and exhibited at Sydney in 1879, both in its own right and in the form of W H Lascelles’s prefabricated cottage.60

Portland cement is more generally regarded as the invention of Joseph Aspdin, who is claimed to have made an hydraulic cement for the first time in 1813, by lightly calcining a mixture of clay and limestone, substantially the same as Vicat’s, but significantly different from, and inferior to, what was later called Portland cement. A C Davis was to refer to this as being ‘ground hydraulic lime’,61 but Aspdin called it ‘Portland’ cement, from a supposed resemblance to the appearance of Portland stone. He patented it under that name in 1824,62 and established a factory in 1825, subsequently run by his elder son, James. In 1828 Marc Brunel used Aspdin’s cement, for the first time on a major scale, in the construction of the Thames Tunnel.63

The systematic experiments of Major-General C W Pasley at the Chatham Naval Dockyard, from 1826 onwards, grew largely from the experiences of Vicat and Frost, and advanced the understanding of cement out of all measure. Most of Pasley’s experiments were conducted using White’s cement, the successor of Frost’s, which at this stage was made of mixed Harwich and Sheppey nodules, and would not qualify as Portland cement.64 An artificial cement was potentially much better than a natural one because the optimum proportions of clay and limestone could be selected, but its development was retarded by the fact that early experimenters, instead of calcining it to the point of incipient vitrification, tended to assume that this was undesirable, and even to sort and remove any vitrified lumps.65 The first certain evidence of the material being burnt to near vitrification, and thus being effectively Portland cement in the modern sense, is at White’s factory some time after 1840.66 It may have been as late as 1845, for it has also been claimed that at that date Isaac C Johnson, works manager of J B White & Sons, first burnt the materials at a high enough temperature to produce what was later understood by the term ‘Portland cement’,67 and in particular realised the importance of grinding and using the clinker rather than discarding it.68

By the 1840s, when Aspdin’s patent had expired, a number of ‘Portland’ cements were on sale, one of which, ‘Pulham’s Portland Stone Cement or Artificial Stone’ was claimed to have been first used in about 1821, and likewise to have been named from its close resemblance to Portland stone in colour, hardness and durability.69 Gwilt dates the appearance of true Portland cement to 1843, and refers to it as being made from the mud of the Medway mixed with chalk, and the ashes of former makings, and calcined at a high temperature almost to vitrification. This seems to be a reference either to the cement now produced by Maude & Co, or to the development work undertaken by Pasley.70 Late in 1843 Maude & Co announced that they had made arrangements with Joseph Aspdin’s younger son, William, to manufacture an improved version of Aspdin’s cement at Rotherhithe. It was explained that Aspdin’s original cement, though generally regarded as superior, had been used only to a limited extent in London because of the cost of transport.71 William Aspdin entered the partnership of Maude, Jones & Aspdin at Rotherhithe,72 and a remark in 1845 that ‘Maude’s’ cement had not been in use long enough to assess it serves to confirm that they were now producing a different material.73 William Aspdin was later a member of Robins, Aspdin & Co,74 but whether this company was the legal successor of Maude, Jones & Aspdin is unclear. By 1855 William Aspdin’s Patent Portland Cement was being made by Aspdin, Ord & Co.75

Other makers had entered the market as well, and by 1852 there were six in all:

Joseph Aspdin, Wakefield

- J B White & Sons, Swanscombe

Robins & Co, Northfleet

Charles Hilton, Faversham

I C Johnson, Rochester

Aspdin & Son, Gateshead76

By 1853 they included also Thomas Freen & Co of Wouldham-on-the-Medway; R Greaves, near the Avon, who sold through Charles Richardson of London; and James Weston of Millwall, Poplar.77

The first Portland cement manufactory was established in France in 1840 and the first in Germany in 1853 at Zülichow near Stettin, by the brothers Bleiptrene,78 coming into full production in 1855. Others soon followed, and although they initially modelled their works upon British ones, the Germans then introduced great improvements, and by the 1880s their cements were 
50% stronger than the British cements.79 Frost established himself in New York, and by 1841 succeeded in making on a commercial scale a fine greyish-white cement, which he had been able to achieve only experimentally in England, and which he claimed was three to six times as hard as marble.80 This venture seems nevertheless to have died, for it is reported that production did not begin in the United States until the 1870s, and even then the majority of the market was supplied by imports from Britain and Germany.81 The first of the next generation manufacturers was David O Saylor at Coplay, Pennsylvania, from 1871.82 It was more than another decade before manufacture began in Australia.

The most substantial guide to cement rendering practice is William Millar’s Plastering Plain and Decorative, of 
1897, and particularly his section of ‘Methods of Working Portland Cement Façades’, which deals with mixtures, application and modelling.83 Verrall recommended the choice of a fine grained, slow setting Portland cement, mixed with no more than 20% hydrated lime, and the desired amount of washed sand and any coarse aggregate (one part of cement to three of aggregate being a typical ratio).84 Lowndes and Boyd accept ordinary Portland cement except where a white stucco is required, when one of the white cements available on the market is 
used in conjunction with white sand or marble dust.85

## Conclusion

This is a field in which there are few sharp distinctions and few clear definitions. But one can say that a change took place at different times in different places. The traditional exterior finish was a predominantly sheer surface render based on hydraulic lime or natural cement. It was commonly ruled and often tinted, but the use of marble dust or similar material had largely ceased by the nineteenth century. If there was modelling of any complexity it was in some other material, such as Coade stone (a terra cotta), one of the various artificial stones, 
or Portland cement.

The new treatment, beginning in about 1840, used Portland or artificial cement. It was a stronger, harsher material, sometimes quite dark in colour and therefore less readily tinted. It was durable and could be modelled in situ or in precast elements, which could be incorporated homogeneously. If the older tradition is called ‘stucco’, then it is better to distinguish the newer one as ‘cement’, even though many writers are not so clear.

Miles Lewis, AM, FAHA, is an architectural historian specialising in the cultural history of building and in vernacular architecture. He is a professor of architecture at the University of Melbourne, author 
of a number of books and papers, and most recently editor of Architectura (London and New York, 2008). 
His web site is www.mileslewis.net/

Stucco: Materials and Finishes

Donald Ellsmore

abstract

introduction

the nature of Victorian stucco

lime and the natural cements

artificial cements

external plasters in early Australian 
building practice

stucco revival

stucco materials and application

stucco layering

surface textures and finishes

stucco materials

natural and applied colour

paints and other applied surface finishes

regional and periodic colour variations

conclusion

## Abstract

During the nineteenth century and early part of the twentieth century, brick and stone buildings were often finished at least in part with external decorative plastering, sometimes referred to as stucco. This form of decoration on the facades of prestigious buildings achieved a high level of sophistication during the boom period in the colony of Victoria. Various forms of lime and cement-based plasters provided the means of decorating entire facades or selected parts of buildings with elaborate detailing that replicated the appearance of finely worked stone. Several different materials were employed to achieve the subtle colouring of stone, and there are some regional variations.

Surviving examples of Victorian stucco include some that have retained their original appearance, although these are usually somewhat altered by the effects of weathering. Others have been painted many times over, and some have been smeared over with sand and cement coatings—thus concealing the fine detailing and subtle colouring of the original stucco finishes. This introduction to the materials and finishes of Victorian stucco, reviews documented trade practices and discusses the types of materials and finishes, as a prelude to the more detailed discussions that follow. It includes some observations about the surviving evidence of past practices to stimulate discussion and encourage further research on this important subject—even though they are yet to be 
fully analysed and understood.

## Introduction

As has been discussed elsewhere, the historical record is not clear or consistent in the matter of the term ‘stucco’. The term appears to have many meanings, or sometimes little meaning at all—it has been applied to a range of different materials and techniques over time. It is Italian in origin, and originally described fine quality plaster executed in lime putty and hand modelled in situ to produce low relief decorations on walls and ceilings. Strictly speaking therefore, the term stucco should apply only to the very fine surface finishes of multi-layered interior plaster work, but in English usage and in common Australian usage it is also used in relation to exterior plasterwork.

There is evidence that the term stucco was used to describe both exterior plasterwork in general, and the final layer in a three-coat external plastering system, as early as 1836 in Australia.86 The term generally applied to any or all forms of exterior plastering,87 irrespective of the nature of the final finish or the number and composition of the layers beneath it.

William Millar, in 1897 gave a detailed account of nineteenth century British plastering practices in his comprehensive Plastering, Plain and Decorative (still considered by most traditional plasterers to be the plastering bible). He described four types of stucco in common use in London and the south of England, and stated that the only difference between the stucco and traditional three-coat internal plasters was the setting coat—the first-coating and the floating being the same for all.88 Millar defined stucco as applying loosely to ‘various plastic mixtures in whose composition lime, plaster or cements enter’,89 thus embracing all the materials used in plastering. What is very clear, from Millar and from others, is that the final appearance of the stucco was usually intended to resemble stone.

The 1929 twelfth edition of George Mitchell’s Building Construction, states that external plastering is usually known as stucco.90 James Nangle’s Australian Building Practice states that external plastering ‘… resolves itself into either the covering of the wall or exterior of the building with the rendering of cement mortar, called stucco, or else the dressing of all base courses, sills, mouldings etc.’91 His diagrams label the former as ‘cement stucco’.

In England, various forms of lime and cement plasters had been used occasionally from at least the sixteenth century as an economical medium for modelling external architectural features in place of carved stone. Robert Adam greatly developed this in the second half of the eighteenth century, and it was to be integral to the Regency style, as Lewis has discussed above. It satisfied the taste for smooth, evenly coloured house fronts at about one quarter the cost of stone.92

In North America and Australia, lime and cement stuccoes were applied to masonry and to selected parts of buildings, even timber buildings, from the nineteenth century until quite recently. In Australia the most sophisticated examples of stucco are found on Victorian Italianate and Boom style buildings and on some of the grand country villas and mansions—especially those constructed on pastoral runs, and in the goldfields towns of Victoria. These examples were described in contemporary reports as ‘cemented’, ‘cement fronted’, ‘plaster fronted’ and even ‘plasterers’ Corinthian’.93 The term stucco did not appear to suit the aspirations of the era that witnessed the proliferation of Portland cement-fronted buildings although it was the more common term in use before the widespread use of Portland cement and it is still the term that is preferred by some.

In his chapter on stucco in Good and Proper Materials – the Fabric of London Since the Great Fire, Frank Kelsall volunteered that:

stucco can be defined as some sort of composition which can be applied to the whole or part of a housefront and can be used equally for a plain covering or for running mouldings and forming ornament.94

Stucco was used increasingly in speculative brick-built structures in England, although it was not universally admired, and was not so commonly adopted where there were good reserves of building stone and the skilled labour to work it. Where stucco was extensively used, as in London, it began to lose favour with many builders and their clients by the 1860s. However, this was not so in Australia, in Melbourne and the goldfields towns in particular, where stucco provided the means of achieving aesthetically sophisticated architectural finishes despite the general shortage and high cost of labour. It provided the means of finishing brick buildings with beautifully executed finishes when stonework was difficult to obtain. The fashion for stucco diminished in the early twentieth century as interest in applied exterior decoration of all forms waned.

## The nature of Victorian stucco

Stucco had several intrinsic advantages, including the ability to improve the appearance of inferior brick and stonemasonry, and some even attributed to it superior thermal and waterproofing qualities.95 However, it was not considered to be superior to well-made brick or stone surfaces in the Australian context. During the boom period of the second half of the nineteenth century, stucco afforded the ability to achieve high quality building finishes within the constraints of limited trade skills and building stone resources.

In the early years of the twentieth century, stucco provided the means of achieving the sinuous lines and eclectic motifs of the Art Nouveau and Federation styles in exterior relief decorations. It even provided a means to decorate early forms of reinforced concrete construction, which were otherwise plain and utilitarian in their appearance. A simple definition of stucco that would appear to suit these later forms of exterior plasterwork in the Australian context is ‘an exterior plaster finish composed of Portland cement, lime, and sand, mixed with water, used for decorative work or mouldings’. However Burden who penned this definition in 2003,96 went on to refer to it as being ‘usually textured’ (which is a misconception). Other references to stucco refer only to mixes of sand and Portland cement, usually in the proportions of 3:1 containing no lime whatsoever, whilst some references to external plasters make no reference to the term stucco at all.

In the matter of Portland cement and Victorian stucco, the papers that follow make two important points and they are worth repeating here to remind readers about the true nature of the material known as ordinary Portland cement, or OPC. First, modern Portland cements are much harder and more uniformly grey in colour than earlier forms of Portland cements (which were available in a range of subtly different colours and were sometimes specified with care to attain contrasting colours on the elements of building facades). Second, the early and varied forms of Portland cement were less hard and more compromising than modern forms, which are more refined in their manufacture. The concept of stucco mixes composed of Portland cement and sand today is challenging because of the growing awareness of the deleterious effects of Portland cement-based plasters on weak masonry surfaces, especially in the presence of moisture and salts.

In recognising the widespread use of Portland cement following its successful introduction in the mid 1850s, Millar advised that:

Portland cement is unquestionably the best plaster material for resisting vermin, damp and fire. In fact, of all the mortars or cements that have been used for plastering the exterior wall surfaces of buildings, Portland cement is unquestionably the best plaster material for this purpose produced in this century or any other.97

Nangle was of the same opinion—that Portland cement and sand together produced the best mix for external plastering, and that even the addition of lime water, to make it work fat, was to be condemned.98

Notwithstanding these opinions, there have been many instances of use of materials other than, or in addition to, sand and cement in stucco. It is therefore useful to return to earlier examples and references to understand how stucco evolved as a material, and how practices were applied in Australia.

## Lime and the natural cements

Before Portland cement became accessible in the second half of the nineteenth century, lime was the most common binder used in mortars. It is still used extensively in mortars and plasters, and is recommended for many building conservation applications. Lime-based mortars are now widely acknowledged as generally superior to cement-based mortars and plasters in repairing heritage places, mainly because they are more compatible with aged, weakened, fragile or porous building fabric, including sedimentary building stones, traditional brickwork and soft bedding mortars.

Common limes harden by the process of carbonation, which occurs when the calcium hydroxide of fresh lime combines with carbon dioxide in the atmosphere in the presence of water to form calcium carbonate. The process produces porous mortars and plasters that are suitable for many types of conservation works and repairs, although their setting is relatively slow, which can be a disadvantage in external plastering.

Hydraulic limes found a use in traditional forms of external plastering because they enabled plasters to set more rapidly without any need for contact with the air. Even more importantly, in external work, they could resist erosion by water, to an extent which common limes could not (and natural cements were even better in this respect). Natural hydraulic limes were produced by burning argillaceous or siliceous limestones and are composed of calcium silicates and aluminates, together with calcium hydroxide.

Roman cement was a natural cement discovered and patented in 1796, more than 20 years before Portland cement. Its development arose from a search for materials to use in finishing London buildings in ‘stucco or composition resembling stone, more durable than the common sort’.99 It was produced from marls or septaria (limestones containing more than 25% clay) and was fast setting, brown in colour, and hard when set. The derivation of the name, Roman cement, was an attempt by its inventor to draw a link between the new material and those of proven quality from the ancient world. Roman cement was used in England in Regency and early Victorian stucco either as the principal binding agent or mixed with lime and sand, although the proportion of sand in such mixtures was of necessity small because Roman cement had a poor affinity with it. This characteristic made it more suitable for casting decorative elements than for flat floated and trowelled surfaces. Roman cement was imported in kegs to Australia and began to appear in construction in the 1830s. However, it was superseded by Portland cement when that material was found to have superior qualities in many situations, although some places appear to exhibit examples of both materials being used together.100 The use of Roman cement in Australia was relatively short-lived.

## Artificial cements

Early attempts to reproduce natural hydraulic properties by artificial means led to the development of hard, fast-curing cements, which had obvious benefits in the production of decorative external plastering, and in the production of ornate mouldings in particular. Portland cement was developed in Britain where an early form 
of it was patented in 1824. Its name derives from its similarity in appearance to Portland stone. The original Portland cement differed from natural hydraulic lime in only minor ways, had similarities to Roman cement, and was used only to a limited extent. Portland cement only came into favour after the 1840s when it was worked 
at higher temperatures and marketed as ‘Patented Portland Cement’.

Some of the early forms of Portland cement were greenish and brownish with tints of grey, and not as strong as the modern forms. Portland cement today has a distinctive, uniform light blue grey colour and very high strength when used in combination with suitable aggregates. Today this modern form of Portland cement is fired at very high temperatures and is used almost universally in the building industry in all forms of concrete, mortars and common external renders.

Portland cement hardens and sets relatively quickly in most environmental conditions, by a chemical process of gel crystal formation—thus making it a very useful material for external plastering. However, the setting process involves the loss of water and shrinkage, which can be a hindrance in fine work and in repairs to heritage building fabric. In addition, it is now understood to be incompatible with many forms of masonry under some conditions. Portland cement plasters are harder, less porous and less permeable than lime-based plasters, and they can be a source of sulphates, which may contribute to the salt decay of traditional brick and stone masonry.

## External plasters in early Australian building practice

When Australia was settled by Europeans there were—at least near Sydney—very few readily accessible sources of limestone for manufacturing limes or cements, so colonial builders resorted to using clay as a binder in their mortars and plasters. Clay was readily obtainable, as were sands of various types. Aboriginal shell middens and live oyster shells were abundant near the early port settlements, and were found to be suitable for calcining to produce building lime—although the early settlers rapidly depleted the resource. Clay, sand and primitive forms of lime (or combinations of these materials with other binders) were employed in vernacular buildings and in more refined colonial buildings.101 Early records refer to various natural and artificial binders used to improve the properties of mortars and plasters and to counter clay shrinkage such as animal manure, blood, various natural forms of reinforcement and fish and shell products.

The early settlers found suitable materials for the limited production of building limes further afield, in the form of deposits of shells and natural limestone. They could burn and slake these to produce both common and hydraulic building limes—materials that were used in both sophisticated and primitive structures in most parts of Australia until the late nineteenth century, when the Australian production of Portland cement commenced.

Considering the limited availability of imported materials in the Australian colonies in the first half of the nineteenth century, it is not surprising that the materials used in external plasters differed from those used in Britain at the time. Nevertheless, Roman cement and early forms of Portland cement were used here during that period. We also know that J C Loudon’s Encyclopaedia of Cottage, Farm and Villa Architecture had some currency in the colonies, and that it would have guided colonial builders in a wide range of building matters. Loudon was of the opinion that in general, wherever good fresh lime and clean sharp sand could be had, an excellent cement might be formed. He wrote (in 1833, prior to the general availability of Portland cement) that:

The Cements for Stuccoing are chiefly the Roman cement, of which there are two kinds common in Britain, Parker’s and Mulgrave’s; the Puzzolano; the tarras; the gypsum; the mastic; Frost’s cement; the metallic cement; and Bailey’s composition… A very hard and durable cement may be formed of stone lime recently burned, and, immediately after being slacked, mixed with clean sharp sand. This about London is called Bailey’s composition… The usual proportions are three of sand to one of lime.102

He also reported that the main purpose for stuccoing the fronts of buildings, or, as he described it, ‘covering the outside walls of cottages with cement’, was generally to imitate stone.103 The need to imitate the natural colour of stone would have been met in the colonial era by the application of some form of natural colouring to either or both the stucco and its surface.

It is well documented, and clearly illustrated in surviving works, that Portland cement began to overtake all other forms of cement for high-grade work after it was imported from the middle of the nineteenth century, and locally manufactured material from the end of the century. However, in Ireland and also to some (unquantified) extent in Australia, lime and Roman cement maintained their value in external plastering until about the 1870s. The English architect and writer, Joseph Gwilt, noted the Irish use of lime:

Stucco work, as it is called, and as executed daily in Ireland for outside work, consists of their roche lime, slaked for 3 to 4 months, mixed with sand and worked with trowels… stands the weather as perfectly as Roman cement.104

Lime was often used in conjunction with Portland cement, which gave accelerated setting times and reduced working times. Although soon overtaken by Portland cement, lime continued to be used in many applications, no doubt because of the higher cost of imported cements, but also because its inclusion in plaster mixes made them more workable. The combination of lime with Portland cement and sand in Ireland went by the name ‘bastard stucco’. But curiously, in the south of England, according to Millar, bastard stucco was a final coat of 2½ parts of washed sand and 2 parts of chalk lime putty which was normally trowelled off and brushed to give it a stone look, and was better in quality than ordinary setting.105

Millar also noted the acceptance and success in England of Portland cement, supplanting stuccos. He observed that, by the end of the nineteenth century, there were miles of streets in the West End of London where nearly the whole of the facades were plastered with either Roman or Portland cement.106 Roman cement had been in general use from the 1790s for plastered fronts but, according to several commentators, after a few years of exposure some showed signs of decay, allowing other, more durable forms of cement to overtake it. Upon the introduction of Portland cement, plastered fronts again became fashionable in England, and their popularity in Australian cities and towns grew substantially during the last decades of the nineteenth century.

Mitchell wrote in 1936:

Lime is now almost superseded by Portland cement [because of its superior strength, uniformity and speed of application]. The general proportion for both rendering and setting coats is 1:3 Portland cement to clean gritty sand.107

The ratio of 1:3 cement to sand quoted by Mitchell derives from the volumetric equation of 1 part of voids in every 4 parts of clean dry plastering sand. The role of sand in solid bulk plasters is to overcome shrinkage—therefore the aim with mixes of 1 part cement to 3 parts sand is to replace the voids completely to achieve a homogeneous mix that would set as a solid mass with minimal unfilled voids. Of course, tradesmen, were aware that the properties of sand varied from place to place, 
and they adjusted their mixes accordingly to obtain the best finishes. Even so, specifications of 3 parts sand to 
1 part cement are still most usually specified.

## Stucco revival

A factor in the brief, mid-century English popular revival of stucco was the construction by Queen Victoria and Prince Albert of a large villa on the Isle of Wight (‘Osborne’).108 The building of this fully Portland cement-faced unpainted Italianate villa inspired a wider use of stucco, especially in rows of terrace houses in London. Once it was chosen by their queen and her consort, stucco suited the aspirations of the emerging middle classes. The impact of the construction of Osborne can be seen in the construction of stucco fronted Italianate villas and town houses throughout the British Empire.

The stuccoed Italianate style of Osborne and other British examples was transferred to Australia, and to Victoria in particular where gold and pastoral production brought wealth and a desire by the nouveau riche to build and decorate in the fashionable London style. We therefore can find very fine examples of high quality stucco in all the major Australian cities and regional towns, and on wealthier rural estates. A high proportion of the stucco work of the era is commonly believed to have been executed in Portland cement, although recent research and a growing awareness of natural and hydraulic limes is causing a re-evaluation of the range and extent of materials used.

## Stucco materials and application

Although the historical record leaves little doubt 
about the widespread use of Portland cement and 
sand mixes, their re-use would be a cause of concern 
to many in conservation circles today. For, although 
3:1 mixes of sand and Portland cement might be authentic at some places, the use of such strong mixes could cause problems. Modern Portland cement and sand mixes are sometimes incompatible in colour, texture and strength and they have a tendency to shrink and craze as well as to promote the movement of moisture and the concentration of soluble salts that can damage masonry. This does not mean that the past use of such mixes was wrong, but it may mean that it would be wrong to re-use them today. The sand and Portland cement mixes of the past were in various ways different from those in use today. In addition, it also seems that the aging process causes the fabric of stuccoed buildings to change over time in subtle ways, which make it unlikely that modern Portland cement and sand mixes would blend satisfactorily with the original finishes.

### Stucco layering

The historical record throws up some inconsistencies in the methods of application of stucco. For example, when we examine some places where stucco has failed and delaminated we can see that it was applied in layers in accordance with Millar’s recommendations—sometimes in three or more coats. However, some other applications appear to be homogeneous—possibly single applications. Furthermore, some of the sound stucco is so hard that it resists sampling of the material for analysis. It is clear that the traditional three-coat plastering system referred to as ‘render, float and set’, or ‘render, float and stucco’, did not always apply to external plastering. The use of Portland cement in particular overcame the need to build up in layers as in the traditional method. Sometimes, Portland cement plasters were recommended to be applied in two coats, or occasionally only one. Modern cement renders are commonly applied in one application, facilitated by the use of additives to reduce shrinkage during setting.

In the traditional three-coat method, the purpose of the first rendering coat was to deal with unevenness in the form and porosity (known as suction) of the substrate, and to provide a uniform surface to receive the floating coat. The floating coat on flat surfaces brought the plaster to the state of being smooth and even, and was finished with a wooden float. The final coat was then worked on top of the even surface to create the desired quality, colour and texture of the finished stucco.

The number of coats appears to some extent to have been a function of the nature and condition of the substrate, and also to some extent determined by the required final finish. Rough masonry surfaces with uneven suction could not be successfully stuccoed without building up the layers to overcome this unevenness. Finer finishes also required more layers to achieve a high quality result—whereas modern machine made bricks and cement mortars provide a uniform surface suitable for rendering in a single application, usually of sand and cement.

Nangle recommended two coats, or sometimes only one, and that the thickness should be no less than ¾ inch (19 mm). Others acknowledged that two-coat work was common but considered three-coat work better. The first coat should the strongest, and he recommended that each coat should be allowed ample drying and shrinkage time before the next was applied, and that the render coat should be scratched to provide a key for the following floating coat. This was sometimes called the ‘scratch coat’. There were various recommendations for scratching surfaces, and a four or five pronged set of cut and sharpened laths was sometimes illustrated for this purpose. However, Millar argued persuasively that a single lath should be used to produce the best keying for the following floating coat, and that this did not require any scratching in preparation for the final setting coat of stucco.109

### Surface textures and finishes

Nangle recommended that the final coat should be finished with a steel trowel, but others advocated either a wooden float or a felt-covered float to achieve a finish as near as possible to the texture of stone. For example, Mitchell advised that textured finishes to represent stone surfaces were worked best with a felt-covered hand float.110 This is largely consistent with Millar, who described the four different types of finishes used in London. It is clear that the choice of finish was based on the location, desired appearance, amount of worked decoration and the nature of the stone being emulated. He acknowledged that some of the terms used to describe these different types of stucco were only used by workmen, and the use of these stuccoes by 1897 was to a great extent superseded by Portland cement for exterior work, and Parian and other white cements for interior work. 111

According to Millar, ‘common stucco’ was preferred for exterior work, comprising 3 parts of coarse sand to 1 of hydraulic lime, to which a small portion of hair was added. It was laid in a similar way to ordinary rendering in one coat, and the surface finished with a hand float. ‘Rough stucco’ was used for plastering churches, corridors, and entrance halls—to imitate stone. The work was floated with ordinary coarse stuff, and then set with stuff composed of 3 parts of washed sharp sand and 2 of grey lime, not chalk. When it was to represent ashlar masonry, the surface was set out with lines to imitate ashlar stonework. The staining of the stucco to represent the colour of stone was achieved by diluting sulphuric acid (oil of vitriol) with water, and mixing with it liquid ochres and other colours to the required tints. The setting stuff of rough stucco could also be mixed with the ochres before application.112

Millar considered the ‘bastard stucco’ he described to be somewhat better in quality than ordinary setting. The final coat of bastard stucco was composed of 2½ parts of washed sand and 2 parts of chalk lime putty, all trowelled off and brushed to achieve the desired finish.113 ‘Trowelled stucco’ was generally used for work that has to be subsequently painted. The stuff for the finishing coat was composed of from 2½ to 3 parts of washed sharp sand to 2 parts of chalk lime putty. The sand was not as fine as that used for ordinary setting, being washed through a sieve having about 12 mesh to the inch, and the finish was worked to a near gloss with the trowel. When dry, the gloss apparently went off, leaving a fine surface ready for painting.114

Millar also described what he termed ‘coloured stucco’, which was used in Italy to execute lime stuccos in colours, by mixing various oxides in the lime. These were the same colours that were used for internal coloured setting coats; suitable also for sgraffito and concrete.115

It seems likely that all the finishes described by Millar were used in Australia, and that some further focussed research would identify examples of these. However, given the diversity of the Australian workforce in the period, it is unlikely that there would be a high degree of parity between the finishes described by Millar and those used here.

In conservation work today, when Portland cement mixes are used in repairs adjoining aged finishes, they are rarely visually compatible. When modern sand and cement mixes are finished with a wooden float, there is often an undesirable visual incompatibility between materials—either because the original finish might have been another type, or because superimposed layers of paint finishes have severely distorted the appearance of the original surfaces. Ways of overcoming this problem (such as removal of all paint layers prior to repairing the stucco) are rarely simple. The incompatibility that can be observed in repair works often leads to the application of paint finishes that are not necessary for any reason other than to conceal the repairs. The application of impervious paint finishes usually has long-term conservation implications.

### Stucco materials

On some aspects of stucco all the main authorities seem to agree whereas physical evidence reveals a somewhat different truth. For example, all agree that sand should be clean, sharp and well graded, yet close inspection of weathered external plastered surfaces sometimes reveals surprising inclusions in the plaster mixes, including shell, unslaked lime particles, cinder and very large sand particles (or fine gravel). All of these inclusions appear to be contrary to best practice, yet the evidence is that they have lasted very well. No doubt, some of these inclusions impart positive qualities to the base layers and assist in overcoming problems such as shrinkage. However, the top layer was usually made with fine sand and pure lime or cement to achieve the desired uniformity of appearance and weatherproofing properties.

The fine material in stucco surface layers has a major influence on the workability, appearance and strength of the finished work. The fine aggregate should be always clean and free from silt and clay because the presence of these would increase the water demand of the wet plaster and reduce its dry strength and durability. Fine aggregates consisting of round (non-sharp) particles produce weaker mixes than those containing angular particles, since angularity allows the particles to lock against each other.116

Lime putty—the form of lime used in traditional stucco mixes—was produced by slaking rock lime with water and leaving it to stand for a long period. The length of time needed to be sufficient for the lime to fully form calcium hydroxide, without any unslaked portions of calcium oxide (which could later cause weaknesses and disruptions in the surface finish). In the past, it was commonly thought that well aged lime putty was superior, although some authorities considered fresh slaked lime to be better. Recent research indicates that freshly slaked lime is no better than lime putty which has aged,117 and that there is no benefit in leaving the lime to slake for months and years as was sometimes done in the past.

There is little information on how changes in the use of Portland cement have influenced stucco, but at the time it was introduced it was generally conceded that ordinary Portland cement had an unattractive colour, which could be rendered pleasing by the addition of pigments or by employing sands of various tints.118 The amount of pigment should be no greater than 5% in any mix.

White Portland cement—sometimes specified today in conservation work to avoid the unpleasant grey look of ordinary Portland cement—differs physically from the grey form only in its colour, although its manufacture is significantly different from the grey product. Apart from 
its purer colour, it does not appear to have any benefits.

### Natural and applied colour

Lime tended to allow the natural colours of the sand to show in the cured stucco, as noted by Loudon:

Where the cement used… is lime and sand, it will resemble stone with little or no colouring matter added; but where Roman cement, or Puzzolano, or tarras, is used, the colour, after being laid on, will be dark, and the cement must therefore be brought to a stone colour by washing it over with washes, composed in proportions of five ounces of copperas to every gallon of water, and as much fresh lime and cement (to which some add tallow), as will produce the colour required. The copperas, or sulphate of iron, oxidises with the atmosphere, and produces 
a reddish tinge.119

Copperas, was mentioned by many as a suitable colouring agent for stuccoes and also for fixing other mineral pigments in stucco mixes. It was by far and away the most commonly recommended colouring agent throughout the entire period covered in this discussion.

In the following paper, Lewis examines various methods that were used to impart colour to stucco, including the addition of pigment to mixes to offset their inherent greyness, careful selection of the types of sand and cement, and the application of colouring to the surface either during or after the finishing process. Since Portland cement derived its name from its similarity to Portland stone, it is obvious that natural Portland cement stucco would not suit the purposes of imitating different sorts of Australian building stones without adjustment. Portland stone was never a suitable model for Australian buildings, although it was used very carefully and deliberately to achieve the desired look in some situations.120 Nevertheless, Portland cement, like earlier types, sometimes was considered quite suitable to be left in its natural colour, provided the selection of sand and cement was carefully specified. This is borne out in field research where the warmer colours of some nineteenth century stuccos exhibit the presence of coloured sands.

Millar summarised the means he encountered to colour Portland cement facades, including the modulation of those facades by adjusting the colours of the different cement parts:

[Elements] were varied in colour alternatively by using a rich yellow pit sand from Gilmerton for some, and a grey river sand for other. Red sand and brick-dust is used for a similar purpose, also for colouring cast concrete. Bullocks’ blood mixed with cement has been used to obtain a resemblance to red brick. Earthy stains are not as durable as mineral oxides; they also tend to weaken the cement, whereas mineral oxides have a reverse tendency. Manganese, or manganite, is also of a suitable nature.121

The warm colour of the popular Caen building stone from the north of France could be achieved by mixing yellow oxide and red oxide in the Portland cement plaster mix. Dark red colours and buff stone colours could be achieved by varying the proportions of the same mineral pigments. Millar concluded that coloured cement or stucco would last as long as the work, whereas if Portland cement finishes were coloured on the surface only, the colour would soon wear off.122

## Paints and other applied surface finishes

Millar’s predictions are born out in the Australian context where a careful examination of the apparently unpainted surfaces of stucco-finished heritage places usually reveals that those places were, at some early time in their history, coated with coloured washes. Other finishes were common but it is not easy to determine whether they were painted early in the life of the buildings, or later; or whether colour washes were present before other coatings were applied. Even when an oil paint was applied as the first finish, in accordance with some recommended practice, the paint could not have been applied until the stucco was fully dry. The drying out process could take months or, sometimes, years.

Oil paint is not a logical finish for external stucco when it is intended to have a stone look. Oil paint has a natural gloss, which cannot be readily suppressed without impairing the properties of the paint. Furthermore, the application of oil paint is arduous, and three-coat work (the minimum that would suffice on stucco) would be costly and time consuming. Nevertheless, the description by Millar of ‘trowelled stucco’ for work which would be subsequently painted, indicates clearly that some stuccoes were intended to be painted with conventional oil-based house paints, or perhaps with one of the newly developed washable distempers, very soon after the plastering work was completed.

Colour washes, by contrast, could be applied immediately to fresh render in a single coat, in various weather conditions, and they imparted what many considered to be a more convincing stone look. However, as Millar and others noted, colour washes were not very impervious or durable.

Copperas, or iron sulphate, appears not only as a colouring agent and mordant in colour washes but also as a type of treatment, in its own right for the surface of cementitious material. One source in the 1960s advised:

It isn’t hard to give concrete that effective ‘stone’ look that relieves the monotony of plain surfaces. A solution of Copperas (ferro-sulphate) will do the job. Dissolve ¼ lb of Copperas in water and sprinkle or spray it on the trowelled surface while damp and before it sets.123

Copperas either when incorporated into the stucco mix or when applied as a wash on stucco, made the lime plaster harder and more durable. It imparted a golden to reddish brown finish and therefore could be used as a substitute for ochres, with better performance over the longer term. There were also various proprietary washes for use on stucco. Some contained cement, with or without size, 
and others were based upon materials such as plaster of Paris or lime. Those based on cement were termed cement washes.

Oil paint, mixed according to the traditional method by combining white lead carbonate with linseed oil, provided the most durable exterior paint. It is therefore not surprising that oil painting was recommended as a durable finish, and specified by government agencies in high quality work.124 Nor is it surprising to find multiple layers of hard oil paint on surviving examples of Victorian stucco despite the practical difficulties and relatively high cost of applying it. Oil paint, also known as lead paint, was a common finish for stuccoed building elements up to the time that lead was phased out of paint in the 1970s for environmental health reasons. The replacement material in most common usage today is so-called ‘plastic’ paint, normally in the readily available form of the acrylic emulsion paints which have become the industry standard for all forms of internal and external painting, irrespective of substrate or colour or finish.

Washable distempers and mineral silicate paints were eminently suited to stucco but it is not clear to what extent they were used in Australia. Mineral silicate paints have been available since the late nineteenth century in Europe, where Keim Mineral Paints were first manufactured in Bavaria. These paints were marketed as the nineteenth century equivalent of traditional fresco paint.125 Silicate paint was specified on the cement stuccoed parts of some brick railway buildings in New South Wales in the early twentieth century, but it is not known whether it was the Keim type or a washable distemper produced by the Silicate Paint Co. The so-called washable distempers were water-based paints that incorporated either or both mineral silicates and emulsified oils that imparted some of the qualities of durable oil paint in the finish. One pigment, called Charlton White—a combination of zinc oxide and barytes invented by J B Orr of London and patented in 1874126—was used by the Silicate Paint Co. to make a product called Duresco, which was used in Sydney and probably also more widely afield. The New South Wales Government Architect stated in his 1890 annual report to Parliament that it was in use on all government buildings.127 This paint was marketed in a dry powder form and recommended to be mixed with clean water and applied hot.

## Regional and periodic colour variations

A large number of rendered buildings in around Melbourne of the late nineteenth century were finished originally with cream and light earth toned colour washes, whereas in the Sydney area warm pink, salmon and terra cotta hues appear to have been more common. This might be explained in part by a desire by Sydneysiders to emulate the warm hues of aged Sydney yellow block sandstone, the principal building stone in the colony. In the Victorian goldfields towns and cities, a high number of mid-brown finishes can be found. It has been suggested that these were obtained with washes that were pigmented with tailings from mining, but no research has yet been able to confirm this. One outstanding example of the mid-brown finishes can be seen on the civic group of buildings in Bendigo’s Pall Mall.128

In a more general sense, stucco colours were made with earth pigments. The range of colours included the earth colours from nature and more particularly the colours of the natural building stones. The painting of stuccoed buildings with conventional house-paints, as opposed to the colouring of the original stucco finishes, followed the same pattern as other painted masonry and timber structures. Over time, the tonal values of the earth colours used to make the traditional house paint colours for the walls of buildings grew darker, culminating in the use of the darkest tones from 1920 to 1940 when they were superseded by the fashion colours of the Modern movement. The brief appearance of Venetian red and other red oxide hues was inspired by the brief fashion for red brick architecture in the Queen Anne and Federation styles. A large number of stuccoed buildings were painted in pseudo brick colours in the 1890s but most of them reverted to lighter earth tones in the following period.

After World War II, Australians enthusiastically embraced modernism, including the use of pastel paint colours, which soon replaced the earth tones on all types of external surfaces. White untinted house paints soon followed those. Post-war changes in the manufacturing and marketing of paint, together with the rise of the home ‘handyman’, resulted in a more liberal use of paint, and this gave rise to the excessive layering of paint coatings commonly found on stuccoed surfaces today.

Stucco enjoyed a revival of sorts in the 1930s when various forms of applied cement decoration appeared on masonry and asbestos cement sheet clad timber-framed buildings. These so-called textured stuccoes were obtained with Portland cement and sand mortars applied by trowel or cast from a spatter device to create Spanish, Italian, English Cottage, Californian and Modern American textures, which could be suitably coloured with Portland cement based paints of almost any hue. Regrettably, these so-called stuccoes have left an inaccurate understanding about the origins of stucco and caused confusion about the term in current usage. For many, today, the term ‘stucco’ denotes only a rough-textured wall finish.

## Conclusion

As a result of the research initiated by the Victorian 
Stucco symposium which was held in April 2007, there
 is a growing awareness of the value of stucco as a material and a heightened awareness of the traditional methods 
that were employed to obtain the outstanding finishes 
and subtle colouring of the material in high class buildings. Many fine examples of Victorian stucco survive intact. Some retain their original appearance unaltered except for the changes wrought over time by weathering. These examples represent a valuable heritage resource, providing priceless evidence of the sophisticated trade practices used to create them. Conservation practitioners are now keener to understand and reproduce the traditional methods in the repair and conservation of the material.

It may be too late to recover the authentic finishes of some, but with greater knowledge of traditional trade practices and by sharing the accumulated knowledge of Victorian stucco materials and finishes it should be possible in the future to achieve higher standards in the conservation of all surviving forms of Victorian stucco.

Donald Ellsmore is a heritage consultant with a career-long interest in applied finishes. He is convenor of the Australian Chapter of the Association for Preservation Technology (International) and a member of the Technical Advisory Committee of the Heritage Council of Victoria. In April 2007, he convened the Victorian Stucco Seminar to promote greater awareness and technical improvement in the conservation of Victorian stucco.

Australian Stucco

Miles Lewis

definitions

materials and imports

rock lime

Roman cement

magnesian lime

artificial cement

local stucco

practice

finishes

moulding and casting

twentieth century painting

conclusion

## Definitions

I will take ‘stucco’ in the Australian context to mean an external rendered surface, which is in practice nearly always—implicitly or explicitly—an imitation of stone. But it is important to remember that the term has also been used in other ways, and it is therefore unwise to assume that historical references to the manufacture, application, surfacing or preservation of ‘stucco’ are useful or relevant to the material as found in Australia.

England, however, is largely relevant, and there ‘stucco’ was described in the eighteenth and the nineteenth centuries as ‘now a species of plastering, occasionally worked to resemble marble. One sort is made of lime, the other of plaster.’129 It was in much the same sense that Haddon still used the word in Australia:

In preparing internal surfaces for painting or decorating, the final coat may be in ‘lime stucco’, half sand, half lime, worked up with a felt float. This brings up a scum, which scum before it is dry is trowelled back into the work with a steel trowel. This when finished gives a hard, glass-like surface. 130

But in practice Australian stucco ranges from this sophisticated form down to the cruder plastering of wattle-and-daub huts. It was not just a question of plaster or common lime stucco. In Australia, as in Britain, there were some rock limes which by reason of the clay in their composition, produced a material with some hydraulic properties. This was essential for a durable stucco finish, for a common lime stucco would quickly wash away unless it was sealed very carefully. Roman cement, which was better still, was hardly produced in Australia at all, but it was quite extensively imported.

A change comes with the transition to Portland cement, which resulted in a surface of a very different character, though still usually emulating ashlar masonry. Robert Haddon sensibly explained in 1908:

The term ‘stucco’ is sometimes applied to cemented surfaces, but it is not of altogether general application, ordinary cement and sand work being generally referred to as ‘cementing’.131

James Nangle was not quite so careful, for he referred to ‘cement stucco’, but in Australia, as elsewhere, the word ‘stucco’ used alone almost always refers to a material used upon lime or natural cement, not upon Portland cement. Here we will consider both types.

## Materials and imports

Neither limestone nor chalk was to be found in the vicinity of Sydney Cove,132 and shells were burnt for lime in the first months of settlement, as they had been in other colonies in North America133 and South Africa.134 Governor Phillip is said to have brought a little lime from England to the settlement, but he had to try to obtain more locally even for his own house. ‘The Governor’, wrote John White, ‘notwithstanding that he had collected together all the shells which could be found, for the purpose of obtaining from them the lime necessary to the construction of a house for his own residence, did not procure even a fourth part of the quantity which was wanted.’135 Such lime as could be obtained from sea shells at Sydney was in great demand for stuccoing and plastering over the other inferior building materials, and therefore not much was used for mortar or other structural purposes.

Loam was also used for plastering. The only surviving Victorian example of external loam stucco, according to Hanut Dodd, is that of ‘Ercildoune’ near Ballarat, of 1859.136 Loam was used more commonly for internal work, as at Robert Hoddle’s house in Melbourne of 1838,137 and a surviving example is the ceiling of St Andrew’s Manse, Port Fairy, of 1856.138

As a general rule shells (see photograph on p. 28) can be easily seen in the mortar of older buildings in coastal and riverine New South Wales. Shell lime was burnt from the piles of oyster shells found in Aboriginal middens all along the coast, and when these were exhausted the bays and inlets were dredged for live oysters.139 In the 1850s and 1860s the activities of the shell diggers had become a problem in the Sydney region, and were resulting in the depletion of oyster supplies, a problem overcome only when the establishment of railway connections in the 1870s enabled rock lime to be brought from inland.140

At Coal River [Newcastle] the lime was made from oyster shells which, according to W C Wentworth, were found close to the banks of the river ‘in beds of amazing size and depth’, which some surmised were the results of the perennial feasts of the Aborigines. Wentworth himself thought it more probable that they were natural beds left aside by some shift in the course of the river. The lime was sold at Sydney for a shilling a bushel,141 and the commandant, Major Morisset, was also expected to maintain a stock of 1,200 bushels in the lime store. In 1816 Captain Wallis established the Limeburner’s Bay settlement north of Stockton, on the Hunter River. When this was abandoned for Port Macquarie in 1823, the manufacture was continued by free settlers who sold the lime to nearby squatters, and shell boats traded on the river until at least 1838.142 At Twofold Bay a large heap of ‘mud-oyster’ shells which were burnt for lime in the 1840s was reported to have been brought ‘from distant shores’, but it is easier to believe that they were gathered in the immediate vicinity.143 On the Clarence River the only lime available was that manufactured from oyster and cockle shells, and it was in use at least until 1866.144

At Corinella in Victoria shell lime was burnt in 1826, and shell lime was burnt by John Allee in early Melbourne for a short time until sources of limestone were discovered. From December 1837 until at least October 1838 government gangs were collecting and burning shells in the vicinity of Melbourne, though limestone was also being used from August onwards.145 Similarly at Moreton Bay [Brisbane] shells were burnt for lime until Captain Logan travelled up the Bremer and found limestone. A specimen of this was sent to Sydney in April, and within a few months a kiln was built at what was then known as Limestone Hills [Ipswich].146 Shell lime was also being produced at Port Arthur, Tasmania,147 and in New Zealand, where in 1840 the best spot for collecting shells was reported near the site of Auckland.148

Coral was an alternative raw material in the more northerly parts of Australia. In 1846 Andrew Petrie is thought to have burnt both shells and coral at Cleveland for use in the building of ‘Newstead House’, Brisbane,149 and both materials were burnt in the kiln established on St Helena island in 1869.150 Even in the 1880s both shells and coral were used at Palmerston [Darwin].151

## Rock lime

At Norfolk Island there was found limestone suitable as a building material in its own right, as well as for burning, and this enabled the construction of durable buildings even in the very first years. By 1793 sacks of lime were being sent to Sydney in the Kitty.152 Limestone was burnt successfully at Collins’s Sorrento settlement in Port Phillip Bay, of 1803–04, but not used after the settlement was abandoned. In Van Diemen’s Land Lieutenant-Governor Paterson on his first arrival at Port Dalrymple in 1804 reported the discovery of limestone, though it proved unsuitable for burning, and within a few weeks a better lime was being made from shells.153 Limestone was also found near Hobart.154 By 1816 a limestone quarry had been opened near Hobart, ‘the Mortar from which is extremely good for Masons’ Work, but not as good as Shell-Lime (which is to be had in the greatest abundance) for the Plaisterer’s use’. Limestone had also been burnt at Gunning’s estate on the Coal River, and deposits had been discovered in other parts of the island.155

Only in the 1820s were deposits of limestone and marble found in inland New South Wales,156 for example at McArthur’s property at Cowpastures, where limestone was burnt in 1821, allegedly for ‘cement’,157 and north of the Mount Horrible Road near Bathurst, from 1822.158 Lime was nevertheless in short supply in most inland parts of the colony, and as late as 1826 James Atkinson suggests that the settler’s stone chimney should be built with loam as mortar.159 The same loam, mixed with some coarse grass, would serve as a first coat in plastering, then there should be a second coat containing ‘a portion of lime’, and the whole should be whitewashed.160 The lime from Bathurst had no impact in Sydney because of the difficulty and expense of transporting it over the Blue Mountains, but lime from Picton and Argyle was being sold in Sydney in the 1840s. After the railway was put through, Marulan lime became the favoured type for bricklayers,161 and by the 1870s limes burnt from the Marulan and Manning River stones were standard items on the Sydney market.162 However, lime was also brought from Victoria, and by 1880 shell lime had been completely superseded.163

In Van Diemen’s Land rock lime was found in various new locations, but the distribution of stuccoed buildings, which were common in the north and rare in the south, was determined more by the lack of good freestone in the north than by the distribution of limestone. In the 1830s several kilns were operated by the government near New Norfolk.164 In Western Australia limestone was available at both Albany and Fremantle, but at Albany shells were burnt in preference to stone in 1826-7.165 Lime was used in the construction of the Round House at Fremantle in 1831, and according to Pearson it would have been burnt either in shallow pits or in small masonry kilns.166 At Rottnest Island, as at Albany, though limestone was quarried for building purposes, shells were burnt to get lime for mortar and stucco.167 Near Perth, limestone could be got from Mount Eliza,168 but none had been found in the vicinity of York, and in the 1860s the government offered a reward of £40 for its discovery.169

It was not long after the settlement of Melbourne that John Pascoe Fawkner remembered the rock lime that had been used in 1803–04 at the abortive settlement of Sorrento, where he had been as a child, and from 1839 an extensive trade developed in lime from Point Nepean, some of it for export to Sydney. Other sources of limestone had been found at Geelong and elsewhere which would produce a slightly hydraulic lime, and it was this that at last made external stucco reasonably durable. Thus it was that Melbourne, in contrast to Sydney, developed a stuccoed architecture of a sort now outmoded in Britain itself. ‘I am sorry to say that the demon of Roman cement has doubled the Cape, and begun to revel in all the luxuries of the Regent-street school of architecture’ wrote a visitor in 1845,170 though most of the stucco which conveyed this impression would not in fact have been made with imported Roman cement, but with locally burnt rock lime.

In 1821 the Sydney architect Henry Kitchen told Commissioner Bigge that limestone had been burnt to produce cement at MacArthur’s property at Camden, but this can at best have been only a mildly hydraulic lime, or much more would have been heard of it.171 In practice, all hydraulic materials were imported to Sydney for some time to come. Parker’s cement was available at least by 1826,172 and was being advertised in 1835 by G S Tucker.173 Other more or less adequate hydraulic limes were brought from Port Phillip and elsewhere.174 In Adelaide, after the failure of the Torrens Weir, T B Strangways was insistent that North Adelaide lime should on no account be used in public works exposed to water, but only the best hydraulic lime.175 In Adelaide that would have meant an imported product, but in Victoria a number of roche or rock limes with hydraulic properties were discovered from the 1850s onwards.

A Victorian specification of 1890 calls for ‘approved Geelong, Waratah [Gippsland] or Lilydale roche lime’,176 while another specification in that year names these three together with Coimadai lime.177 Coimadai or Pyrete Creek, near Bacchus Marsh, was a source of common lime from the 1850s onwards. By 1886 three lime claims there were in the hands of the Alkemade Hydraulic Lime and Cement Company, a partnership of Petrus Alkemade, builder, and Matthew Egan. Nearby George Dibley also established a Hydraulic Lime & Cement Co. Lime from these sources was in high demand during the building boom of the 1880s, and J C Newbery, chemist at the Victorian Museum, claimed that it was equal to the best imported English hydraulic lime. Dibley’s works ceased production in 1892, doubtless as a result of the depression, but Alkemade’s continued well into the twentieth century.178

## Roman cement

As local production of lime was improved in the latter half of the century, the importation of hydraulic lime from Britain and elsewhere (which had been substantial) was reduced considerably. What did not reduce was the importation of cement. Roman cement was probably imported to Australia fairly extensively and used for special purposes. Major Mitchell’s memoranda of about 1828 note the desirability of lining a cesspool with Roman cement,179 but these are probably notes transcribed from English sources, and it does not follow that anything of the sort was being done in Australia. It was essential, according to James Thompson, that brick or stone walls on the south or weather side should be stuccoed ‘for, if this is not done, the rain penetrates the bricks or stone, and makes the walls always wet.’180 For such purposes ‘Roman’ cement was imported. T H James reported amongst the abandoned detritus at Port Adelaide in 1836 ‘blocks of Roman cement’, now as hard as stone, wanting nothing but the staves and hoops’.181 In 1856 barrels of Roman cement were listed amongst the contents of ‘Barwon Grange’, Geelong. All this is consistent with what is found at the house ‘Lullote’ at Inverleigh, west of Geelong, thought to date from the early 1850s. The west or weather wall only is rendered, and the (distinctly odd) verandah columns are of brick rendered in a material which is partly exposed, and is probably Roman cement.

Portland Cement was also imported by the Australian colonies, and of course attempts were made to emulate both types locally. The first attempts in Australia at producing a hydraulic cement seem to have been those of Charles Mayes in 1853. It does not appear that any system of patents was operating in Victoria at the time (the first patents were issued in the following year, the second being to Mayes himself for his improved pisé). However, Mayes claimed to have invented ‘an incombustible building material’, and on the strength of this sought from Lieutenant-Governor La Trobe a licence to search for and remove ‘certain rocks or cement stones for the manufacture of calcareous, hydraulic and other cements’ required to make his material, as well as to construct kilns and do other things ancillary to the enterprise. As there was no patent specification, we do not know what he had invented. Nor did he gain his licence. The file is annotated by ‘JF’ [J F L Foster, Colonial Secretary], ‘I do not feel at liberty to grant all his applications give the sanguine gentleman a proper answer.’182

The only significant local manufacturer of Roman cement was the Patent Septaria Cement Company 
at Mornington, Victoria, which constructed its kilns in 1862 and struggled on until 1865. It was to be more 
than 20 years before local makers were able to produce Portland cement successfully. Much later William Shearing, of G & W Shearing, South Australian brick and pottery makers, discovered a cement stone within reach of Adelaide, and in 1889 the cement was reported to be available in any quantity.183

## Magnesian lime

In Victoria there were abortive experiments with magnesian limestone cements, which probably reflect earlier developments in India. A British colonist in India, Dr Macleod, had discovered the hydraulic properties of magnesian limestone and brought them to the attention of the Madras government. Tests were conducted by 
A T Cotton of the Madras Engineers, who found magnesian cement to be equal to Parker’s.184 Its cost 
was about the same, but within 15 years it dropped to a tenth due to the discovery of major magnesium deposits at Salem and Trichinopoly.185 The new material came into wide use in India, where it was also tested 
by J T Smith. Next, during the 1830s, Pasley tested magnesian limestones from the north of England, but was not optimistic about their usefulness.186 In France, Chatoney and Rivot asserted that magnesian limestone produced a superior cement for hydraulic works, but a commission report took the reverse view, and actually recommended that magnesian cements be barred from use. In the United States Q A Gillmore challenged the stance of the French commission and pointed out that the most reliable local limes, under the various Rosendale brands, were from magnesian stone.187

Specimens of newly discovered limestones were tested by J G Knight in a small kiln set up for the purpose in 1859, and produced a hydraulic cement. Amongst these, it seems, were the ‘shelly or magnesian’ limestones used in combination with ironstone to produce a cement according to a patent taken out by T P Edwards in 1862. Edwards seems to have referred to two different stones, a shelly limestone from the coast near Geelong and elsewhere, and a magnesian limestone or dolomite discovered in the excavation of the Reilly Street drain at Collingwood. Although the latter was reported in the Australian Builder as a likely source of ‘good artificial cement’, it seems to have contained such a mixture of ingredients as to be almost a natural cement stone, and was clearly inspired by the success of magnesian cement in India. Edwards was followed by W H Hughan, who made two patent applications, of which one was granted, for a cement using clay and quartz tailings. The other, for ‘Hughan’s Portland Cement’, was refused in 1861, probably because it used magnesian clay and was similar to Edwards’s patent.188 It would seem that it should not be regarded as a Portland cement, but it is not clear whether Hughan was a local resident or an overseas applicant.189

## Artificial cement

Portland cement was generally available in the Australian colonies by the middle of the nineteenth century,190 and was imported in increasing quantities for the next 40 years. It was first listed in Melbourne in 1857,191 but the Co-Operative Society of Plasterers had in the previous year recommended it as the best material for external use192—doubtless meaning render or stucco. In March 1857 Charles Laing specified it for the stucco of buildings at Brighton,193 and it was also used at ‘Glass Terrace’, Fitzroy, built in stages during the 1850s, where it survives.194

In 1862 Dyer’s Lime & Cement Stores, of Melbourne, advertised four British brands: Wouldham’s; Knight, Bevan & Sturges’s; White’s; and Hilton’s.195 In 1863 the Sydney importer Richard Wynne negotiated with another manufacturer, Booth & Co of Borstal, on the Medway near Rochester, in Kent. He was concerned with issues of quality, price, freight rates and quality of barrels,196 but there is no positive evidence that anything came of this, for there is no report of the use of Booth’s cement in Australia. In 1871–72 Portland cement was used at the Alfred Graving Dock in Williamstown, though the fact that contemporary reports mention only ‘hydraulic cement’197 suggests that a common terminology had not gained currency. In Darwin Portland cement was used by J G Knight for concrete flooring and for the foundations of government buildings, as mentioned above, notwithstanding the fact that shell lime could be obtained locally and was used in other parts of the same buildings.

In 1881 the current prices listed in the Australian Engineering and Building News named three British brands, Knight Bevan’s, White’s, and Gostling’s,198 and the current price list in the Australasian Builder & Contractor’s News in 1888 named ‘British Lion’, ‘Tunnel’, Hilton’s and Francis & Co’s ‘Nine Elms’.199 But this gives no idea of the range available. Nearly 50 imported brands, mostly British but some German, were either advertised locally or shown at trade exhibitions in Australia by 1888. There are in fact only a handful of British brands which are not recorded in Australia, amongst them: Ashton & Green’s ‘Castle’ brand;200 that of Coles, Shadbolt & Co;201 ‘Earle’s’, by Thomas & George Earle of Hull;202 and the Rugby Portland Cement Co’s ‘Rugby’ brand.203

These imported cements continued to be used quite routinely well into the twentieth century—Knight Bevan Sturge’s, for example, was specified for additions to a Melbourne shop in 1907,204 and was used again in Australia’s most remarkable reinforced concrete structure, the Dennys Lascelles Austin Wool Store at Geelong, of 1911.205 It is presumably the ‘K.B.’ cement still being advertised by James Moore & Sons in 1913, along with 
a previously unrecorded ‘Black Eagle’ brand.206

The prominence of German brands reflects the position in Britain itself, where A C Davis complained of the fact that ‘our Continental neighbours’ were now making a first class cement at a price low enough for it to be shipped ‘not only to this country [Britain] but to the very centres of the export and colonial trade which English manufacturers once thoroughly relied upon as their own market.’207 The importation of German cement to Australia was worth £20,000 prior to World War I, but then decreased to zero, whereas imports from Denmark rose from £261 in 1914–15 to £20,502 in 1915. This gave rise to the not unnatural suspicion that the German product had simply been rerouted. However, the Danish Consulate pointed out that there were large cement works in Denmark, and that the establishment of a direct steamship service had enabled the product to be brought onto the market. There was no possibility that any was of German origin.

There seem to have been substantial differences between the brands, not merely in terms of their engineering properties, which were rarely critical before the advent of reinforced concrete, but also their appearance. A major function of Portland cement in the 1870s and 1880s was the surfacing of buildings and the casting of architectural ornaments. The specification for a South Australian bank in 1878 directs:

Every care must be taken in putting on the last coat to keep it of a uniform tint. “Goslings” [sic] or “Johnstons” [sic] brand is to be used in the setting coat, and in the event of this not proving satisfactory to the Architects the work must be neatly distempered of an uniform approved tint.208

It is impossible to define the point at which a true artificial cement was manufactured in Australia, still less one that can reasonably be described as ‘Portland’. Hughan’s patent of 1861 had in fact used the word, and was an artificial mixture. The Schnapper Point company’s cement was certainly an artificial mixture. In 1871 the word ‘Portland’ again appeared in the patent of W H Malyon,209 but whether this was of local origin is unclear. In 1873 J M Robertson, who had previously patented a way of manufacturing hydraulic cement, received a further patent for improvements in the manufacture of hydraulic or ‘so-called Portland cement’. Infusorial limestone from Waurn Ponds, Moorabool or elsewhere was ground with basalt in a ratio between 2:1 and 4:1, mixed with water, formed into bricks, calcined, and ground again into powder.210

The first sustained attempt at artificial cement manufacture seems to have been made in South Australia. William Lewis, a limeburner, is said to have experimented for some years with mixtures of limestone and clay, and at last produced a material which was claimed to be ‘but little inferior to Portland cement’.211 On 12 December 1882 Lewis’s Marino Cement Works were opened on the 39 hectare site at Brighton. The new venture struggled financially, unable to compete with imported cements, and closed down in the following year, but new works were to be built on the same site in 1892. These used the same raw materials, and more than a million tonnes of Portland Cement were produced there in the ensuing 60 years.212 The Cullen Bullen Company claimed to have made Portland Cement in New South Wales in 1884, though they did not achieve commercial production for some years.213 The more or less enduring enterprises were: in Victoria, the Australian Portland Cement Co214 set up in 1889, and the Victorian Cement Works in 1890; in South Australia, Shearing’s Portland Cement Co in 1892 (which immediately became the South Australian Portland Cement Co); and in New South Wales, the Cullen Bullen Lime and Cement Company (later Commonwealth Portland Cement) in 1889215 
and Goodlet & Smith, who began production in 1893.216

## Local stucco

The British tradition of plastering materials such as wattle and daub was naturally transmitted to Australia. But the distinction between the vernacular and the high style was not maintained, for Australian vernacular examples might be ruled in imitation of masonry just as in more pretentious buildings. Most of this work was the result of habit and tradition in the truest vernacular sense, and we have very little documentation of it, but a certain amount can be learnt from inspection.

Peter Cunningham advised an external plaster for slab houses consisting of ‘alluvial soil, mixed with a portion of cow-dung to prevent it from cracking, and with chopped straw to enable it to adhere.’217 ‘Hawthorn Bank’, Port Albert, Victoria, is a wattle and daub building possibly dating from the 1840s, and a close examination of the daubed or rendered surface shows that it contained animal hair and probably a significant proportion of lime. Although few have been closely investigated, many examples seem to be similar, amongst them Leschenault House, Western Australia (since clad over in weatherboard).

A now demolished pair of houses in Vine Street, Ashfield, Sydney, was built by a German in the 1850s and presented a very convincing face of stucco ruled as ashlar, though underneath it was a building of fachwerk and lehmwickel. Around Wattle Flat, Hill End and Gulgong is a strong school of pole and pug construction, which, as indicated in the Holtermann photographs of 1872, was sometimes daubed very crudely, but in other cases ruled perfectly as ashlar.

A composition, or ‘compo’ as it was known, of sand and hydraulic lime or cement was the common material for facing brickwork. There were in theory ways of producing a reasonably durable stucco from a good common lime, and there is some evidence of this in Australia. The Settler’s Hand Book, of 1861, advised:

Take 56 lbs. [25.4 kg] of pure coarse sand, 42 lbs. [19 kg] of pure fine sand, mix them together, and moisten them thoroughly with lime-water; to the wetted sand add 14 lbs. [6.4 kg] of pure fresh burnt lime, and while beating them up together, add in successive portions, 14 lbs. of bone ash; the quicker and more perfectly, these materials are beaten together, and the sooner they are used the better, 
as they harden rapidly.218

Higgins’s cement was also claimed to be suitable, but if it was used in Australia at all it must have been quickly overtaken by Parker and Wyatt’s ‘Roman Cement’. The advantage of Parker’s cement, of Mulgrave’s Roman cement, and indeed of gypsum plaster, was that they set rapidly. Frost’s ‘cement’ (actually a hydraulic lime, though Frost did later produce a cement), was slower, especially as it was sometimes mixed with common lime. So was Bailey’s composition, a stone lime slaked immediately after burning and mixed with three parts of clean sharp sand.219 By the mid-nineteenth century the usual options for an external compo or stucco in Britain were Roman, Portland, Bailey’s, Johns’s, Brown’s or Robinson’s cement, and London builders often used the same materials for internal plastering, running cornices and casting ornaments.220

In external work the aim was always to imitate the appearance of stone, and a typical English specification for an exterior stucco surface the early nineteenth century was ‘to lath, lay, set, and colour stone colour ...’221 The addition of materials other than pigments is not recorded in Australia, despite the rich history of such mixtures overseas. The second government house at Parramatta, built by Hunter in 1799, had a stucco finish grooved to imitate stone, as will be mentioned below, and it would be of some interest to know what lime was used for it, or whether some of the new Roman cement was imported for the purpose. The locally burnt lime was of course not sufficiently waterproof to make a durable external stucco, and as soon as good bricks could be made they were adopted as the main material for important public buildings. This is characteristic of the work of our first important architect, Francis Greenway. It is by no means clear how a durable stucco was achieved in most early buildings, but it is notable that for two good quality terrace houses in Melbourne a specification of 1854 called for a stucco of Sullivan’s artificial stone.222

These earlier buildings tend to be mainly flush-faced, but where mouldings were required, they could be formed in rough brick or stonework, just as for internal plastering, and then built up to the required profile. A good example of this is the Wesleyan Chapel in Paterson Street, Launceston, designed by Samuel Jackson in 1835. 
The front is a strange and vaguely Tudor Regency design with panelled pilasters. The side flank shows the same pilasters set out in brickwork for a render coat, which never eventuated. On the main surfaces a resemblance to ashlar masonry was commonly attempted by ruling the stucco in an ashlar pattern divided by shallow grooves, pencil or crayon lines, or both, and by colouring the surface, as will be discussed below.

Portland cement was to acquire its name in England because of its resemblance to Portland stone when used as a stucco. This was undoubtedly its major use in the Australian colonies as well, especially on important public buildings, such as the St Kilda Town Hall, Melbourne, in 1859.223 Cement might be used for the dressings only, but with the same objective of evoking the appearance of stone. Hornabrook’s shops in Adelaide were completed in 1887 with a brick front and cement bands, dressings, cornices and pilasters, all coloured in imitation of stone.224

Most late nineteenth century buildings of any architectural elaboration depended upon Portland cement, either because they included castings and mouldings that required it, or because they were fully coated in it, as was the case with ‘Mandeville Hall’, Melbourne, in 1877.225 Indeed by this date Mayes could say that, for external work, stucco or lime plaster had been entirely superseded by Portland cement ‘compo’ in Melbourne and Sydney. Nevertheless, specimens of stucco 20 years old were to be found in Sydney, still in good condition, and in country districts where limestone was available, lime might still be the best material to use. If it were properly coated, and treated with chunam, it would be just as durable as cement compo.226 The word ‘chunam’ had a meaning other than its original Indian one—a fine plaster of shell lime, jaghery water [sugar water], egg white and ghee [clarified butter] in various proportions.227 Mayes meant a mixture of one bushel [0.36 m3] of lime to two gallons [9 l] of best ‘thin black oil’.228

Portland cement render, unlike earlier types, was commonly left in its natural colour, which itself depended very much upon the brand of cement used and the choice of the sand. In one instance, ‘Benvenuta’ in Melbourne, the work was formed using Knight, Bevan & Sturge’s, the leading British cement, but finished in the German ‘Stern’ or star brand, with different sands in the two mixes, and with the finished surface ruled as blockwork:

The whole of the outside cement work to be Worked in Knight Bevan’s and finished in Star brand, composed of three parts of washed Sandridge sand with one of cement for the first coat and two parts of washed Caulfield sand with one of cement for the fining. To cement in two coats as above described, the whole of the external brickwork (excepting back walls of the main building above conservatory roof and to outbuildings) also inside walls of Conservatory and face of retaining wall to same also insides and tops of parapets and shafts of chimneys. The whole finished to an even thickness of ¾" and to a uniform colour, all to be block lined (with the exception of the insides of parapets) including cross joints to all mouldings and arches. The whole of the face mouldings to be run clean and sharp and all work to be of an even colour and well watered at the various stages of progress.229

## Practice

For Australia, the first detailed account is that of Robert Haddon:

Outside cement work of all kinds is best done in damp weather, freedom from actual rain or frost on the one hand, and from excessive dryness on the other, being advisable.

Cement work should always be kept damp. The surfaces upon which it is laid should be wetted, and if practicable, rough to form a good key, and the work should be kept moist for at least seven days after completion.

...

In all cement work the nature and character of the Portland cement used should be ascertained, as the strength and time of setting varies greatly in this article. Coarse sand is best for first coating, and fine washed sand for finishing.

The following is a workable recipe: - First coat (‘floating’). – Four parts of sand, one part of Portland cement, gauged clean and used fresh and laid evenly on to the walling in a ¾-in. [19 mm] thick first coat.

After first coat has set, second coat (‘finishing’), with a ¼-in [6 mm] thick finish, compounded of 2½ parts fine sand to one of cement.

The finish may be brought to hardness by the steel trowel or to a granulated (sand) surface by wood float.230

Nangle differs from Haddon in minor respects. He recommends sand-cement ratio of 3:1, or 2:1 for arrises and exposed portions, or in first class work 2:1 throughout. The rendering is usually put on in a single ¾ in [19 mm] layer, but sometimes a ¼ in [6 mm] outer coat is used.231

## Finishes

As in Britain, ashlar ruling was common, for example, in John Lee Archer’s work in Van Diemen’s Land. Specifications rarely give any details of this ruling process, but say something like ‘well hand floated trowelled rubbed up and lined off as may be directed by the Architects.’232 To further improve the effect, an appropriately coloured sand could be used in the mix, a pigment could be added, or a wash applied to the surface, to create an effect even more like that of freestone, more especially the Portland or the Bath stone favoured in Britain.

At Old Government House, Parramatta, the rear extension of the building built in 1815 fortuitously preserved some of the wall surface of 1799, which is ruled as ashlar and mottled or daubed with an ochre tint in a rather crude way, though it may have looked well enough at a distance. At ‘Pontville’, Doncaster, Melbourne, of the 1840s, a section of the external stucco was preserved above a false ceiling built into a verandah, and the surface is similarly ruled but uniformly coloured with a warmish brown tint. No doubt there is some change and deterioration in such finishes, as in all others, but enough examples survive (more usually exposed by peeling paint), to suggest that this was fairly standard. I would cite ‘Mountford’, northern Tasmania, 1830s onward; the upper window architraves of the original portion ‘Glass Terrace’, Fitzroy, about 1853; and the former Volunteer Arms Hotel, Port Fairy, of 1868. At the original hospital, New Norfolk, Tasmania, a large area of ashlar ruled stucco remains, though it probably dates from the 1850s rather than from Archer’s original building. Beneath the verandah, the joints are picked out in white, while above they are reported to be simply ruled233 (unless this reflects erosion of the exposed areas). Blind windows are painted in trompe l’oeil effect, a practice that was probably fairly common in Australia, though few survive.

In Australia the Settler’s Hand Book of 1861 proposed colouring stucco with a distemper made of skimmed milk, quicklime, linseed oil, and a colouring agent such as whiting or ochre.234 A better guide to general practice is ‘Altyre’, a stuccoed house in Melbourne, which was specified in 1889 to be refinished with ‘best weatherproof colour set with tallow + copperas [iron sulphate] or other approved ingredients’.235 Twenty years later Robert Haddon described as typical ‘a mixture of lime, colouring matter, and a fixer such as copperas or salt.’236 Various proprietary washes were marketed in England for use on stucco, to enhance its resemblance to the more fashionable building stones, some of them actually containing cement, with or without size, and others based upon materials such as plaster of Paris or lime.237 To what extent they were used in Australia is uncertain, but the best-known brand, Johns’s Patent Stucco Wash,238 was marketed in Melbourne by Dickson, Williams & Co.239

As more sophisticated cements became available they were sometimes combined to create a colour scheme in their own right, just as was done with hard plasters internally. The specification for ‘Benvenuta’, quoted above, is an example of this. Even where the surface remains exposed it is rarely possible to read such a scheme today, though I know of one example where it is more or less discernible, doubtless preserved by the clean country air: ‘Noorilim’ at Goulburn, by James Gall, of 1878–79. John Sulman referred in 1887 to shops in Bond Street, Sydney, where ‘the mouldings and their ornaments are run in a white cement in contrast with the plain grey of the body of the walling, and the effect is by no means unsatisfactory’.240

But, while some buildings were left with their original cement coatings, tinted or otherwise, there were those who felt that paint was essential, though this would not be done for the first few years. When the ‘exterior cement plaster’ of the Royal Mint at Melbourne began to crack within 10 years of its application, this was attributed to the lack of painting. The Public Works Department asserted that ‘plaster facings’ should receive at least five coats of paint after three years, and after that a coat every two years.241 The paints were generally designed to evoke the colour of freestone, and one should not forget that they were sometimes sanded to give them a greater verisimilitude. In the United States A J Downing said ‘Stuccoed or cemented buildings should be marked off in courses, and tinted to resemble some mellow stone; Bath, Portland stone, or any other of the light free-stone shades, are generally most agreeable.’ He even went so far as to illustrate such tints, probably for the first time in published form.

## Moulding and casting

The whole system of enrichment used in the boom style was dependent upon the introduction of reliable cements. Earlier and simpler stuccoed buildings might have been enriched with a cornice, a row of dentils, a name plate and modest scrolls or modillions. We know in some cases, and can reasonably assume in all, that these were done in a higher quality lime or cement, usually distinct from the material used in the body of the work. But with the widespread use of Portland cement any part of the building could be enriched, and often was.

External cornices were run in much the same way as internal ones, the rough shape being first formed in the brickwork of the structure. If this was done in rough stone rather than brick three coats might be required, but according to Haddon two were the norm, ‘the stuff being gauged not too rich, otherwise fine cracks may occur’.242 A good example of brickwork prepared for the purpose, with projecting courses roughly hacked to shape, can be seen in the Greek Orthodox Church, Victoria Parade, East Melbourne, by Walter Butler.

As indicated above, incised decoration, in which a decorative pattern of linework is recessed into the face of the render, is an enigma so far as documentary sources go. There is a traditional type called ‘impressed plaster work’, but unfortunately, though Millar’s chapter on Portland cement facades promises a discussion of this in the contents, it does not actually appear.243 However, craftspeople can still do it, and Barrie Cooper explains elsewhere that the pattern is pounced onto the surface, and the design cut out with an implement while the render is stiff but not yet hard.

In 1864 the Corinthian capitals, urns and modillions of the Launceston Town Hall were cast in Portland cement. They were first modelled in a very fine pipeclay from Cataract Hill, then a plaster cast was made, and this then used to create the cement versions. It was reported, somewhat over-optimistically, that this novel material would be denser and more indestructible than freestone ‘as the elements which wreak such certain decay on every species of freestone seem to have no effect on the manufactured Portland cement.’244

In the 1880s ‘Patent Victoria Hydraulic Freestone’ was marketed in Melbourne by a company of that name, and this also seems to have been based upon Portland cement.245 It was used especially by the Melbourne architects Crouch & Wilson, for water tables and other details of their many churches. The material was first exposed to public examination in 1881 at the Artificial Stoneworks at the corner of St Andrew and Church Streets, Middle Brighton. It was reported to be manufactured according to R H Stone’s patent. The architect Michael Egan appears to have been an active partner, and Charles Webb and Evander McIver are referred to as well.246 The works were moved two years later to Sandridge [Port Melbourne], where they were officially opened on 1 October 1883.247 The patentee was apparently a local man, R Holden Stone, for he wrote to the Argus to state that no chemicals were used in the process, and that therefore, unlike other artificial stones, no soluble salts were produced.248

The scientific community was enthusiastic. J Cosmo Newbery found that the stone:

contains no soluble constituents which would cause disintegration, or exfoliation, and that the more it is exposed to moist atmosphere the harder it becomes; in fact the stone has hydraulic properties.

R W E McIvor also found that it seemed to harden during exposure, rather than to deteriorate, that it performed well under other tests, and that it was ‘admirably suited for building purposes’.249

The first reported use of the Victoria stone was in the new premises of David Munro at 154 Queen Street, corner of Little Lonsdale Street, in 1882.250 It was used in 1884 for Terry & Oakden’s E S & A Bank, Brighton, and for Evander McIver’s Presbyterian Church, Brunswick.251 Also in 1884 T J Crouch mounted an appeal against the Melbourne City Council’s refusal to allow the use of the material in a city building façade, and surprisingly enough he was successful: the referees determined the material was a stone within the meaning of the Melbourne Building Act.252 The most extensive use of the material was in the Presbyterian Church in Alma Road, West St Kilda, built 1885–86 to the design of Wilson & Beswicke. The body is of bluestone, but the dressings, water tables, enrichments, mouldings, tracery and pinnacles, and the whole of the prominent spire, are of Victoria stone.253

A material based upon Portland cement, like the Victoria Hydraulic Freestone, seems a natural enough extension of the earlier ‘artificial stones’ based upon lime or natural cement. Indeed, by the 1880s one hears little of specific patents, though the amount of ornamental cement casting increases exponentially, using the extensive range of Portland cements now available on the Australian market. Nor do we hear much of the specialist casters and modellers involved, though a fountain at 11 Redmond Street, Kew [Melbourne], probably contemporary with the house, of 1887–89, is branded:254

L MURPHY
C[...] D[...]

Haddon gave an account of the manufacture of enrichments and ornaments in what he called ‘
pressed cement’:

The work is first modelled in clay and cast in plaster of Paris piece moulds, which are well coated with shellac. ‘Stuff’ of Portland cement and sand gauged two or three to one is then mixed and pressed into the molds with ramming tools. When slightly set the molds are removed piece by piece, and the work laid out upon drying boards, trimmed, and afterwards kept moist by watering for several days until hard.

In gauging the cement and sand care should be taken to thoroughly mix the two, and to wet so that the mortar may be damp without being sloppy.

Pressed cement work may be attached to stuccoed surfaces with cement mortar, and strengthened with galvanized iron hooks, nails or clips. 255

The architect Norman Hitchcock, of Melbourne and then Fremantle, was one of the few whose ornaments are so characteristic that it seems certain that he owned not only the designs but also the actual moulds. His buildings in the inner suburbs of Melbourne are immediately recognisable by the combination of standard types of mask, vermiculation and swags, but most of all by the lush parapet scrolls with radially placed perforations and projecting spikes (which survive in rare cases). These scrolls are quite unknown in the work of other designers. A terrace of houses by Hitchcock in King Street, Fremantle, uses these scrolls and is almost identical to ‘Walkham House’, 902 Swanston Street, Carlton. A rather more specialised element used by Hitchcock is a cupid acting as an atlante, which appears in the former Buckley and Nunn building at 198–204 Faraday Street Carlton, of about 1886. It reappears more than 20 years later in George Street Fremantle, made almost unrecognisable by the change of context. Whereas the Carlton building was a lush Renaissance/Baroque confection entirely executed in cement, in Fremantle we are looking at a terrace of gabled, almost Gothic, red brick houses, in which cement is used only in the dressings. It is only the fact that Hitchcock signed the building that makes us confident that it is the work of the same man.

The most revealing document in this context is the specification for the Melbourne mansion ‘Benvenuta’, of 1891. It has particularly fine classical figures standing on the parapet, and the oral tradition that they were imported from Italy by the owners is more believable than in most cases, given that they were specified as being supplied by the ‘proprietress’, Leah Abrahams. A number of other details are specified, including the cornices with ‘modillions (face leaf planted on)’.256 However all the other ‘enrichments’ of the exterior were provided by the local modeller Otto Waschatz—egg and dart mouldings and scrolls on the chimneys; large scrolls and a ‘loft’ on the tower; egg and dart and running leaf moulds on the tower cornice and architrave; an ornamental head, corners and festoons, also on the tower; balusters in the parapet; figure modelling in the pediments (partly detached); ‘small flower and leaf on plate’ in the pedestals; modillions with leaves planted on in the upper and lower cornices, distorted to suit the curve of the central pediment, with mitre leaves and acorn drops at the corners of the modillion course; further friezes, architraves, archivolts, spandrel sprays at the arch springings; corinthian capitals; enriched panels in the window spandrels; deep foliage and shell panels in canopies over doors and windows; an enriched impost course; festoons; and foliated keystones. There were also four stock vases to be provided by the principal contractor, not by Waschatz, with holes in the bottom to receive 3/4 inch [19 mm] galvanized iron pipe fixings.257 Truly, Portland cement must be seen as the main generator of the Boom Style.

Cement casting did not end with the Boom Style, but in the twentieth century the imperative was to achieve a better verisimilitude of real stone, quite distinct from the stucco tradition, and this was done by the use of colouring agents and crushed rock finishes. One such was the Architectural Pre-Cast Stone produced in Victoria and Tasmania by Picton Hopkins & Son, who stressed that the facing was cast integrally with the body of the block.258 Here, then, stucco facing and cement casting practice have entirely diverged, for simulating stone in 
the wall surface was now seen as a dishonest technique. The underlying concept of stucco had simply ceased to be relevant.

## Twentieth century painting

The decline of the old stucco tradition is marked by Nangle’s dogmatic assertion in 1911:

All surfaces of the work should be finished quite smooth by a steel trowel; but on no account should the work be struck out in joints to imitate stone. In the first place the imitation is fraudulent, and in the second place this scratching of the cement surface generally means a crevice into which the weather penetrates.259

Consistent with this new attitude, stucco was no longer painted in colours specifically evoking stone: a much wider range was used, and white or near-white came 
to be especially favoured.

The paint manufacturers Lewis Berger & Sons (Aust.) offered a detailed rationale for painting stucco:

The architect appreciates the advisability of painting exterior concrete or stucco walls. This is advisable for two reasons: first, the control of the decorative effect in colour, as required by the type of building, which paint affords, and the ease in which the building can be cleaned up in appearance and the change of colour scheme effected. Second, painting a concrete wall renders it water-tight, and prevents the appearance of hairline cracks and chipping off caused by the penetration of moisture and frost.

Interestingly, though, Berger’s were by no means dismissive of cement stucco. They claimed that their paint did not ‘destroy the interesting texture of the stucco wall as does a gloss finish’. Of their four colours, one was ‘light stone’ and another, ‘ivory’, was within the traditional spectrum, while a third was a warmish grey actually called ‘cement colour’, and the last was ‘slate’.260 The evolution of stucco paints is discussed above by Donald Ellsmore, but essentially they had already adapted in the later nineteenth century to deal with Portland cement, and the range now expanded, especially in terms of colour.

Robert Haddon advised that oil paint would not adhere well to new cement work, but it could be painted after a few years. He recommended a good priming coat to ‘stop the excessive suction and form a hard body’, preferably red lead and raw oil, after which ordinary paint was used.261 In 1931 Bergers specified the application of their ‘Dusseal’ cement sealer, and the Sherwin-Williams Company (Australia) required that fresh concrete be treated first with the company’s ‘Prymseal’, and linseed oil was under no circumstances to be added.262 However, Taubmans Limited had a ‘cement-proof paint’ which did not require priming:

It positively resists the chemical reaction of new cement, which during the process of setting, liberates lime. It remains unaffected by this free lime (alkaline), which quickly destroys ordinary Linseed Oil Paints.263

But the truth was that cement finishes were in decline, and the real market for stucco paints lay in the existing and now unfashionable nineteenth century building stock. Even ‘Benvenuta’, where such care had been taken in specifying the best cement finishes, acquired a white coating, of which only traces now remain. Jenny Dickens has found it to consist of lime, chalk, fine sand and casein, and it seems likely to be a twentieth century proprietary product, either a cement paint or another finishing material. Cement paints were reported in a British article of 1946 to be in increasing demand, and were characteristically supplied in shades of white or near-white.264 The British ‘Snowcem’265 was prominent, and the Taubmans cement-proof paint was one local example. Other facing materials, such as Pittsburgh Cementhide,266 Cullacrete267 (referred to elsewhere by Donald Ellsmore), the British Stic B Semi-Stone Covering,268 and the American Minwax Brick and Cement Coating269 are of largely unknown composition.

So extensively was the ashlar tradition abandoned in new building work that by 1931 the Australian Cement Manufacturers’ Association was promoting the use of textures in Portland cement stucco—‘Spanish’, ‘Californian’, ‘Modern American’, ‘English Cottage’, ‘Italian’, and ‘Italian Travertine’.270 By a strange transposition these textures came to be widely understood as representing the definition of stucco.

## Conclusion

Common stucco, like so much else in Australian building, is essentially British in character, but somewhat retardataire in British terms, for it was still on the rise in Australia at the time when Pugin was castigating it in Britain. Cement, however, presents a different picture. In the 1880s, when the Gothic Revival and Arts and Crafts movements had driven cemented surfaces into retreat in Britain, the Australian Portland cement industry was taking off, and the Boom style encouraged the cementitious elaboration of ‘Benvenuta’ and other less distinguished buildings. So, vulgar though it may have been thought by some critics, the Boom style was distinctive, and it was largely generated by Portland cement. In the twentieth century the creative use of stucco declined, but so much of it already existed that it could not be ignored. The moral guilt associated with the Boom and Bust, the unfashionableness of cement ornament, and the gloom of discoloured Portland cement all combined to demand cleansing, lightening and simplification. Only in recent years has there been much call to halt and reverse this puritanical destruction.

Materials and Techniques 
of External Stucco

Barrie Cooper

abstract

introduction

materials

setting out

mouldings

features and enrichments

creating an original mould

conclusion

## Abstract

The main focus of this paper is external stucco as executed in Australia during the Victorian period (1837–1901). Stucco is the term used by the Italians for a superior plaster finish originally intended for internal use, and introduced into England during the Renaissance. The introduction of external stucco to give a brick house the appearance of stone is often attributed to the Adam brothers, and in particular to Robert Adam. Although this is not strictly true, it was their use of it that made it a generally acceptable external finish.

Early stucco, which was not very durable, and commonly fell off in patches, was executed by using sand and lime at 3 parts sand to 1 part hydraulic lime, finished with a set coat of five parts lime and two parts sand.271 This coat contained an additive (such as casein, crushed brick dust, or sometimes silicate) to increase the resistance to weathering, thereby making the finish coat a stucco finish. If hydraulic lime was used, an additive was not essential. In another form of application a thick coat of lime and sand in a similar mix as used in the finish coat is applied by splashing on with a brush over roughcast finishes to provide protection against the weather. Roman cement was used with some success, and examples such as Lyndhurst House, Glebe, NSW, of about 1834, still exist. External stucco was further improved by the advent of Portland cement in the mid-nineteenth century.

## Introduction

The art of plastering is one of the oldest trades known. From the various mixtures of mud and straw used over sticks and branches to form the walls and roofs of temporary dwellings (the precursor to wattle and daub) it has progressed to plasterwork on wooden laths, and thence to modern plastering techniques, and materials such as metal lathing. However, the materials and techniques of traditional plastering were basically the same throughout the world, because the conditions were essentially the same.

Although it is one of the oldest and most useful trades, very little technical literature has been written to inform the conservation architect or aspiring plasterer about the methods, technology and materials that can be used to replicate or restore traditional plastering work. Most books were written by plasterers who had a great knowledge and understanding of their craft, but tended to use technical terms without realising that the lay reader would fail to understand them. Meanwhile large multinational companies have promoted various methods and materials, which utilise less labour, and this has accelerated the decline of the plastering trade as once practised.

## Materials

During the early Victorian period, sand and lime plasters were commonly used on very simple external stucco with simple cornice work, and marked with ashlar blocking. Several examples of Roman cement stuccoed buildings were also built in the period 1830–1850, probably using imported Roman cement. Roman cement was so named following the discovery and use of nodules of septaria (the petrified excreta of extinct animals) found in the London clay formation, and was patented in 1796272—the nodules were fired to vitrification and crushed to a fine powder ready for use. The name was used because of the similarity of the material to original durable cements found in and around Rome.

Portland cement, which is in fact a form of hydraulic lime, superseded Roman cement for external stucco mainly due to the unreliability of the latter, of which the only real advantage is that it sets very rapidly. Portland cements are composed of clay and chalk or limestone, crushed and ground to a paste in water, allowed to deposit and then burned at high temperatures (1800ºC) again to the point of vitrification. The lime component was commonly unequally overburnt273—so great care was required in grinding and combining the materials of calcination to ensure regular setting properties (lime and natural cements fired at high temperatures are very difficult to slake, and need to be broken into small pieces or ground to a fine powder before use). Portland cement replaced Roman cement and the sand and lime mixes for external work when it became available in the mid-nineteenth century, and more elaborate decorations were possible. However, sand and lime internal plastering continued and many examples are found up to the 1950s, when internal cement render finishes started to gain favour, especially in Sydney.

The early types of cement were very different from those available in modern times, and the their hardness was far inferior to that of today’s Portland cement. Early cements were obtained from many sources and it is not possible to identify the origin of the cement used when carrying out repairs on cement stuccoed buildings. Therefore, the materials to be used are usually determined by the tradesman after visual examination for sand size, and mechanical testing to estimate the hardness. It is common for repairs performed on Victorian renders to be executed using a sand, lime and cement mix even though it is well known that when early cements were used they were not normally used with lime. The extreme hardness of modern cements makes them incompatible with early cements when they are used without lime, and usually results in excessive cracking at the joins between the old and new render.

The mixes used to simulate the various finishes range from 3 parts plastering sand to 1 part putty lime with pozzolan added at the rate of 25% to the lime component by volume, to renders consisting of 6 parts plastering sand, 1 part lime putty and 1 part Portland cement. Cement mouldings are usually run with a mixture of 
7 parts fine sand, 2 parts lime putty and 1 part cement so a sharp finish can be obtained. Early lime mixes used cow hair in the render and float coat to minimise cracking, but hair is not used in cement mixes.

## Setting out

Setting out is the first stage of a successful project. The façade is normally the most important part of the building, and the architect’s design needs to be transferred from the drawing to the building and brought to life. Where cornices are to be run, the bricklayer or stonemason would provide corbelling to carry the cornices and further corbelling where enrichments are to be installed over and under windows.

The first requirement for a perfect job is a plumb and flat wall. To this end, the façade is set out with dots using a plumb rule (in preference to a spirit level) to provide vertical and horizontal points for the screeds. The screeds are applied in a box format and then the area inside the box is filled in and the material ruled off flat to the screeds. Once the flat areas are completed, the mouldings can be run from the flat and plumb surface.

The dots are applied by placing a small dab of the mortar being used for the job at one end and a piece of lath or wood is bedded into the dab and tamped to the desired depth thus establishing the level of the finish. Other dots are then placed vertically taking a plumb line from the first dot. Dots are then applied to the other end of the wall in the same manner so the wall has two perfectly plumb sets of dots at each end of the wall. A string line is fixed horizontally to the corresponding dots at each end of the wall, and horizontal dots are installed across the wall at the depth indicated by the string line. After the dots have set or taken up, screeds are applied and ruled off the dots—to provide box screeds over the wall. Then, the inside of each box is filled in and ruled off the screeds. In some cases on large areas the mouldings are run off the screeds prior to the broad areas being filled in. After the mouldings are completed, the rendered surface is finished in the specified way. Some plasterers use nails for the dots instead of mortar.

The mortar applied should never be stronger than the substrate, as a stronger mix will eventually delaminate from it, or excessive cracking will appear in the surface. In some external stucco, crazing can be clearly seen, attributable to the sand used having a high clay content, or to the second or finishing coat of render being harder than the background. Prior to the availability of graded sands, it was common for plasterers to sieve their own sand for the pending work. To minimise the amount of sand to be sieved, the first coat application would contain the larger aggregate, and, to provide the fine finish, the sand would be passed through a fine sieve. If mixed at 
the same ratio as the first layer, the fineness of the sand would result in the top layer setting harder than the underlying layer, resulting in crazing of the surface. Therefore, the plasterer had to adjust the finish layer 
to avoid this.

Following the running of the cement moulds, enrichments—such as corbels and motifs—are cast in rubber or gelatine moulds and fixed in position by bedding with a cement mortar, or in the case of heavy enrichments, held in place by steel reinforcing pins set into the wall prior to fixing.

## Mouldings

The term ‘mouldings’ can be used to describe the in situ run moulds or the enrichments added after. Run moulds are formed with a cornice horse—as used for running internal plaster cornices—with the main difference being the time left between coats while building or coring out the background of the cornice before finishing. When running cement mouldings, each coat of the coring out should be applied in increments of no more than 20 mm, thoroughly scratched to provide a key for the following coat, and left at least 24 hours between each layer. Coarse sand can be used in the backing coats to minimise cracking and shrinkage, and again, the backing coats must be stronger than the finishing coat, or cracking will result. A safe mixture to use would be 
6 parts sand, 1 part slaked lime and 1 part cement for 
the coring out, and 7 parts sand, 2 parts slaked lime and 1 part cement for the finish coat. The accuracy of the gauging of the mixture is of paramount importance, and should be done with gauging boxes or buckets: a shovel should never be used because it is not possible to obtain accurate measurements.

The cornice profile is ‘horsed up’ and a running rule attached to the wall for the bottom slipper to run along—the top slipper runs on the finished render or the running screed installed for the purpose. The cornice horse must be checked and be perfectly plumb prior to running the cornice to ensure the render above the corbelling is parallel to the render below the corbelling—if they are out of line, the finished cornice will appear twisted. The top slipper has a zinc plate fixed to the front edge to prevent the wood from furring up, while the bottom slipper is coated with grease to make the horse slide freely. The cornice is sometimes finished by hand with small wooden floats shaped to the various profiles; all returns and stop ends are finished by hand using a joint rule.

In repair work, it is sometimes impractical to run short sections of mouldings, especially if remnants of the existing mould need to be retained and included in the repair—in which case the moulds are formed by hand in line with the original. In the instance illustrated, the original render and mouldings were executed in Roman cement, to match the qualities and hardness of the existing Roman cement, using modern materials. A mix consisting of 
12 parts of plastering sand, 4 parts of lime putty, and 1 part of class A Portland cement was used: the cement used at 25% of the lime by volume is similar to mixes using hydraulic lime (where a pozzolan would be used in place of the cement). Roman cement, early Portland cements and bagged hydraulic limes are more difficult to use than mortars made with putty lime. The ratio of sand to binder needs to be much richer to compensate for the lack of plasticity in the materials, and mixes ranging from 1½ parts of sand to 1 part of binder and up to equal proportions of sand and binder, were common. Mixes of 3 parts sand to 1 part binder are impossible to spread and very ‘hungry’ (a term used to describe a mortar rich in sand). In 1836 the New South Wales Government specification for plastering called for external render to consist of 50% sand to 50% cement, and a similar 
contract dated in 1864 specified the render to be 50% sand to 50% best Portland cement. The first contract was probably specifying Roman cement and the second an early Portland cement.274

## Features and enrichments

The Victorian house was commonly enriched with ornamentation in the form of cornices and castings—iron lacework was used as a feature, and elaborately decorated roof parapets with balustrades and finials cast in cement adorned the façade. Various methods were used to create the different effects and finishes including using stencils, casting and fitting cast cement moulds, and using timber mouldings to carry the ornamentation over timber substrates. Creating an original model in clay and then making a mould to be used for the casting is similar to the methods used for internal plaster moulds. In former times, moulds were made using gelatine (from animal) or elgin (from seaweed). However, both had the common problem of splitting during the removal from the cast—on projects with repetitive enrichments, it is quite easy today to establish the point at which the mould had deteriorated to a level where the casting quality had declined, and it was necessary to renew the casting mould. The original carving, made from clay or wood or a combination of wood and plaster or clay and plaster, was kept close by so new casting moulds could be made as required.

## Creating an original mould

The first requirement in creating a mould is to make an original. In the example illustrated, a motif to be used on the gables of an 1836 colonial house275 and featuring the Prince of Wales feathers, is made in the same method as used to make corbels, decorative rosettes and other enrichments. The original mould is made using modelling clay for the feathers and plaster for the border. The plaster surround is run on a bench in circles and the sections cut and fitted to their positions to form the border. After the mould is completed and all the details checked (it is important that the details are checked thoroughly at this point because after the silicone is poured and set, the mould cannot be changed), a barrier is formed around the whole model to contain the liquid silicone rubber276 (which is to be used to make the casting mould). The height of the barrier should be just above the height of the highest point of the model, and the barrier should be kept close to the model to minimise the amount of silicone used. After the silicone has been poured and allowed to cure, the mould is backed with a plaster backing (which must be applied before the silicone is released from the model) and this will hold the rubber in position during the casting process. When the plaster backing is cured, it is removed from the silicone. The silicone is then peeled from the model and laid into the plaster backing, and the mould is now ready for casting.

There are various other methods of making moulds if the model is made with plaster or wood. One method is to cover the model with a thin layer of clay and form the plaster backing over the clay. The plaster backing is removed when set, and the clay removed from the model: the backing plaster is then fitted back over the top of the model, and holes are drilled in the plaster backing allow the silicone rubber to be poured in through the holes, filling the void left by the clay. This method is particularly useful in reducing the amount of silicone rubber being used, and thereby lowering the cost. For models with low relief modelled from clay, wax moulds are commonly used, as are plaster moulds. The latter require a release agent to be applied to the surface prior to casting—the most common of which is a very fine coating of clay applied in a liquid form, utilising the suction of the plaster to control the thickness of the clay coating.

After the casting is set, the mould is turned over and tapped on the bench to remove the cast—an action termed ‘knocking out’. When the castings are complete they are fixed into position and in the instance illustrated the moulds have been recessed into the substrate so the surface, which would have been the line of the casting table, is in line with the finished render.

Because of the size and weight of the moulds (800 mm diameter and approximately 12 kg) stainless steel pins are fitted into holes drilled into a thick section of the casting with corresponding holes in the substrate. The pins are cemented into position during the fixing of the castings, which are normally well soaked before adhering with a cement rich mix, or in modern times an epoxy modified mortar. Once fitted, the render around the moulds is repaired to match the surrounding surface finish, and painted after a thorough drying. The mix used for the castings was 3 parts sand to 1 part cement with a super plasticiser and de-foamer added to increase the slump and reduce air entrapment. Unlike gypsum plaster castings, cement based mouldings need to be left to cure for at least two days before removing from the mould to avoid breakages. The method for making the more common mouldings and enrichments is the same. Cornices run in situ are often enriched with cast mouldings fitted into a purpose-formed recess.

Many mouldings and enrichments used on Victorian houses—from the smallest homes to the largest mansions—share common features. This is especially true of the later period, when Portland cement was the favoured material for external plastering. For example, heavy bracketed cornices, usually enriched with floriated medallions and corbels, were used to support a balustrade or roof parapet. There is often a central feature incorporating a cast decorative acroterion, together with other decorations chosen by the architect or plasterer. The terrace houses ‘Romla’ and ‘Frelin’277 are classic examples, and contain some fine Victorian stucco and enrichments. There are corbels in cement and wood; acanthus leaf capitals; half rounded fluted composite stucco pilasters; a heavy cornice and balustraded parapet; vermiculated blocks; and unusual sgraffito. (Graffiato, sgraffiato, or scraffito, mean simply scratched into the surface.) The methods of creating the majority of these features have already been addressed: the methods of creating the other enrichments are as follows.

For incised work, a scratch coat of 3 parts sand to 1 part cement (6 parts sand, 1 part lime and 1 part cement for modern materials) is applied to the substrate and thoroughly scratched to provide a key for the top coat and to reduce the suction. The scratch coat is allowed to cure overnight before applying the top coat. The top coat is applied and finished with a wooden float and steel trowel. An outline of the intended pattern is drawn on a thin piece of board and the outline thoroughly pricked, the pattern is placed and fixed into position over the work area and the surface ‘pounced’ (a cloth bag containing charcoal powder is tapped over the holes in the pattern) to mark the outline of the design onto the rendered surface. The pattern is removed and the design carefully cut into the render extending down to the scratch coat—a tool with a rounded end gives the desired cupping effect inside the dug out areas. After the whole pattern has been cut, and the material removed, a small log brush is used to gently clean the pattern to an overall smooth finish.

Sgraffito decorations are created in much the same way, with the addition of a coloured background in the pattern. Where sand and lime or a cement rendered building were left unpainted, which was often the case, sgraffito was the main mode of decoration and was used in conjunction with coloured stucco finishes on the flat areas of the wall with ashlar blocks lightly marked in the surface—sometimes with mouldings providing a frame for the sgraffito work.

The application of a scratch coat is the same for the vermiculated pattern, then the design is marked over the scratch coat and approximately 3 mm of coloured render is applied—only in the areas that will be exposed when the top coat is removed. The thin coat of coloured render is allowed to cure until firm; the top coat of render is then applied over the top at the normal 10 mm thickness and finished with a wooden float and steel trowel pressed; and the pattern is then fixed into the same position as for the background and pounced. The pattern is removed and the render carefully dug out to expose the coloured background. The cuts in the design should be slightly angled towards the centre to give an illusion of greater thickness. The finished design is cleaned with a small log brush to remove excess material from the coloured background. There is no coloured render used if the building is to be painted—in which case the design is placed over the scratch coat while still green, pounced and the surface of the scratch coat flattened in the marked area. It is important to use the same fixing holes in the pattern and the corresponding holes in the wall each time the stencil is used..

## Conclusion

The term ‘stucco’ originally referred to the material used to effect the finished plastering work and create a coloured, imitation marble or weather-resistant surface. Although there is no Latin word ‘stucco’, in the Ten Books on Architecture, Vitruvius devotes a chapter to the topic, and states that walls ‘rendered solid by three coats of sand mortar and as many of marble [dust], will not possibly be liable to cracks or to any other defect.’278

The revival of stucco work in the Renaissance period utilised lime plasters modified with animal glue or size (stucco duro) and it gained wide acceptance for internal use. The stucco materials were similar in many respects to the gesso materials used by artists and for decorating wooden objects, the main difference being that the gesso made use of gypsum in the form of plaster of Paris and used greater amounts of glue or size. Wilfred Kemp refers to ‘the stucco for the finishing coat’279 and states that ‘the stucco coat can be coloured by mixing certain metallic oxides and earths with it.’280 He later says:

When stucco is composed of plaster of Paris instead of lime lukewarm size water is very generally employed for gauging it. This is usually made by dissolving some fish glue or gum Arabic in the water so as to cause the mixture to be homogeneous and avoid porosity of the surface, thus, in cases where the stucco is subsequently polished, enabling a superior degree of gloss to be obtained.281

However, in a later example of a specification for a dwelling whose exterior is to be stuccoed, Kemp describes the whole of the external plastering, including the walls, cornices, string courses and mouldings, as using a ‘compo’ of blue lias lime mixed with sharp river sand in the proportion of 2 parts sand to 1 part lime.282 He relies upon the fact that the plasterer would know how the walls are to be stuccoed following the application of the compo. The methods employed for external stucco and internal stucco are different in the manner of application. Also, the external stucco layer must be applied while the preceding coat is still wet, so the render coat is applied and thoroughly scratched, the render or scratch coat can be left to cure but the float and stucco are applied on the same day. For internal stucco the base coats can be allowed to cure before applying the stucco layer.

The term ‘stucco’ applied to external finishes means that a stucco layer has been used to finish the work and close the surface, making the plasterwork harder and more durable. A typical specification such as that above would typically read, with details added:

Compo the whole of the walls including the cornices, string courses and mouldings with 1 scratch coat and 1 float coat at a minimum of 5/8 inch thick total 
for the two coats. The mixes to consist of 2 parts sand to 1 part blue lias lime, on the same day apply 
a third and final coat of stucco at approximately 
1/8 inch thick, the stucco layer to consist of 1 part 
fine sand to 1 part blue lias lime and trowel to a smooth flat and closed surface, the total thickness of the stucco work not to be less than ¾ inch thickness.

The introduction of Portland cement allowed external plastering to be completed in two-coat or even one-coat work, and although most modern cement rendered walls did not utilise a stucco layer they were very often referred to as stucco, so the original term became misused to describe all external plastering and often ordinary internal plastering, which appears to be the current practice.

Barrie Cooper is a third generation plasterer and during the past 47 years has been involved in plastering in England, Italy, China, Malaysia and Australia. In 1980 to 1984, he completed four years of a seven year course on Industrial and Analytical Chemistry and has also worked for the last 
24 years as an industrial chemist. Since 1976 he has been Managing Director of Westlegate Pty Ltd, manufacturers and suppliers of the Westox range of traditional building materials and restoration systems. He has also been employed as a casual lecturer on traditional plaster restoration by Sydney University and Sydney College of Technical and Further Education.

External Renders: Materials, 
Properties and Conservation Issues

David Young

Introduction

limes

non-hydraulic lime

lime putty versus dry hydrated 
lime powder

hydraulic limes

cements

comparison of lime, hydraulic 
lime and cement binders

aggregate—sand

mineralogy and colour

impurities

grain shape

size grading

clays and fine silts

void ratio

conservation issues

significance

compatibility

application of significance 
and compatibility criteria

conclusion

## Introduction

External renders are made from the same materials commonly used for mortars: a binder, such as limes or cements, or a combination of these, and an aggregate, which is generally sand. Additives are sometimes used to modify the properties of the wet mix or the performance of the cured material. Like mortars, external renders are applied in a wet (plastic) state and allowed dry out and set, gaining strength on the wall. This paper is a brief review of the nature, production and properties of their materials. It concludes with a discussion of some of the issues that should be considered when conserving nineteenth and early twentieth century examples. The common term ‘render’ is used throughout this paper to distinguish external renders (and associated mouldings) from internal plasters.

## Limes

Prior to the development and widespread use of Portland cements in the latter part of the nineteenth century (see Lewis, in this volume) the dominant binder was lime, a material, which has been used in building construction 
for thousands of years.

Lime binders come in several forms and it is important to be clear about the differences between them, and the sometimes confusing terminology. Limes may be ‘non-hydraulic’ or ‘hydraulic’.

### Non-hydraulic lime

Non-hydraulic limes were the lime binders most commonly used in Australian building construction. They were used for bedding mortars in domestic construction until the major changes in industry and building that followed the Second World War. Generally described as just ‘lime’, the term non-hydraulic implies that they do not set by reacting with water, in contrast to hydraulic limes and cements, which do. Instead, non-hydraulic limes set by reacting with carbon dioxide in the air. The term ‘air-lime’ is sometimes used to describe these limes and to indicate the nature of the setting reaction.

Non-hydraulic limes come in two distinct forms: as a wet putty, commonly described as ‘slaked lime putty’ or just ‘lime putty’; and as a dry powder, known as ‘dry hydrated lime’, or simply as ‘hydrated lime’. This latter material is the ‘builders lime’ that is sold in bags by hardware merchants. Do not confuse these materials with ‘agricultural limes’ (ag limes) which are used by gardeners and farmers for sweetening otherwise sour (acidic) soils. Agricultural limes are simply limestones that are ground 
to a powder; they have no binding power.

Non-hydraulic limes are made by burning (calcining) relatively pure limestone (or shells, or marble) in a kiln at a temperature of about 900˚C to produce quicklime (also known as rock lime) as shown in the following reaction. Carbon dioxide gas is given off to the atmosphere, there to add to the greenhouse effect.

1.	Limestone (calcium carbonate) + heat = quicklime (calcium oxide) + carbon dioxide gas
CaCO3 + heat (900˚C) = CaO + CO2

After cooling, the quicklime is combined with water in the process known as slaking, or hydration, to form either slaked lime putty or dry hydrated lime.

2.	Quicklime + water = slaked lime (calcium hydroxide) or just lime CaO + H2O = Ca(OH)2

In traditional production excess water is used to produce a wet lime putty, a mixture of lime and water—Ca(OH)2 + H2O. In modern industrial production exactly the right amount of water (as steam) is used to produce the dry powder form—dry hydrated lime, Ca(OH)2. Adding water to produce a dry powder may seem counter-intuitive, but it happens because the water is incorporated into the new chemical structure. The separate use of the terms slaked lime (for putty) and hydrated lime (for powder) is not strictly correct. Both the putty and the powder have been slaked and both are hydrated lime.

Lime is chemically calcium hydroxide, and this, either as a wet putty or as a dry powder, is the binder that is mixed with sand (and water, if using the dry powder) to form a mortar or render material. Once in the wall, the lime sets by absorbing carbon dioxide from the atmosphere to produced calcium carbonate according to the following reaction, which is known as carbonation.

3.	Lime + carbon dioxide = calcium carbonate + water
Ca(OH)2 + CO2 = CaCO3 + H2O

The excess water produced evaporates, leaving interlocking crystals of calcium carbonate that bind the sand grains together in the render or mortar. The cured binder is chemically the same as the limestone raw material, and the whole process forms a cycle, which 
is illustrated here.

### Lime putty versus dry hydrated lime powder

Though apparently the same chemistry, there are noticeable differences between a mortar made with lime putty and one made from the dry powder. Lime putty is more workable (buttery or creamy) and produces a stronger mortar than the dry powder. This is because maturing the lime putty before use leads to finer particle sizes and more planar shapes, both of which make the mix more workable, an important factor for renders (and internal plasters). The higher surface area of the finer particles leads to greater reactivity and stronger bonds.

Dry hydrated lime powder can be made more workable by soaking it in water 24 hours before use. This is not ‘slaking’, but running to a putty, or slurry, as it is described in Australian Standard 1672.1. Even so, the result will not be as good as a mix made from a directly slaked lime putty. This is because the particle size will never be as fine and because some of the dry powder will set (carbonate) in the air, so that a proportion of material has already gone off.

### Hydraulic limes

Like cements, hydraulic limes (or rather, a part of them) set by reacting with water in a process known as hydration. They do this because of the presence of finely divided silica (either in the raw material, or added later). The material produced on setting, hydrated calcium silicate, is a very different binder from the calcium carbonate of non-hydraulic limes. Hydraulic limes 
can be ‘natural’ or ‘artificial’.

Natural hydraulic limes are so named because their limestone raw material naturally contains silica (as flint nodules or as silicate minerals in clays) in the correct proportions for the binder. Such limestones are described as argillaceous (for clay bearing) or siliceous (for silica bearing) limestones. They are burnt at temperatures of up to about 1000˚C, which produces a reaction between some of the quicklime and the silica to produce calcium silicates according to the following reaction.

4.	Limestone + silica + heat = hydraulic lime 
(calcium silicate) + carbon dioxide
CaCO3 + SiO2 + heat (~1000˚) = CaSiO3 + CO2 (formula not accurate)

The chemistry of calcium silicates is complex and the reactions shown here are not accurate but are included 
as a guide. The hydraulic component sets by reacting with water as follows.

5.	Hydraulic lime (calcium silicate) + water = hydrated calcium silicate CaSiO3 + H2O = CaxSiOy(OH)z 
(formula not accurate)

Again, the formula is not accurate; x, y and z represent variables. There are also reactions between quicklime and alumina in clays, but these have been omitted for simplicity. As they set, the hydraulic components consume the mixing water and grow as tightly interlocking needle-like crystals, leading to greater strengths than are possible with non-hydraulic limes.

Like cement, natural hydraulic limes are available only 
in dry powder form. It is important to be clear that in 
a bag of hydraulic lime there are two types of material; some which is hydraulic (and sets by reacting with the mixing water) and some which is non-hydraulic (and sets by reacting with carbon dioxide in the air), the relative proportions of each determining the degree of hydraulicity. Setting of hydraulic limes involves both hydration and carbonation reactions.

Natural hydraulic limes are not made in Australia, but are imported from Europe where there are a number of manufacturers. These products are commonly described as NHL2, NHL3.5 or NHL5, depending on the degree of hydraulicity (NHL stands for natural hydraulic lime, and should not to be confused with non-hydraulic lime).

Artificial hydraulic limes can be made by combining non-hydraulic lime with reactive siliceous materials known as pozzolans. The term ‘pozzolan’ is derived from the original source, Pozzuoli, near Naples in Italy, where there are large deposits of volcanic ash. Pozzolans have no binding power of their own but when mixed with non-hydraulic lime make a portion of it hydraulic and so increase the strength of the resulting binder. Pozzolanic materials include volcanic ash, such as the original from Pozzuoli, and a German ash known as trass, as well as a variety of manufactured materials such as crushed underfired bricks, fly ash from coal-fired power stations and activated kaolin (metakaolin) which is a calcined (heated) clay.

Although the pozzolan and the lime are mixed cold (and are not burnt together in a kiln) a reaction occurs between them because of the very fine particle size (and hence high surface area) of the pozzolan. The reaction produces a similar result to that of a natural hydraulic lime.

6.	Lime (calcium hydroxide) + pozzolan (silica) + 
water = hydrated calcium silicate
Ca(OH)2 + SiO2 + H20 = CaxSiOy(OH)z 
(formula not accurate)

Pozzolans can be added to lime putties or to dry hydrated limes. As before, better results will be achieved with putties because they are more reactive. Pozzolans can also be added to hydraulic limes to increase their hydraulicity.

The terms ‘natural’ and ‘artificial’ apply only to the source of the raw materials and are rather archaic. It is important not to be seduced by the feel-good connotations of the term ‘natural’; except for deep beneath the earth’s crust, there’s not a lot that is natural about being at temperatures around 1000˚C.

## Cements

Cements differ from hydraulic limes in consisting only of hydraulic materials. Like hydraulic limes, there are natural and artificial cements, and the terms relate to the source of the raw materials. Natural cements are made from argillaceous (clayey) limestones of just the right proportions so that on firing at moderate temperatures they produce a material that, after grinding to a fine powder, reacts with water to form complex hydrated calcium silicates and aluminates.

Artificial cements such as today’s ordinary Portland cement (OPC) (described as Type GP by Australian Standard 3972) are made by grinding together a mixture of about 80% limestone and 20% clay or shale (as sources of silica and alumina) together with other minor ingredients, and firing them at a temperature of around 1450˚C. The resulting partially-fused clinker is not reactive until it is finely ground, whereupon it becomes so reactive that a retardant in the form of gypsum is added to provide working time sufficient for normal use. Portland cements have a complex chemistry and the following reactions are considerably simplified.

7.	Limestone + shale (alumino-silicates) + heat = cement clinker (complex calcium alumino-silicates)
CaCO3 + AlSiOn + heat (~1450˚) = CaxAlSiOy 
(formula not accurate)

Cement sets by reacting with the mixing water to form 
a hydrate.

8.	Ground clinker + water = cement paste 
(complex hydrated calcium alumino-silicates)
CaxAlSiOy + H20 = CaxAlSiOy(OH)z + Ca(OH)2 
(formula not accurate)

Although the cement binder is entirely hydraulic, its setting produces free (non-hydraulic) lime, which makes up about 20% of hardened cement paste. This free lime is utilised in ‘blended cements’ (type GB, Australian Standard 3972) which contain about 20% of pozzolanic materials such as flyash. The result is a cement, which sets more slowly but ultimately reaches higher strengths than OPC.

## Comparison of lime, hydraulic lime and cement binders

The following table compares the properties of limes and cements. It is a considerable simplification of a large amount of data across a wide range of materials. Although grouped into the three categories previously described (non-hydraulic limes, hydraulic limes and cements) there may be a wide range of results for each listed property and the variation within any one group can be high. Thus the setting rate of hydraulic limes, which is described here as intermediate, varies from relatively slow to moderately fast depending on the (increasing) hydraulicity of the lime. Similarly, the workability of non-hydraulic limes will vary with the ‘richness’ (purity) of the lime; a ‘lean’ (impure) lime will be less workable and require a stronger mix than a rich or ‘fat’ (pure) lime. And the strength of cements will vary depending on whether they are natural or artificial. Further, modern Portland cements are many times stronger than the Portland cements of the late nineteenth century.

| Property | Limes (non-hydraulic) | Hydraulic limes | Cements |
| --- | --- | --- | --- |
|  | Includes rich and lean limes, putty and dry hydrate | Includes natural and artificial hydraulic limes | Includes natural and artificial cements |
| workability | good | moderate | poor |
| pot life when mixed | long | intermediate | short |
| setting mechanism | carbonation | hydration + carbonation | hydration |
| setting rate | slow | intermediate | fast |
| strength | low | moderate | high |
| elasticity | good | moderate | brittle |
| pore structure of mortar | open | partially blocked | mostly blocked |
| salt content | negligible | negligible to low | low to moderate |

## Aggregate—sand

The attention paid to sands is often slight compared with that devoted to binders. Yet sands make up the greater proportion of mortar and render mixes and their selection can be critical to achieving workable and durable results. While good sands will make good mixes, acceptable mixes can often be made from poor sands, provided care is taken in their formulation and mixing.

Sands are technically described as fine aggregate, and are distinguished from coarse aggregates (gravels) that are also used in construction. Sands are generally natural materials and are excavated from dunes, pits, river beds and river terraces. Though ‘natural’, sands are often highly processed, being passed through sieves of varying sizes (screening) to remove over and undersize particles and to adjust their grading. Materials from different sources are often blended to provide sands with particular properties. Washing of sands is commonly undertaken during screening to remove clays and other unwanted materials. As their name suggests, dry-screened sands are unwashed.

The relevant properties of sands include:

- the mineral type (mineralogy) and colour of the sand grains

- unwanted impurities, such as organic matter and salt

- the shape of the sand grains—‘sharp’ or ‘soft’

- the range of grain sizes—the size grading

- the undesirable presence of clays and fine silts

- the proportion of voids between grains—the void ratio.

### Mineralogy and colour

The most common sand mineral is quartz, which is the principal component of many light-coloured beach sands and has a typical clear or light grey-colour. Quartz is chemically silica (SiO2) and is very strong and durable. Sands with darker coloured particles include silicate-based materials that can also be strong and durable.

Some beach and coastal dune sands consist of shell fragments, broken up and reduced by constant wave action. These sands are chemically calcium carbonate (CaCO3—the same as limestone) and are known as lime sands. Being softer, their grains tend to be more rounded in shape and their whitish colours are more opaque. While they are not as strong as silica and silicate materials, they may make acceptable mortars.

Although pure quartz is clear, many quartz sands have yellow, pinkish and reddish colours due to very small amounts of various iron minerals dispersed through the quartz. Further, the colour of some quartz sands is due to thin clay and iron oxide coatings on the outside of otherwise clear grains. Where the coatings are weakly bonded to the grains, the sand will not make a strong mortar and washing alone may be sufficient to remove the coating, and with it, the colour. The overall colour of many sands, and mortars made from them, is largely due to the colour of the finer particles.

### Impurities

Good sands are free of impurities, which commonly include organic matter, salts and clays. Organic matter may be leaf and tree litter and humic material from soils. These are avoided by careful selection during quarrying and by washing and screening the product. Salts are a problem, as they may lead to salt attack in the cured render. Sands may therefore need washing to remove salts, particularly if they were obtained from coastal locations. Sand excavated from ephemeral inland streams may also contain salt. Another source of contamination can be sand containing sulphide minerals, such as pyrite (iron sulphide), which oxidise on exposure to air to form sulphate salts, which can be very aggressive. Clays as impurities are discussed later.

### Grain shape

Good sands are ‘sharp’—they feel sharp or abrasive when rubbed in the hand. Their angular shape leads to good interlocking of grains and good contact between sand grains and the substrate, which may be brick or stonework, or previous layers of render. In contrast, ‘soft’ sands are well-rounded, leading to weak mortars and renders, which do not key well to their substrates. Grain shape is technically described by the range: angular—sub-angular—sub-rounded—well-rounded. Good sands are sub-angular to angular in shape.

### Size grading

Size grading refers to the range of different grain sizes found in a sand and is perhaps the most critical property. Good sands have a wide range of grain sizes, so the gaps between the coarse grains are filled with medium size grains and progressively finer grains fill the smaller gaps. One result is a reduction in the void ratio, which is explained later. Another is improved workability. Although it may sound unlikely, a sand with a good range of grain sizes (including coarse grains) will be more workable than a sand made from a single or narrow range of grain sizes even though they may be fine or medium sizes. This is because the components of a ‘well-graded’ sand fit well together and fill up the gaps between grains (the void space) as described above.

### Clays and fine silts

As the grain size becomes finer, we pass from fine 
sands into silts and then clays. While a small proportion of coarse silts may be acceptable, fine silts and clays are problematic because of their high surface areas, which must be coated to ensure good bonding. With fine silts and clays the particle size is more similar to that of the binder which leads to a stacking effect where the binder (in order to coat all surfaces) must force the aggregate grains apart, which in turn means more binder to fill the additional voids created.

Sands with high clay contents are often favoured for use in bricklaying because the clay improves the workability of otherwise harsh cement mortars. This is common, but bad practice; sands should be free of clay and workability should instead be sought through good size grading, choice of binder and appropriate use of additives.

Note that this discussion applies to renders made from sand and a binder, and not to those renders that were clay-based, such as may have been used on earth constructions like adobe and pisé de terre. In these the clay material is both the binder and the aggregate and the use of clay for their repair or reproduction is entirely appropriate, whereas clays should be excluded from renders made from sand and lime and/or cement.

### Void ratio

The void ratio of a sand is the proportion of voids (or air) in a dry sand and is expressed as a percentage. The void ratio of normal sands ranges from about 30% to about 40% of the volume of the sand. In a good, sharp, well-graded sand the void ratio will be about 33%, or one third of its volume. When making a mortar mix the aim is to fill this remaining space with a binder, and this leads to the traditional mix proportions of 1:3, one part binder to three parts of sand. Void ratios of up to about 40% can be found in some sands such as beach sands that are well-rounded and poorly-graded. Such sands require mix proportions of 1:2.5, one part binder to two and half parts sand (i.e. 40 to 100) simply to fill the voids. Very fine sands will require higher proportions of binder (often 1:2 and sometimes as rich as 1:1.5, or even 1:1) to allow for the poor size grading, the increasing surfacing area of the sand and the stacking effect noted above.

The void ratio may seem like an academic consideration, yet it is critical to determining the workability of a mortar 
(or render) mix. A sand with a 40% void ratio will not produce a workable mix if used in the standard proportions of 1:3 (one part binder to three parts sand). At these proportions the sand will be ‘hungry’ and the plasterer will want to add more water to make it workable. Better practice is to add more binder instead of adding water. Better practice still is to know the correct proportions from the beginning, by measuring the void ratio of the sand. Even then, some licence must be given to the tradesperson to adjust the mix slightly to suit the particular materials being used.

## Conservation issues

As well as treatment of the existing renders, their repair and conservation may involve patching small areas and reconstruction across larger areas. For patching and reconstruction work, decisions about the choice of materials and their mixes should be based on two criteria:

- significance of the building and the existing renders

- compatibility of the proposed replacements.

These criteria are explained below, followed by some examples of how they are applied.

### Significance

Where the existing renders are of cultural significance, their conservation should be based on the principles of the Burra Charter, including, retention of as much significant material as possible, the preferred use of traditional materials and techniques, and like-for-like replacement where needed. These imply matching the original materials in nature, colour, texture, grain size and proportions. To do this well, the existing renders need to be researched and closely studied and analysed in order to determine their make up.

Significance cannot be the sole factor determining the choice of materials. Some traditional materials are simply not available, or are not available in the form they were in when used in the nineteenth or early twentieth centuries. This may force us to choose alternative materials and here the question of compatibility is critical.

### Compatibility

New materials, and render mixes made from them, should be compatible with the existing render and with the substrate to which they are to be applied. This will commonly mean producing a mix with porosity and strength characteristics which are similar to the original. The key compatibility criterion is that the new materials and mix should not damage the original render or the substrate.283

In developing a replacement render mix we should begin with the original materials and mix (or as close to them as we can get) and then consider whether the compatibility criterion will be satisfied in the particular circumstances. We may need to modify the original mix to ensure that:

- it is weaker than the original (and so behaves sacrificially)

- it has appropriate porosity and permeability

- potential problems such as soluble salts can be managed

- there are no adverse side effects of the repairs.

### Application of significance and compatibility criteria

The following examples illustrate how the significance and compatibility criteria are applied.

Replacing a lime-based render on a soft brick substrate with a hard cement-based render would not only fail the significance test (because it’s not the same as the original) but also the compatibility test, for the new render would be incompatible with the original render and with the substrate. It is important that a replacement render is weaker than the original, so that any failure will preferentially occur in the repair work, thus protecting the older fabric of heritage value.

Replacing a nineteenth century 1:2 or 1:3 cement:sand render, such as a recommended by Nangle,284 with a 1:2 or 1:3 render made with modern Portland cement would fail the compatibility test, because modern Portland cement is much stronger than that of the nineteenth century. A new render made this way would be too strong for the adjacent original, and possibly too strong for the substrate as well. The challenge in these circumstances is to design a cement-based render that is slightly weaker than the original, yet has similar porosity and permeability. One approach would be the use of masonry cements (Australian Standard 1316). These are cements, which have lime or inert fillers (such as powdered limestone) added to reduce the strength of the resulting mix. Another would be to obtain cements made to lower strength standards than are used in contemporary reinforced concrete construction—but even here there may be the need to include an additive to reduce the strength of the resulting mix. In either case, the final proportion of cement to sand will be very much lower than 1:2 or 1:3. Strength is only one of the characteristics which need to be taken into account: thermal and moisture expansion, flexibility, durability, porosity and permeability all need to be considered and, depending on the particular circumstances, one or two of these characteristics may be more important than others.

Providing appropriate porosity and permeability characteristics may necessitate adjustment of the 
size grading of the sand (to remove clays or fine silts) or the judicious use of air entraining agents.

Managing salt problems will be necessary where failures in the render have allowed rain to carry soluble salts into the masonry over a long period, or where ineffective damp-proofing has allowed rising damp to carry salts up into the walls. Even after a desalination treatment, such as poulticing, some salt will remain in the masonry and the replacement render should be designed to allow the salt to migrate into the new material and so protect the original. 285 This will mean careful control of porosity and permeability and may require the use of air-entraining agents, porous particulates, or the replacement of some of the cement in the mix with lime, which has greater porosity.

Pre-wetting, the thorough wetting of the substrate to control suction and prevent rapid dehydration of the mix, is an important aspect of good practice. However, there may be an adverse side effect should too much water penetrate through the full thickness of the wall and lead to damage to valuable internal finishes. In such circumstances, the use of water-reducing agents in the mix may be appropriate.

## Conclusion

Good conservation of external renders requires a thorough understanding of the mechanical, physical and chemical properties of the existing renders286 and of the reasons for their failure. Successful repairs will only be made where this knowledge is combined with similar understanding of the properties of the replacement materials. To this must be added the essential trades skills needed to carry out the work.

David Young, OAM, is a heritage consultant with a science and materials conservation background. 
He provides specialist advice on the repair of historic buildings and sites throughout Australia. He writes technical guides and runs heritage training programs, including summer schools in building conservation and heritage management at the University of Canberra.

Testing of stucco

David West

visual inspection

general overview

hands-on overview

detailed survey

tap testing for drumminess

infra-red thermography

sampling

opening up

finishes

visual testing in the laboratory

chemical testing

physico-chemical testing

physical properties

samples

Validating reproductions

These notes summarise my thoughts on the testing of stucco—from the general to the specific. They are intended to provide some basic pointers rather than to be a manual on the topic. Readers wishing to gain more detailed information about the methods described here will find several informed articles in APT Bulletin: the Journal of Preservation Technology.287

## Visual inspection

I’m going to start with one of the most important tests for assessing stucco—visual inspection. Looking at the stucco can tell us many things about it. How do we look at it? I would do the following:

### General overview

Start by walking around the outside of the building:

- as close as possible

- at least 30–50m away from it.

This is done in order to get perspective on the 
distribution of:

- the stucco itself and other materials on the building

- any discolouration or staining

- any cracking

- any loss or spalling.

### Hands-on overview

Get close enough to the stucco to touch it and look at a range of things including:

- the texture of the surface

- the presence of any evidence of past surface finishes or treatments

- interfaces with other materials (for evidence of original finishes)

- hidden areas of original finishes

- each type of discolouration or staining—to identify what it is, and if possible, how it was caused

- each type of crack—to determine if it is active or old, whether there is associated delamination (drumminess) and if possible, what caused it

- each type of loss or spalling—to determine possible mechanisms of deterioration

- other evidence of deterioration.

This will provide the basis for a typology of deterioration and defects in the stucco in preparation for a detailed survey.

### Detailed survey

The detailed survey is preferably done close up (hands-on survey) but could be done by binoculars or telescope (visual), and:

- involves mapping the distribution and quantity of each type of deterioration and defect

- probably includes drumminess survey

- might identify location for opening up or sampling 
of stucco

- might involve taking samples for lab analysis.

Visual inspection is a necessary precursor to testing, because it allows you to define what you want to find out, and why—without this, testing is spending money to get data that may be of little use or meaning.

## Tap testing for drumminess

This basically uses sound to map areas of delamination between stucco layer or layers and the substrate. There are many different methods, the most common are:

- hammer

- dragging.

Tuning (attuning) the ear is very important: one can often differentiate between delamination at different depths in wall coating system and different thicknesses of gap from the different sounds. This needs experience and careful attention, as well as later correlation.

Testing for drumminess involves:

- mapping the distribution of drumminess

- using a grid system, or relating sounds to cracks and architectural detail

- removing samples of drummy material to validate drumminess survey (often combined with a safety survey to remove pieces at risk of falling into public areas).

## Infra-red thermography

This is undertaken away from the building, and needs a clear view of façade to be feasible. To be effective, it requires a temperature difference and active temperature gradient, as it is dependent on heat contrasts. The surface temperature of the stucco over an air-gap (delaminated region) is different from the temperature of stucco which is bonded to the substrate. The temperature gradient is most commonly achieved in early morning as façades warm up with sunlight, but it can also be achieved at night as the surfaces cool down. Interpretation requires care, as areas of dampness will also be represented by different temperatures. The survey provides a tool to identify areas of differentiation, rather than absolute demarcation of the drumminess.

Infra-red thermography is generally used to identify:

- anomalies

- structural changes

- moisture

- intermediate layers.

If the materials are known, appropriate modelling can be used to quantify time and energy, but very sophisticated software is required, and it is usually not conclusive.

## Sampling

Where stucco samples are to be removed for laboratory analysis, it is necessary to identify which tests are to be done, as this will determine the size, mass, and condition of the samples required. When samples are taken from areas of loss or spalling, it is important to know whether they are truly representative. All samples should be removed with care to minimise overall damage to the building. All must be labelled at the time of collection to avoid any future confusion, and stored in protective containers together with their labels.

## Opening up

Stucco or other materials may need to be removed to reveal unseen conditions and to identify areas of original finish or unweathered material for the purposes of comparison. This might establish the number of layers of stucco, and the approximate thicknesses in different areas, and might also establish or confirm the nature of the substrate material.

Opening up may be done by means of drilled holes, core holes, saw cut slots or patches, or rough chiselled-off lumps. Sound areas (with no evidence of deterioration) and deteriorated areas should be compared.

## Finishes

To determine the true nature of finishes, paint scrapes may be done, samples taken, or original surfaces exposed by removing original fittings or early additions. The samples should ideally be examined under a microscope, either on site or in the laboratory. Comparative elemental analysis of samples of the surface and the body of the stucco can be done to determine whether a finish coat is of a composition significantly different from that of the body mix. Scanning electron microscopy with x-ray analysis might be useful to answer particular questions about the composition of finishes.

## Visual testing in the laboratory

Using a hand specimen, stereo microscopy should reveal the surface texture, layering, deterioration and original finish.

Using a thin section under a petrographic microscope, it may be possible to determine the identity of the binder (whether lime, natural cement, hydraulic cement, or Portland cement). It is very difficult to distinguish between different pozzolans except by petrography, and even then, this is dependent upon the skill of the operator and the fineness of particles. The aggregate type and shape, the percentage of each component by point count, and the porosity can also be determined.

Scanning electron microscopy may be useful to establish the original finishes, the binder type and any alteration that has taken place in it.

A key consideration in commissioning testing is ensuring that the person or laboratory undertaking the work really has suitable experience, so that they can interpret the findings. A written report is rarely sufficient: discussions with the person doing the testing will often reveal far more information than a written test report.

## Chemical testing288

Elemental analysis can be done using atomic absorption spectroscopy, ICP spectrometry, or x-ray fluorescence. This provides data on the key elements, enabling the percentage of each component to be calculated. It reports CaO and/or LOI, thus enabling the calculation of carbonate content, but makes no differentiation between lime, cement, or aggregate, which contains carbonates. It may be useful to identify trace elements to indicate additives or minor components, or to compare variability between samples.

Organic extraction and analysis by Fourier Transform Infra-Red (FTIR) spectroscopy can be useful to identify any organic additives in the original mix, though they are not always found. It is necessary to be aware of significant alterations that take place over time. With a carefully selected sample, it may be possible to identify organics present on the surface of the stucco.

## Physico-chemical testing

Loss on ignition (differential thermal analysis or DTA) identifies calcium carbonate and magnesium carbonate not determinable through standard chemical analyses. It is important in determining the percentage of binder, but is not relevant if a carbonate aggregate such as limestone or marble has been used.

X-ray diffraction, for crystallographic phases and mineral identification is semi-quantitative, and is useful to identify binder and aggregate components, especially if carbonate aggregates have been used. It can also identify mineral phases of lesser components.

Soluble salts are identified for the analysis of salt attack. This is subject to the influence of original material, and may need to be correlated with other analyses.

Acid digestion and sieve analysis can be used to determine the size distribution of the aggregate, and may determine the percentage of non-carbonate minerals—the combination of aggregate and silica or impurities in cement and lime.

## Physical properties

Porosity and permeability are useful to give an indication of degree of weathering, and correlate with original composition, especially the binder type. This provides a baseline for comparison with patch and repair mixes.

Water vapour transmission testing using the ASTM E96 procedure289 is good as a comparative test, but not particularly useful for absolute measurement.

Strength testing (compressive, bending) is not particularly relevant in most situations.290

Thermal expansion can be important if there is extensive delamination, as there may be differential thermal expansion between stucco and substrate. This provides a baseline for comparison with patch and repair mixes.

## Samples

The number of samples taken is important. Historic batching techniques mean that some variability is to be expected. An absolute minimum of three directly comparable specimens is required, but five to seven is preferable. More should be taken if a comparison between sound and deteriorated fabric is desired.

The sample size and shape must be sufficient for relevant test methods. More, rather than less, is usually good for the testing laboratory, but that is a problem when dealing with a significant building. It can be physically difficult to procure suitable samples if the stucco is in good condition.

## Validating reproductions

Prototype materials for repair and restoration work should be tested for compatibility with the existing fabric.

Samples of the mix can be subjected to mortar analysis to confirm the composition and tested for cure, set, porosity and strength.291

Prototype samples should be applied to the wall to validate mixing, application, curing, and performance in situ. Pull-off tests can be used to verify adhesion, visual mapping for shrinkage cracking, and permeability testing to assess porosity.

Cleaning trials should also be carried out.

In all cases, comparative tests are by far the most useful. One-off tests of a single product or system tell us very little, because there are no absolute standards against which they can be measured. Instead, a test of the material prior to treatment compared with the treated material can provide some data for assessment of performance.

David West is a materials scientist with training in architecture, geology and materials testing. He has consulted on the conservation of historic building fabric throughout Australia, with a focus on stone, masonry and ceramics. He is the Executive Director of International Conservation Services, a multi-disciplinary conservation business based in Sydney.

The Analysis and Conservation 
of Stucco Surface Finishes

Jenny Dickens with a contribution by David Tilbrooke

introduction

materials

stucco materials

stucco colourants

stucco coatings

maintenance coatings

surface deposits

materials identification

methods of examination

documentary research

sampling

visual examination

visual microscopy

technical analysis (with contributions by David Tilbrooke)

semi-micro analysis in architectural conservation investigation

instrumental techniques for micro sample analysis

spectroscopy

chromatography

electron microscopy

X-ray Fluorescence (XRF) and Particle Induced X-ray Emission (PIXE)

X-ray Diffraction (XRD)

philosophy of analysis and intervention

determining the architect’s or builder’s intent

approach to intervention

applying the results

conclusion

case study: ‘Benvenuta’

background

project

results

summary

conclusions

## Introduction

Our understanding of the nature and true colour of Victorian stucco finishes has been challenged in recent research, which reveals a much greater degree of subtlety and sophistication than previously understood. This understanding can be extended with the aid of conservation science.

The colours and surface textures of buildings influence the way they are perceived by the general public. And perceptions can impact directly on conservation decision-making. For example, buildings with damaged or dirty surfaces can be perceived as structurally flawed leading to a lack of will to conserve them. Some will be demolished and replaced through a general lack of appreciation of their true significance. This applies equally to modest and grand buildings, including those with plaster or cement façade treatments, or stucco. The surfaces of stuccoed buildings are particularly important in understanding their significance, as they were generally intended to have the outward appearance of stone. It is therefore very important to have a good understanding of the precise nature, materials and appearance of stucco finishes and maintenance layers before any intervention.

Whichever technique is chosen to analyse a stuccoed building, it is critical to have a good understanding of the materials likely to be found on or in historic stuccoed surfaces. These layers can be thin and easily confused with each other. They are (from the interior outwards):

- rendered masonry

- stucco materials (including colourants) used to make and finish the stucco

- coatings (such as paint or limewash) applied to the stucco in the post-construction period

- maintenance coatings (such as paint or limewash) applied to the stucco as part of routine or occasional maintenance

- surface deposits—accretions and post-construction alterations which may be found between any of the above layers.

It is important that the person interpreting the results 
of technical analysis has sufficient understanding of the historical significance and the chemistry of materials, and of the history of building technology. A team of specialists, including at least an architectural historian and a conservator, is often better able to determine the significance or otherwise of a particular layer than a single individual, however expert.

Examination techniques commonly used to establish the original appearance of a stuccoed building are:

- documentary research

- visual examination and enhanced visual examination

- materials identification

- laboratory based identification techniques

- instrumental techniques.

Each technique focuses on a different aspect of the materials, and will have its own strengths and weaknesses. Usually a combination of one or more of these techniques would be the most successful. A clear understanding of scientific method is also essential for achieving accurate and meaningful analyses. This is to ensure that the evidence is collected accurately and evaluated carefully, that the research and testing is sound, and that there is no undue reliance on prior assumptions when developing the final conclusion.

The surfaces of buildings are constantly changing, whether intentionally, or due to ageing or damage—and it is erroneous to assume that the appearance of a building at a particular point early in its life is necessarily the original appearance. For example, it is not possible to apply resinous paints to a stuccoed building until after the stucco has completed carbonation, which may take up to three years.292 Ashurst reports that the use of oil paints on stucco became general in the United Kingdom in the 1840s. Research by the author has shown that ‘Benvenuta’ in Melbourne was white for much of its life due to applications of stucco, paint and whitewash. Should it be returned to its newly constructed grey appearance, or to the appearance it had for the majority of its life? Krotzer discusses an example where a building’s exterior woodwork was originally painted to match the colour of the building’s stone dressings.293 If the stone has developed a darker colour over time (and this type of darkening often can’t be removed), should the woodwork be painted the original colour (which would not match the stone any more) or painted to match the new colour of the stone? These types of issues need to be considered in conjunction with the results of documentary research and technical analysis.

## Materials

Stuccoes were applied to buildings as fine finishing layers over layers of coarse plaster, and were intentionally coloured using carefully selected materials. They were also coloured with various water-borne materials while they were still green (uncured) or very soon after. Conventional distempers and oil based house paints were applied, but a period of drying and carbonation of the stucco was required before application.

To start to identify the original appearance of a stucco surface it is necessary to attempt to identify the materials used to make the stucco and any coatings applied to it at the time of construction or soon after. Dirt and other additions must be identified and separated from the original and authentic surface finishes and any later maintenance coatings. Plasterers in the nineteenth century had access to a very wide variety of materials, and would have chosen them according to personal preference, price, availability and short- and long-term performance.

### Stucco materials

Ellsmore’s review of stucco materials and finishes, above, lists the main materials found in Victorian stucco. The chemical constituents of these materials are complex due to the chemical interactions between the components during manufacture, use and ageing. Ellis lists the constituents expected in Portland cement [hydraulic lime, pozzolanic lime, lime putty (non-hydraulic) and dry hydrated lime (non-hydraulic)].294 These, as well as Roman cement and gypsum plaster, have many chemical similarities but with subtle differences caused by differences in source materials and processing. As time passes, many of these materials continue to carbonate and identification using their current chemical state may be quite inaccurate.

Organic binders were sometimes mixed into the final layer or layers of stucco in order to give a finer and smoother surface. Many of the same organic materials as those used in limewash (see below) would have been used, but with the addition of fine sand to give the mixture a bit more body. For example, the stucco layer at ‘Benvenuta’ (see case study below) was found to be a mixture of hydrated lime (calcium hydroxide), chalk (calcium carbonate or whiting), binder (probably casein) and fine sand. This was grey white in colour and rested on the masonry render. No dirt or pollutants were found between it and the render, which indicates that this layer was applied during construction or very soon after (within the first few years).

### Stucco colourants

Again, Ellsmore lists the main colourants found in and on Victorian stucco. There is a very large variety of materials. The constituents of the most common are listed below.

- Limewash. The basic components of limewash are lime and water, usually with an organic binder. Herm lists a large range of materials used as limewash binders: ‘…1) oils, fats, soap, paraffin; 2) casein, milk, resin varnish; 3) salts; 4) cement, brick dust; 5) cellulose ether, glue, sugar, beer, glycerine; 6) polymer dispersions.’295 Polymer dispersions would normally be found in more modern coatings and may include synthetic resins such as polyvinyl acetate (PVA) or acrylic.

- Sealants. Organic materials such as those listed above, used alone form a clear coating. Transparent resinous coatings used on buildings would tend to be made from the cheaper resins such as rosin (pine resin). These would have been used to give a glossy coating; because these materials are visually saturated and thus temporarily disguise a dusty surface; or in the mistaken belief that a clear coating would stop or prevent flaking of underlying layers. 
A layer of rosin (pine resin) was found at ‘Benvenuta’ (see case study).

- Pigments mixed with the stucco. Pigments may have an organic or inorganic origin. Most pigments have a historic name (e.g. raw sienna) and a chemical identity (e.g. iron oxide), and many have more than one name. Research by Matero and Snodgrass296 on 20 nineteenth century buildings in New Orleans identified a very large palette of colours on the exteriors of the buildings. These included Paris green (copper arsenate), chrome green (copper chromate), iron oxides (used raw and ‘burnt’ e.g. raw sienna and umber, burnt sienna and umber), Venetian red, Chinese white (lead carbonate), and various carbon blacks. All these pigments are inorganic—that is, they are minerals. Most mineral pigments are light-stable.

- Organic pigments are generally made by precipitating a natural or synthetic dye (such as madder or indigo) onto a colourless powder (such as gypsum or alumina) thus forming a pigment known as a lake (madder lake being a popular example). It is likely that these materials have not often been used for colouring buildings given their greater propensity to fading. However, their presence cannot be completely discounted.

- Pigments may have very similar compositions to each other, or change to a new chemical compound over time or on exposure to the lime in stucco. Both these will complicate visual examination and technical analysis. For example, the red pigment cinnabar or vermillion (mercury II sulphide) was sometimes used to give a pink colour to stucco297. On exposure to light, the pigment can recrystallise to black metacinnabar, which still has the same chemical composition although a different crystalline structure298.

- Given the vast array of pigments and the chemical changes they may undergo over time, identifying pigments is a very complex process best done by a conservator or conservation chemist.

- Conversion coatings. In these coatings, the colour results from a chemical reaction between the colourant and the stucco. An example of this is copperas, which is a mixture of iron sulphate (known as iron vitriol or copperas) and lime water.299 The chemical reaction between these two materials and air forms ferric oxide, which is an orange/ochre colour. Analytically, it can be difficult to tell the difference between the ferric oxide from copperas and iron salts deposited from industrial pollution.

### Stucco coatings

There are two types of paints: those which harden by evaporation of a solvent, and those that harden by chemical change. However, when examining them it is more useful to consider whether they have formed a water resistant surface film or bonded with the stucco.

Paint which dries by evaporation of a solvent is defined as ‘any dispersion of a pigment in water, oil, or organic solvent.’300 The two main types of traditional paints found on buildings are known as distemper and oil paint. Traditionally, both these use natural materials as binders.

- Distemper is ‘an opaque, aqueous paint that dries to a matte finish [which] may have gum, glue, or casein binders.’301 The solvent for this type of paint is water and therefore it remains fully or somewhat water soluble.

- Some types of paint are made from a resin dissolved in a solvent such as copal resin dissolved in turpentine. These may have been mixed with a drying oil or used alone.

Modern paints tend to use synthetic materials, which dry by evaporation as binders. These include alkyd, acrylic, latex and epoxy. After 1940 many oil paints contained alkyd binders to decrease the drying time.

Coatings which harden by chemical change include the following.

- Limewash, coloured or left in its natural creamy white colour, hardens stucco302 and was very commonly used as a coating.

- Oil paint is a ‘paint made by grinding pigments with a drying oil such as linseed oil.’303 A drying oil ‘dries’ by cross-linking to form a hard film. In some cases, some solvent such as turpentine is also present in this type of film to aid in spreading.

- Epoxy, polyester, and other modern coatings harden by chemical reaction rather than by solvent or carrier evaporation.

Paint ageing behaviour will especially affect visual examination. Pigment changes have been discussed above. However, it is common for binders also to distort the appearance of painted surfaces over time, by yellowing or darkening. For example, when binders become yellow, a formerly white paint will appear cream and a formerly pink paint will appear orange. In particular, lead white paint is known to become yellow in the dark,304 such as under later layers of whitewash or paint.

### Maintenance coatings

The analysis of a stucco sample from ‘Benvenuta’ (see below) found evidence of limewash (whitewash) being used regularly as a maintenance coat on a painted stucco building. In this case, the whitewash was made from lime, chalk and a casein binder. A number of authors document the use of limewash as a maintenance coating on historic stucco buildings. Other studies in relation to cultural elements have found that the widespread belief that whitewash was used as a maintenance coat on outdoor stone sculpture is completely inaccurate305 and that these items were more commonly coated several times with oil based paints, waxes or varnishes in the ‘noble colour of stone’. So it is difficult to generalise about maintenance practices. Many authors also document the use of various oil and silicate based paints as maintenance coatings.

During the life of a building, various poisons may have been used to destroy biological growth such as lichen or moss. It is likely that traces of these materials could remain on stucco and confuse analysis. A patent from 1891306 lists the following:

‘… corrosive sublimate, metallic chlorides, mercury binoxide and salts, potassium cyanide, calcium sulphide, carbolic acid, paraffin oil, prussic acid, etc., iodine and iodides, mineral and organic acids, sulphur, sulphides, sodium bichromate, camphor, arsenic, verdigris, phosphorus, tannic acid, essential oils, strychnine, sumac, staphisagria, lead acetate, coal-tar derivatives, and carbonic-oxide gas. … the latter may be applied with a brush after admixture with paraffin scale dissolved in spirit. If to be applied to steeples, etc., a bag of soluble material may be suspended near the top so that the rain washes it down. In the case of the soluble materials the stone etc. after impregnation is coated with paraffin wax, etc.’

Thicker layers of modern cementitious materials are unfortunately very commonly found on the surfaces of historic stucco. These may be thin and flat or thicker if applied by spray (as shown in some of the images below). This work is usually done in an attempt to waterproof the building. Or it is done in the mistaken belief that it replicates an authentic finish. As well as disguising detail, the layers also create a waterproof barrier under which the stucco may continue to deteriorate. In addition these disfiguring layers can be difficult to remove without destroying the original stucco.

### Surface deposits

In conservation science it is accepted that dirt is ‘undesirable foreign matter’.307 Dirt, or surface deposits may be harmful (in which case they should be removed) or benign. However dirt and surface deposits may also contribute to the appearance of age and the dignity of a heritage place, sometimes referred to as ‘patina’. The grimy appearance may even be valued by the community and have significance in its own right.

The dirt layer on buildings is usually a complex mixture of materials. In polluted city environments in Australia, deposits on buildings consist of organic carbon compounds, elemental carbon or soot, salt, sulphates, nitrates and dust.308 Dust may be made up of sea salt, particles of earth, fibres, hairs and other natural materials. This type of dirt is black (grey in thin layers) and can be hard, or greasy in nature due to the presence of organic compounds such as uncombusted fuel or tyre particles.

Hard black crusts or thinner grey layers are found on buildings in urban environments. These can consist of a mixture of soot, gypsum and organic materials. Anecdotal evidence suggests that iron vaporises from tram and train tracks and deposits on nearby buildings—an ongoing issue in cities like Melbourne with an extensive tramway network. All these deposits can provide nutrients for microscopic bacterial or fungal communities. The by-products of these communities are compounds such as oxalates or acetates. Where the dirt layer is thin, the building can have a greyish cast and it will be black when the dirt is thicker. The streaky appearance of buildings in polluted environments is caused by rain washing this dirt off exposed areas, which allows thicker and blacker dirt layers to build up in sheltered areas.

Salts generated by damp problems in the base levels of load bearing masonry structures, or cementitious repairs in other parts, may be found also on the surface of stucco. These salts may consist of gypsum or other sulphates, carbonates or chlorides. When buildings are located near the sea or made from improperly washed beach sand, sodium chlorides can be present. Acid rain does not appear to be the major problem in Australia that it is in Europe.309

It is common for buildings to have layers of some or all of these types of surface deposits and for the deposits to be interspersed with coatings. It can be difficult sometimes to distinguish between applied coatings (intended) and surface deposits (unintended) in heavy accumulations on old masonry structures.

## Materials identification

Materials scientists routinely use a range of analyses to identify the organic and inorganic compounds found in building materials such as stuccoes and paints. They 
are summarised here to convey an understanding of 
their potential and their limitations in this area of research. There are a number of reasons why building materials such as stucco should be identified:

- documentation of the building

- dating/authentication

- evidence of use and users

- identification of deterioration

- identification of past conservation materials

- evidence of past environments

- designing interventions

- developing future preservation and maintenance activities.

Many analytical techniques are destructive—a sample must be removed from the building—so before starting any analysis project, the following should be considered carefully.

- What do you need to know and why?

- What information does the client, manager or owner need?

- Is the analysis necessary?

- What information is already available?

In order to get optimum results, it is critical to collate this data before approaching a scientist: most scientists are too busy to undertake basic documentary research. If they have to spend time doing this, they will either spend less time on the analysis or charge more for their services. For example, it is far more productive to give an analytical scientist a sample of stucco together with information on the materials it may be made from rather than just asking ‘What is this?’. Most scientists do not have training in historical materials technology, so you will save them time and yourself or your client money if you can provide this information.

Before starting any materials identification process:

- understand the characteristic appearance and composition of particular materials and manufacturing techniques

- understand the characteristic appearance and composition of deterioration specific to particular materials

- look for inconsistencies

- see if expected evidence of use is visible or identify its characteristics

- determine the physical and chemical characteristics of the previous use and environment or environments

- consider factors which may disguise any of the above

- develop assumptions and develop precise questions.

In the instrumental analysis:

- consider which analytical technique will be most suitable for the object and will best answer questions

- determine sampling opportunities and restrictions, and whether destructive testing is possible and if so to what extent

- identify an appropriate testing laboratory

- approach technical analysis experts with developed assumptions and clear questions and restrictions

- discuss the problem and questions with an expert to refine questions and determine if the proposed technique is suitable

- obtain costs and determine if these are fixed or will change, noting that any new questions or requests will incur additional costs.

During and after testing:

- document positive and negative test results

- do not hold fixed assumptions

- be prepared to change assumptions in the face 
of evidence from testing

- be prepared for results to disagree with the documentary evidence

- do not try to force or ignore facts that do not agree with prior assumptions

- discuss reasons for variations with analytical staff.

## Methods of examination

### Documentary research

Other authors in this publication have extensively covered the evidence from documentary research for stucco materials and methods, and this will not be repeated in detail here. It is important that all analytical techniques and their results are documented and included in any reports. Photographs of cross-sections should be made and copies of raw and manipulated test data should be included. Where possible, the samples should be retained as well.

### Sampling

For enhanced visual, laboratory and instrumental analyses it is usually necessary to remove a sample of the material. To ensure accurate results all the procedures below should be followed.310

- Ensure that you collect a representative sample—in most cases, this will mean that more than one sample must be collected. For publication in scientific journals, it will be necessary to design the sampling program to ensure that a statistically valid number of samples are collected.

- For examination of cross-sections, the sample should contain all the existing layers including the substrate, i.e. masonry, in the case of stucco. For other sorts of testing it may only be necessary to sample the layer or layers of interest.

- It is important to record which is the inner, and which is the outer surface of the sample.

- Do not allow the sample to become contaminated with surrounding materials.

- Ensure that collection of the sample does not damage the fabric of the building or stucco in any way. It is best to collect samples from the edges of pre-existing areas of damage. If this is not possible, it is essential that the samples are taken from inconspicuous areas; are as small as possible, while providing the required information; and that the sample areas are promptly and properly repaired with compatible material.

- For removing samples of stucco and render, usually a scalpel or sharp hobby knife is sufficient. If a chisel is used, this should be done with a great deal of care. It may be necessary to suspend a layer of plastic below vertical areas to catch samples. Use a new scalpel or knife blade for each building or area (if it differs considerably from the previous area).

- For most samples, a piece about 5 mm in diameter 
is sufficient.

- Use medical specimen jars or polyethylene zip-lock bags to hold the samples.

- Do not put more than one sample into each container.

- Label every container with the date, name of building, name of person collecting the sample, location of the sample, orientation of the sample, and sample number.

- Photograph the location of the sample close up, and indicate the sample collection position on a drawing 
of the building.

- Keep the samples in their containers for delivery to 
the laboratory.

- Ensure the samples are packed carefully for transport so that the container does not break.

### Visual examination

This is the simplest and safest technique, since it is not necessary to touch or sample the building, but it is surprisingly easy to get inaccurate results. It is important to have good illumination, and to be aware of the effects of different types of illumination on colour perception and sharpness, e.g. the fact that interior incandescent bulbs give a very yellow light. Wear prescription lenses 
if required, but don’t wear sunglasses.

When undertaking visual examination to determine the colour of a painted or stuccoed finish, a number of important points must be considered.

- Approximately 1 in 12 men and 1 in 200 women have some form of defective colour vision311 and it is important that this possibility is excluded for personnel undertaking colour matching projects.

- For close examination, anecdotal evidence from conservators says that small hand lenses, dental magnifiers or other forms of magnification should be used by all those over 40 years of age.

- Thin or incomplete layers can be easily missed.

- Ageing of paint and stucco materials (as discussed above) may cause considerable visual distortion of 
the visual appearance of colours, to the extent that 
it should not be the only technique relied upon.

### Visual microscopy

There are two types of microscopes that can be used for visual examination—stereo microscopes and compound microscopes.

Stereo microscopes:

- generally enable magnification from x10 to x60

- can be used to examine the thicker layers in samples

- have lower magnification, meaning it is often easy for thin layers to be missed—for example, the finish layers on ‘Benvenuta’ (see case study below) were only fractions of a millimetre thick.

Compound microscopes:

- generally enable magnifications from x20 to x400+

- can be used to view all the layers of a mounted 
cross section

- allow pigment particles to be seen at higher magnification

- can also have UV lighting options as well as polarising filters, which further aid identification.

Note that the light sources in many microscopes are quite different from daylight and may make colours look quite different, often bluer. Sometimes stereo microscopes are used only with room lights; however, these are also different from daylight. Even when daylight is the light source, the optics of microscopes means that colours will not be rendered accurately. Therefore, microscopes should not be used to identify colours visually but rather to identify layers (stereo microscopes) and materials (compound microscopes).

To examine samples under a compound microscope, it is usually necessary to embed the samples in resin, which is then polished to make all the layers of the sample accessible. This will change the colours but this is irrelevant as this technique is not designed for visual colour identification. However, it is easy for layers to be missed if they are present on one part of a building and not another, so it is important that several samples are examined.

It is possible to examine samples using light sources outside the visible range such as ultra-violet and infra-red. The most commonly used alternative light examination techniques are ultraviolet light (UV) and Infrared light (IR).

Ultraviolet light:

- is commonly used to identify resinous binders as resins which look similar under daylight, and to fluoresce different colours

- has to be used in the dark, and so is most useful 
for samples rather than in situ

- can be harmful to vision and should be used with appropriate protective eyewear.

Infrared light:

- could be useful as it can sometimes ‘see’ through the outermost layer of dirt to identify original patterns and some materials, but not colours

- can be used to examine a building in situ using an 
IR vidicon (analogue or digital), a digital IR camera or 
a film SLR camera loaded with IR film.

## Technical analysis (with contributions by David Tilbrooke312)

The main areas of chemical analysis, as defined by the requirement of sample size used, are: micro-, semi-micro- and macro-chemical analysis. Each area of analysis has its advantages and its drawbacks.

In micro-chemical analyses, the samples are usually in the range of 1 microgram [μg] to one milligram [mg] (a raisin or paperclip weighs about 1 gram [g]: 1 μg is 0.000001
of a gram [a millionth], while 1 mg is 000.1 of a gram [a thousandth]). Because the samples are so small and cross-contamination is easily possible, special precautions in terms of handling and quality of the laboratory environment must be observed. Such small samples often require using instrumental methods. A brief outline of these instrumental methods is given below.

Semi-micro chemical analyses usually work well with samples of about 10 mg upon which analyses for several elements or inorganic active groups (and some organic groups) may be undertaken. At this level of sample, estimates of the level of the elements and/or components present can be made. Semi-micro chemical analysis does not require special laboratory conditions, although some specialist equipment may be required. Such analysis can therefore be undertaken in any normal, analytical laboratory.

Macro-chemical analysis uses samples in the 10 mg to 
1 g (or more) range and is more often than not applied to samples of known composition and where the quantitative composition is the most important aspect of the analysis.

Semi-micro chemical analysis has advantages for the conservator as it allows analyses to be undertaken with mostly normal chemicals and equipment—the results of which can guide the conservator in his or her work, without demanding a large sample, taking an inordinate amount of time, or costing too much.

### Semi-micro analysis in architectural conservation investigation

In an architectural conservation investigation, the sample is often much larger than that taken from a work of art. However, it is also very common in this field to find that the material to be analysed is present only as a thin layer (paint, distemper or varnish finish—of which several may be present, each needing to be analysed) or only available from a small piece of residual paint or plaster (and very little is available to the analyst). In addition, when samples also have to be used for other studies, then only small pieces 
of the material of interest may be available to the analyst.

The application of the semi-micro chemical method may be appropriate for the analysis of such architectural samples. This is particularly so when a polished cross-section of the sample is prepared and examined under the high power of the optical microscope. This can aid in the identification of multi-layered structures.

In many cases of architectural sample analysis, a polished cross-section of the sample is prepared.313 This aids the identification of sample layers and, in many cases, allows them to be isolated, by slitting and scrapping from the main sample and analysed—again using semi-micro chemical techniques.

Examination of a cross section of a sample can also allow identification of organic layers such as paint and varnish, and inclusions such as iron dust and other detritus.

If paint is found, it is possible to extract it and analyse its pigment by semi-micro chemistry and its binder by Thin Layer Chromatography (TLC).314 The resin binder extracted can be saponified315 and the free fatty acids produced from this can be analysed also using TLC.

Many organic materials used in building construction, from ancient times into the early twentieth century, were derived from natural products and not highly refined. 
They are complex in nature and therefore require some pre-treatment before analysis can be undertaken.

There are a large number of chemical techniques used by chemists to undertake this type of analysis, and these will not be outlined here. It is important to note that many of these dissolve the sample in acids or solvents, or burn it (pyrolysis) thus destroying it. Once components of a sample have been extracted using chemical techniques, they can be subjected to the instrumental techniques outlined below to gain further information.316

### Instrumental techniques for micro sample analysis

There are many complex techniques for analysing the exact composition of materials. Before embarking on this sort of work, it is important to consider what information is needed and determine which sort of technique may be most useful. If a number of layers are to be identified, it will be necessary to separate each one, as they will have to be analysed individually due to the extreme sensitivity of the techniques. It should be noted that these techniques are generally expensive and, because of their precision, may produce results that are not relevant to the practitioner asking the question, or appropriate to the problem. For example, it can be quite common for a technique to identify every single element on a surface, and these results can disguise the elements of interest. They also require a well-informed client and an experienced operator to interpret the results. A number 
of the more common techniques are listed below; however, there are many more available.

### Spectroscopy

Spectroscopy detects the intensity of emission or absorption of electromagnetic radiation or particles as a function of frequency or energy. It is particularly useful for identifying organic binders in paints and stuccos, but some techniques will also identify pigments and other inorganic compounds. There are many types:

- Spectrophotometry (visible light)

- FTIR - Fourier Transform Infra-Red Spectroscopy (portable equipment is available)

- FT-PL Fourier Transform photoluminescence spectroscopy

- Ramen Spectroscopy

- MS - Mass Spectroscopy

- Mössbauer Spectroscopy

- Electrochemical impedance spectroscopy.

### Chromatography

Chromatography is a separation and identification technique that uses the different solubilities or sizes of materials in mobile and stationary phases (or solvents) to separate, and thus identify, components of a mixture. This is most useful for organic materials such as resins. There are many types, the most common being:

- Gas and Ion Chromatography

- GC-MS Gas Chromatography with Mass Spectroscopy.

### Electron microscopy

This is a very high magnification microscopic technique using a beam of electrons rather than light.

- It may have XRF included—this is often known as EDAX and is advantageous as it is possible to do an elemental analysis of a selected area being viewed under the beam.

- In Scanning Electron Microscopy (SEM) a solid sample can be used but it may need to be coated in gold or carbon.

- In Transmission Electron Microscopy (TEM) a thin section of the sample must be used.

### X-ray Fluorescence (XRF) and Particle Induced X-ray Emission (PIXE)

This technique identifies elements such as iron or calcium but not compounds such as iron oxide or calcium carbonate. This makes it less useful for many architectural analysis applications. Features include:

- surface sensitive technique.

- only tests top 1/10 of a mm

- difficult to measure below 0.1%

- portable equipment is available

- PIXE uses similar principles to XRF but is far more sensitive i.e. more trace elements can be identified.

- measurement can be done in air or in evacuated chamber allowing the use of a larger sample.

### X-ray Diffraction (XRD)

This technique identifies crystalline compounds (phases) such as pigments and minerals, this makes it more useful for architectural analysis than XRF or PIXE. It is also known as powder diffraction. Features include:

- solid or powdered samples can be analysed

- graphs produced are compared with large databases

- portable equipment is available.

## Philosophy of analysis and intervention

### Determining the architect’s or builder’s intent

When a building was designed, there was usually a clear intention on the part of the designer to achieve a particular finished appearance—although this often changed in minor or major ways according to circumstances, especially depending upon supplies of materials and labour. Therefore, the designer’s intent may have changed, even during the construction process. With the passage of time, it can be even more difficult to identify this original intent due to factors such as changes in the surface caused by alteration, degradation of materials in the outdoor environment, later additions, and the effects of maintenance, dirt and pollution. In some cases, contemporary documentation may provide some information, but the inevitable gap between documentation and practice means that this is not always reliable.

Stucco in Australia dates from a period when long-standing traditions in plastering were giving way to new manufactured materials and, most significantly, to manufactured cements. So the first step in identifying a finish on a stuccoed building is to consider the materials which were available at the time and may have been used in the construction. However, this is a complex issue because materials that were similar in type might have been different in their properties and appearance according to the brand (e.g. Portland cement). In addition, many builders, manufacturers and architects conducted experiments and developed their own formulations for cements, stuccos, paints and washes. In many cases, these were not published, so as not to advantage competitors.

### Approach to intervention

Analysis is one small part of the process of investigating authentic finishes. Then follows the important part—the interpretation and application of the results. This is just as critical. One area of ongoing discussion concerns the merits of cleaning. For example, in recent times there has been spirited debate about the cleaning and appearance of oil paintings.317 The materials conservation profession has resolved on the view presented by Sheldon Keck that the:

decision on how a painting is best presented as representative of the artist and period will always be a subjective act on the part of owners, public or private. As for us, the conservators, no matter how hard we try, it is impossible to eliminate the influence of our own time and taste upon our concept of the past. Although it is salutary to recognize historical patterns of thinking, which have accompanied altered appearances of paintings down through the ages, we should remain undistracted from our responsibility to prolong the life of each painting we treat with minimal alteration from its actual state.318

The approach seems less consistent in the field of conservation of the built environment. Some heritage professionals and property owners prefer to return historic buildings to their assumed ‘as new’ or original appearance. This might be defined as the appearance the building allegedly had when new, even though this can be impossible to identify accurately. Matero notes that Ruskin attributes ‘beauty to age, combining and promoting historical and aesthetic values over original appearance.’319 And other heritage professionals adopt this approach too, preferring an aged appearance where all or part of the age, use, damage and history of the building are retained as significant features. Some consider this aged appearance to be a legitimate aspect of a building’s aesthetic significance. Inevitably, even this approach is subjective, as only dirt and damage that correspond to the aesthetic of the audience are referred to as patina and are valued, while less visually pleasing evidence of age, such as accretions, is not.

The question of the acceptable degree of age or ‘patina’ is difficult to resolve. It is assumed that there is an overwhelming public preference for new looking buildings, and therefore it is not always easy to argue the merits of an aged appearance, especially when property values are at stake. But in fact researchers have found that a certain level of blackening of historic buildings is accepted and valued by the public as evidence of a building’s age and venerable status.320 Ellsmore has noted that ‘professional opinion favours the removal of harmful deposits whereas benign deposits are seen as dignified patina, to be retained.’321 However, it may be that visually attractive evidence of age such as fine cracking is harmful to the structure of the building; while less aesthetically pleasing materials such as modern acrylic paint may be harmless or even protective.

Layers of paints and limewashes interspersed with dirt and other deposits can be a valuable record of the maintenance of a building throughout its life and should not be removed without full consideration, especially if they are not contributing to a building’s deterioration or preventing interpretation. For example, long periods of neglect as evidenced by heavy dirt layers may correspond to periods of economic hardship for the owners. The abandonment of traditional maintenance practices in the 1960s illustrates the significant advances in materials technology and social change of the time, and the lack of value accorded to historic buildings. It should be noted that dirt layers contain a record of the pollutants to which the building, and therefore the city, have been exposed. They are accurate documents of the past. Aggressive washing and abrasive techniques used to ‘prepare’ building surfaces will remove most if not all historical layers, destroying the historical record and all chances of accurately identifying materials in the future. In many cases, a more careful treatment design can eliminate the need to do this.

### Applying the results

There has been little research done on the long-term effects of the application of restoration materials to historic stucco, whitewash and paint. Because of this, and because of the ethical issues outlined above, it is difficult to find a completely satisfactory solution to the problem of protecting, conserving, repairing or restoring historic stucco surfaces, especially where dirt or maintenance layers are present. Ideally, a system should be chosen which allows the preservation of all historic evidence while ensuring that the building is interpreted correctly. Possible choices are:

- limewash/whitewash

- stucco colourants

- replicated original stuccos

- mineral paints and washes

- thicker cementitious coatings

- paint—modern or historic paint formulations.

There are three further issues which must be considered—colour, thickness and texture.

The choice of colour is complicated by the ubiquitous use of titanium dioxide as the base colour or filler in the modern forms of most of the above materials. Because it has a high refractive index it reflects visible and UV light very effectively, giving it a bright, almost bluish white appearance under normal light. This gives very bright white colours, which would never have existed in the past. When a paint or wash containing titanium dioxide as a base colour or filler has coloured pigments mixed with it, the resulting paint will also appear brighter in colour. Titanium dioxide was first used as a pigment in 1921,322 but before this time white in limewash was achieved with lime and chalk (calcium carbonate); and in paint with lead white (lead carbonate) or zinc white (zinc oxide). None of these materials has the same brilliant white and filling properties as titanium white. As a result, many modern coatings, whether white or coloured, produce a far brighter and more opaque appearance than would ever have been possible in the past. While it is sometimes possible to produce small amounts of coatings that do not contain titanium dioxide, the cost can be prohibitive for many projects. As a result, it is often not possible to re-create the exact colours of the past.

It may seem obvious to state that all aspects of the appearance of restoration materials need to be compatible with the original fabric. In practice, it is unfortunately very common for new coatings to have thicknesses and textures very different from those of the original. Thick coatings may be very protective to a building but can completely distort or destroy the appearance of fine mouldings and stucco details. A change in texture can alter the way light reflects off a building and again considerably damage its appearance. This also means that new stucco (whether traditional or modern formulations) may be suitable for repair of stucco gaps and losses, but should not be applied over sound existing stucco. Original stucco in good condition is so rare that it is preferable to apply a thin limewash over it only if necessary to blend colours. In this way, a reversible strengthening layer can applied over the original layers without destroying them.

While limewash is a traditional maintenance material, it may not always be a practical solution when it cannot be re-applied regularly. Genuine limewash does not contain titanium dioxide though some modern limewashes or whitewashes may.323 It appears to be possible to re-create original colourants such as the ochre colour produced by copperas on new stucco, although further research is needed to quantify formulations.324

Oil or water-based traditional paints are most suitable for surfaces that have been previously painted. It is beyond the scope of this paper to discuss the details of the compatibility or otherwise of different paints, but there is considerable information on this topic in the literature. The major disadvantage of resinous paints, whether acrylic or oil based, is that they can constitute a moisture barrier, which can be a problem in a building suffering from damp.

Mineral paints based on sodium or potassium silicates have many characteristics that make them suitable for use in the repair of historic stucco. They are durable, compatible with many historic and modern stucco materials, and allow moisture to continue to move through the masonry. However, all appear to contain titanium dioxide,325 and some may also contain acrylic resin.326 
In addition, they are not reversible once applied, and often all other underlying paints must be completely removed before they can be applied, thus destroying the history of previous maintenance and the early coatings. Hughes et al note that while silicates can strengthen weak stucco, if used frequently they can also over-consolidate surfaces, which can eventually lead to delamination. To avoid this problem, they suggest applying the silicate paint over a layer of recently applied limewash, although they note that this technique requires further research.327

The Burra Charter, article 22.2, requires that new work should be identifiable. However, this can be difficult to achieve when conserving stucco and coatings. This approach is problematic for stucco and coatings for many reasons, some of which are provided below.

- It is not possible to mark a new coating the way, for example, a new wooden component can be labelled, so it can be impossible to identify visually. Paper- and computer-based documentation can assist, but are likely to be more difficult to access as time passes.

- To ensure that a new coating adheres to a substrate, it may be necessary to remove damaged or flaking layers of whitewash. This would destroy the history of maintenance of the building and may damage the original stucco.

- The use of materials that are chemically identical to the original materials might compromise future analysis because it will be impossible to tell if a coating is original or a later repair.

- Many modern coatings are far more durable than the underlying stucco and paint. As a result they are likely to damage original materials when they decay or are removed at a later date.

- Surfaces of buildings are particularly subject to changes over time. There is a case to be made for returning a building to the appearance it had for most of its life rather than a ‘new’ appearance that it would only have had for a short time.

## Conclusion

We cannot hope to exactly re-create the original appearance of a stuccoed building, although with careful testing and selection of materials it is possible to get very close. In some situations, it is not possible even to identify precisely what the original appearance was. Scientific analysis and documentary research are often seen as providing definitive answers, when in many cases they can only give indications. While the preservation of the building and its materials may be of most importance, the perception and use of the building altered over time, and the preservation of these aspects is also significant and must not be ignored. Matero quotes Brandi saying that ‘all restoration is a product of its time and as such is an act of critical interpretation.’328

The materials chosen for the restoration of surfaces can influence the long-term survival of the building, and will almost certainly alter its appearance either permanently or temporarily. These issues must be considered when selecting replacement materials. In many cases, it appears that the lack of traditional maintenance practices means that very interventional measures are preferred by the industry, because the building may not get any other attention for many years. In fact, the public may be happy with a less than spic and span appearance and the preservation of the thin and fragile historic surface layers should be a prime consideration in the selection of a treatment methodology for a stuccoed surface.

Jenny Dickens is the Senior Conservator at Heritage Victoria and has qualifications in Materials Conservation and Materials Engineering. She works in archaeological, collections and architectural materials conservation and teaches in the Conservation of Cultural Materials program at the University of Melbourne

Case study: ‘Benvenuta’

Background

‘Benvenuta’ (now Medley Hall) was 
built in 1893 for Mrs Leah Abrahams 
by the builder Richard Stockdale, 
to the design of the architect W S Law, designer of many elaborate houses and terraces during the boom period of the 1880s. The profusion of fine stucco 
work and mouldings, both internally 
and externally, is unsurpassed and epitomises the period.329

Project

Heritage Victoria staff wished to know what the original colour was, especially as evidence of a white under layer was visible. Image research showed that the building was white in the 1930s. Close examination also showed considerable traces of a white coating. Two cross section samples were removed and subjected to microscopic examination, and semi-micro chemical analysis by David Tilbrooke.

Results

Six distinct layers were found in the samples. All the layers were very thin, fractions of a millimetre per layer. The results of the examination and analysis of these are outlined below.

Layer 1:

- outermost, i.e. currently visible, 
grey layer

- distemper made of

- hydrated lime (calcium hydroxide)

- chalk (calcium carbonate or whiting)

- binder probably casein

- surface contamination

- high concentration of iron, probably from the nearby trams

- sulphate—industrial pollution

- silica dust—environmental.

Layer 2:

- off-white

- distemper made of

- hydrated lime (calcium hydroxide)

- chalk (calcium carbonate or whiting)

- binder possibly casein.

Layer 3:

- brown resinous layer

- rosin (or colophony or wood resin): the solid, resinous residue left after the distillation of turpentine from pine resin, often used as a ‘mortar improver’.

Layer 4:

- off-white colour

- this is a distemper made of

- hydrated lime (calcium hydroxide)

- chalk (calcium carbonate or whiting)

- binder probably casein.

Layer 5:

- visible white layer—slightly yellow in protected areas

- this is a paint made of

- lead white (lead carbonate)

- linseed oil (drying oil)

- no dirt, iron or sulphate contamination, indicating early date

- lead white in oil produced a very durable, hard and non-porous paint film that will yellow in the dark, over time.

Layer 6:

- grey in colour

- this is a thin stucco made of:

- hydrated lime (calcium hydroxide)

- chalk (calcium carbonate or whiting)

- binder, probably casein

- fine sand 15–20%

- low levels of iron commensurate with amounts found in sand

- no sulphate or dirt surface contamination, indicating no dirt build-up had occurred before it was applied.

Summary

- Layer 1—whitewash with a layer of dirt—outermost layer

- Layer 2—whitewash

- Layer 3—varnish

- Layer 4—whitewash

- Layer 5—lead white paint

- Layer 6—whitewash and sand mix, i.e. a pale grey coloured stucco layer.

Conclusions

- The dark colour of the outer visible layer (layer 1) is caused by exposure of the outermost layer of whitewash to industrial pollution for many decades.

- The stucco layer (layer 6) is made from lime, sand, chalk and a casein binder.

- A white lead oil paint was used over 
the stucco.

- No contamination from pollution is evident on the stucco and oil paint layers, indicating an early date of application of the stucco and white lead oil paint.

- It appears that the building was given a fine white painted finish early in its life—further testing should be done to confirm this hypothesis.

- The white colour was maintained over time using whitewash

- A layer of varnish was applied, probably in an attempt to consolidate peeling whitewash or to improve the appearance.

- The layers of dirty grey coloured whitewash are peeling off the lead white paint, giving the building a disfiguring patchy appearance.

Cleaning and Re-coating Victorian Stucco

Donald Ellsmore

abstract

introduction

the natural appearance of stucco

paints and applied finishes

colour variations

problems with heavy paint layering

benefits and risks of cleaning and paint removal

cleaning

dealing with clear coatings

paint removal

today’s options for finishing stucco

clear finishes

limewashes

distempers

cement paints

oil paints

mineral silicate paints

acrylic resin paints

other paint types

conclusion

## Abstract

Victorian stucco is commonly found today in three conditions—unpainted, fully painted, or skimmed over with Portland cement. These conditions are not characteristic of the authentic finishes as originally intended. Usually, the unpainted examples are degraded by weathering, soiled by airborne deposits, and have lost much of their original surface colouring. Painted or cemented examples may have their original characteristics hidden beneath the coating. There is now a common trend to clean (at a minimum) and re-finish stucco and change its appearance—often involving the application modern paint finishes which are assumed to be the same or similar to the original finishes. However, the cleaning and painting of stucco carries a high risk of distorting its correct intended appearance and cultural values. Therefore, cleaning, painting and re-finishing stucco surfaces should not proceed without due consideration of the short- and long-term effects of such interventions. This paper discusses the merits and risks of cleaning and re-coating external stucco finishes, assisting readers to assess the likely impacts and make informed decisions about the most suitable ways of meeting the legitimate needs of property owners without further adverse impacts to heritage values.

## Introduction

The nature of Victorian stucco finishes is poorly understood today. Until recently, it was believed that the unpainted appearance of cement stuccoed building façades was false and inaccurate—an aberration, perhaps due to pecuniary constraints at the time of construction. What was not understood (or possibly overlooked) was that the apparently uniform grey finish of unpainted stucco is a product of years of weathering and urban soiling, and that beneath the layers of dirt—in places protected from wind, rain and sun—evidence of the authentic colouring of the stucco can be found. These authentic finishes were obtained at the time of construction by careful selection of the materials (sand and cement) or by the application of colouring agents in the finishing of the stucco, or were applied to it soon after. The aim was always to replicate the appearance of natural stone.

The application of paint to stucco was not common, but some stuccoed buildings were painted from the outset, presumably after using the trowelling method to finish the stucco and make it suitable for painting soon after curing. This process was explained by Millar and confirmed in Victorian works schedules.330 Other types of stucco, according to Millar and others, were finished by other methods to expose the coarse grain of the plaster and create a more convincing stone-like finish.331

Many stuccoed buildings now carry a heavy build-up of paint finishes after successive applications of paint over many years. This accumulation of paint can inhibit moisture movement in the stucco and cause concentrations of salts—leading to localised salt decay and damage to the stucco and to the underlying plaster and masonry. Multiple layers of paint can obscure the fine detailing of decorative elements. Yet the removal of paint can be problematic too. It can damage the stucco and contribute to further problems with soluble salts by introducing harmful chemicals. The cleaning, painting, re-coating or removal of paint layers from stucco is therefore a complex issue, which requires careful consideration to avoid further damage or new problems that could adversely affect the conservation of the material.

## The natural appearance of stucco

The aim in most stucco work was to achieve the appearance of dressed stone. This did not mean that the stucco should deceive the casual observer, but rather that the finish should have the aesthetic characteristics of stone. For this reason, various recommendations were made about the best methods for achieving a finish as near as possible to the texture and colour of stone.332 Stucco established itself as the fashionable material of the day at a time when brick was conveniently out of favour among Regency architects for its alleged poverty of appearance. With a stucco coating in imitation of stone, brick easily acquired some measure of respectability.333 This meant that any applied finish that did not provide the same aesthetic characteristics as dressed stone would be contrary to the designers’ intentions.

The natural colour of stucco was achieved by careful selection and fine adjustment of the materials in the mix or by the application of a compatible colouring agent at the time of application, or both. The most common colouring agents were mineral pigments which were added to enhance the natural colour of the stucco mix, or carried in a lime or cement wash applied to the fresh stucco while it was still green. These were not coatings as such, because they did not form a surface film on the stucco. Rather, they bonded and integrated to some extent with the stucco. However, these finishes were soluble in rainwater and easily abraded by wind-borne particles, and therefore not durable over the longer term. This is why many aged stucco façades appear to have never been painted—there is no clear evidence of colouring on the surfaces of the stucco. However, upon close examination, the original colouring can usually be detected in sheltered areas.

The look of stone could readily be achieved with non-hydraulic lime-based stucco mixes because the lime binder in the stucco mix was not very opaque—it did not completely obscure the natural colour of sand grains in the mix. Rather, it allowed the colour of the sand grains to appear on the surface, especially after a short period of exposure to wind and rain. However, some hydraulic limes and cements, including Roman cement and Portland cement were more opaque and quite unlike the colour 
of most Australian building stones. The inherent darkness of Roman cement and the unattractive greyness of ordinary Portland cement could be overcome only to 
a limited extent by adding pigments and sands of various tints, including aggregates made from crushed stone. At least one supplier of Portland cement products therefore sold a stucco mix that was pre-coloured for use as a finishing coat of stucco in Portland cement-based plaster systems.334

The accumulation of layers of house paint on stucco is another matter altogether. The leading architectural finishes historian, Ian Bristow, has noted that in England ‘the unattractive appearance of Portland cement together with the soiling that inevitably takes place with the passage of years’, leads to a situation in which the painting of stucco goes largely unquestioned.335 It is clear that the accumulation of many layers of paint on the surface of the stucco—a condition encountered commonly today in urban areas—is contrary to the original aesthetic objective. Most of these paints would have been conventional house paints, and they might or might not have been applied in accordance with the original designer’s directions. The majority would have been applied after a period of exposure of the unpainted stucco, possibly many years later. Some of these applications of paint were probably intended to restore the properties of the stucco and its imagined original appearance.

Justifications for the application of paint to stucco include protection of the stucco finish, improved weatherproofing, stabilisation of the plaster, and the achievement of a different character or more fashionable appearance. Regrettably, careful examination of many examples leads to the conclusion that in the majority of cases the application of paint did not strive for any functional ideal beyond a fresh appearance. The wide variety of paint colours used on stucco indicates that paint was applied in accordance with individual owner’s whims and preferences and not to enhance the architectural aesthetic—at least not the stone look. House paints were applied to a high proportion of stuccoed surfaces, and they continue to be applied to previously unpainted and painted stucco surfaces today. Each additional layer of paint further diminishes the resemblance of the stucco to its original intended appearance.

## Paints and applied finishes

In the early nineteenth century, there were relatively few options for colouring stucco. The choices were to colour the material through the careful selection of natural ingredients; to colour it with a compatible water-based application of colour wash; or to paint it with oil paint when it was completely cured and dry. Examples of these three methods have been studied in the research for this paper. Tinted lime-based colour washes appear to have been the most common of the methods—possibly following J C Loudon’s advice that where the cement used was only lime and sand, it would resemble stone with little or no colouring matter added, while Roman cement might be brought to a stone colour with washes to produce the colour required. ‘Oil colours’, he said, ‘should not be used on cement laid on walls in the open air for a year or more’.336

In Loudon’s time, it was the plasterer’s job to apply colouring systems on a base of lime or chalk. Therefore, the 1836 Schedule of Contract for Plasterer’s work for the service of the Honourable Board of Ordnance in Sydney included materials and plasterer’s labour under the heading ‘Lime White, Whitewashing, and Colouring Including Size’. Within these categories, there were specific items of interior and exterior work, and specific references to the stone-like colours ‘stone, buff and salmon’.337

The introduction of common Portland cement-based stucco, and its incremental increase in use in the second half of the nineteenth century, was associated with the appearance of a wider range of finishes. By the time Portland cement was produced in Australia, there was an even wider range of coloured washes and paints available, including casein-bound washes and distempers, cement washes, washable distempers, silicate paints, and zinc oxide-based oil paints—in addition to the traditional white lead-based oil paints. All of these were seen as having some advantages over traditional limewashes and distempers, such as greater permanency and better covering power to overcome the inherent greyness of common Portland cement.

Limewashes were suitable for colouring lime stuccoed surfaces, with which they had an obvious affinity, forming an integral bond with the uncured or cured stucco. Lime was readily available from the early times, and limewashes were prevalent.338 Distempers were normally reserved for indoor use, being water soluble and impermanent,339 but they could be made more suitable for outdoor use by adding oily or greasy matter.340 The addition of oils, fats, proteins and mordants (such as alum or copperas) to the colour washes made them less pervious and more durable. Colour washes based on lime or chalk and tinted with mineral pigments were applied to fresh stucco in various weather conditions to achieve a convincing stone look.341

Oil paint was used extensively, but not immediately, on lime and cement-based forms of stucco. It was not normally the first application of surface colouring—but as Bristow lamented, ‘paint inexorably triumphs over original design intentions’.342 Oil paints based on white lead and linseed oil were a poor choice in many situations—they did not have a convincing stone look and could not be successfully applied to damp and alkaline surfaces. Furthermore, their application to the rough and porous stucco surfaces was an arduous and therefore costly undertaking. Even so, oil paints were commonly applied, and it must be assumed that the aim was to improve the appearance, durability and water resistance of the stucco. There is no evidence of a more general use of oil paints as original finishes, at or near the time that the stucco was applied: it appears that in most cases the oil paints came later. Field research commonly reveals the presence of chalky, loose-bound colour finishes below the oil paints.343

Mineral colours in solution, also called colour washes (but distinct from limewashes and distempers, which obtain their opacity and covering power from their lime and chalk bases) have a long history of use as colouring agents on brickwork, and to a limited extent also on stucco. When applied to brickwork the term ‘raddling’ was used to describe this type of unbound, water-based colouring.344 It appears that colour washes were applied to stucco to enhance the appearance and to produce dark colours such as Venetian red, when transparency or deep toned colours were sought. It is not surprising that the methods used to colour brickwork before the nineteenth century use of stucco were transferred to the colouring of stucco. Although there is not a reliable or substantial body of knowledge regarding the extent of the use of colour washes on stucco, there were three common situations that called for coloured finishes that could be obtained with colour washing and pencilling techniques. These were the brick red colours, used to achieve polychrome effects with cream brickwork; the golden hues, used to achieve polychrome effects with red brickwork; and black, used to define the incised lines of imitation ashlar. These colours were applied using techniques more often used in colour washing and pencilling of brickwork.345

Various techniques were used to improve the life of the somewhat transparent colour washes on masonry—such as the inclusion of binders and mordants to fix the mineral pigments. Some of these colour wash components imparted colour directly to stucco by reacting with the lime. The most commonly recommended component, which served as both a colouring agent and a mordant, was copperas, or sulphate of iron. Traditionally copperas was used to fix the colours of washes, including limewashes, and it reacted with lime and cement to create a deep golden or reddish yellow colour. The benefits of copperas were well known, judging by the many references to it. Loudon recommended the inclusion of ‘five ounces of copperas to every gallon of water’ in washes. He noted that ‘the copperas, or sulphate of iron, oxidises with the atmosphere, and produces a reddish tinge’.346 Another reference claimed that copperas could be used to tint limewash to ‘a strong buff colour’.347 Some prominent buildings in Victoria reveal evidence of a reddish yellow or buff colouring on their stuccoed surfaces, which fits the description of the finish achieved by an application of colour wash containing copperas.348

Copperas was an item of surplus stores offered for sale in Sydney by the Commissariat Office in 1833.349

The new products of the late nineteenth century included mineral silicate paints, sanitary washable water paints and cement washes.350 Mineral silicate paints were well suited to stucco and cement plasters because they had the ability to bond with the surface in the same way that fresco colours integrate with plaster. These paints, made with a base of potassium or sodium silicate, had a history of use on the façades of buildings in Eastern Europe. A patent for liquid silicate paint was granted to Keim Mineral Paints in Bavaria in 1878351 and, although it is not known whether Keim’s paint was marketed in Australia at that time as it is today, the term silicate paint did appear in specifications for colouring stucco.352 Perhaps it was the new form of paint called ‘Duresco’—a so-called washable distemper marketed in Australia by the Silicate Paint Co. That product was claimed to be the ‘first in the field and foremost ever since’.353 It was made with a new pigment called Charlton white, developed in the 1870s,354 and was sold in powdered form, to be mixed with hot water and petrifying liquid, ready for application to interior or exterior plasterwork.355

Another class of water paints readily adapted to stucco were the cement washes, which contained cement powder but were otherwise similar to distempers—being mixed with powdered pigment and glue size.356 To these base constituents were added small quantities of plaster of Paris, lime and alum. It was claimed that, unlike distempers and lime washes, cement washes would resist damp and would not crack or chip off.357 They were designed for use on unpainted cement, stucco and concrete, and were sold in powder form ready to be mixed with water on site, and applied by brush. Upon drying, these washes bonded with the surfaces of the like material to form a moderately porous finish with no gloss. In Australia, they went by trade names such as Wesco and Boncote.358 They are sometimes referred to as ‘cement paints’, but that term is better reserved for those paints which are designed for application to cement surfaces, but do not themselves contain cement.

The Australian paint manufacturing industry expanded greatly in the early years of the twentieth century, and the advertising in journals and trade publications shows that there was fierce competition between manufacturers. Dozens of manufacturers produced hundreds of types of paint for general and specific uses. Several of the paints were claimed to be alkali-resistant and therefore suitable for use on stucco and other cement-based surfaces. They went by names such as anti-cement oil paint and cement-proof paint.359 They were intended mainly for the concrete and cement surfaces which were becoming more common and, as the paint manufacturers stated, these materials released free lime which destroyed ordinary linseed oil paints. The manufacturers of these new paints incorporated new technologies to meet the specific requirements of different surfaces in a process of improvement that continues to this day.

## Colour variations

While stucco colouring was aimed at replicating the appearance of stone, the natural colours of building stones vary from place to place, and so too did the stucco colours. The tradition in Britain was to emulate the colour of the local or preferred building stones. Bath, Caen and Portland stone colours were favoured. Portland cement was so named because of its similarity in appearance to the colour of Portland stone. It was a suitable colour for London terraces but it was not so well suited to Melbourne or the other major growth centres in Australia, where the preferred colours were the warmer earth tones of local stones. These were imitated with colours ranging from straw, biscuit, buff and Sienna to the yellow browns referred to by house painters and paint manufacturers as light stone, stone, mid stone and dark stone—generic descriptors for colours that could be produced with earth pigments.

Colour variations have not been exhaustively investigated for this paper, but there are some indications that the interpretation of stone colours varied with time and place. For example, the salmon and terra cotta hues of weathered Sydney sandstone are commonly found in paint colours on stucco in the Sydney region, but rarely observed in Victoria. Mid-brown hues for colouring stucco were common in the Victorian goldfields towns, but not in Melbourne. Cream to light stone hues are found consistently everywhere on stucco when used for the dressings of brick masonry buildings in the Queen Anne and Federation styles. However, there may also have been regional variations due to the availability and prevalence of use of different types of cements.

A large proportion of stuccoed buildings outside Victoria are painted with impervious paint coatings, whereas in Victoria, a substantial number survive unpainted or with only modern grey Portland cement washes, which are rarely seen in the other states.

## Problems with heavy paint layering

It is clear that modern impervious paint finishes and Portland cement washes can have an adverse impact on aesthetic values of stucco, and on the fabric. The build up of paint layers can cause a concentration of salts in vulnerable parts of a composite stucco façade, and applications of Portland cement can promote the development of harmful salts. In situations where there is a heavy build up of paints and cement washes, it may be necessary to remove the entire build up of coatings in order to conserve the stucco. The benefits and risks associated with cleaning, including the complete removal of accumulated layers of paint and other coatings are discussed below to assist in determining when and how stucco façades should be cleaned.

Very profound changes occurred in the manufacturing and marketing of paint because of wartime developments in polymer technology. Two modern paint types have been widely used on stucco with some damaging results—one is polyurethane resin, which is now the base of many clear coatings, and the other is acrylic resin emulsion, which is now the industry standard for opaque house paints.

In the 1950s, the first 100% acrylic emulsion paint was marketed as a latex paint suitable for indoor use. By the 1970s, a range of semi-gloss emulsions was developed, followed in the 1980s by full gloss emulsions. Today, according to the paint manufacturing industry, 100% acrylic paints have conquered every house-painting frontier, and they are moving rapidly towards the displacement of all other types of paint, including some that would be more suitable for painting aged stucco.

This evolution of easy to manage painting materials, together with the post-war rise of the ‘home handyman’, resulted in a liberal use of paint on stucco. Modern house paints are sold predominantly as application-ready and water-compatible, making them suitable for easy application to any surface, irrespective of their suitability for the application, or the potential problems that will arise with multiple applications. They require no special expertise, enabling almost anybody to apply a decent paint coating to any surface with relative ease. This gives rise to the excessive layering of paint coatings routinely found on heritage places and their stucco façades today. In situations where there is a substantial accumulation of paint, the paint may need to be removed to liberate moisture and remove harmful salts; to provide a suitable foundation for future painting; or to reveal the authentic appearance of the stucco substrate.

Examples of Victorian stucco which remain unpainted and which retain their original characteristics, including evidence of their original surface colouring, are becoming rare under the onslaught of enthusiastic property owners. These unpainted examples may require no treatment, or nothing more than gentle cleaning with water to dissolve and remove harmful surface deposits, leaving them sound and natural looking.

## Benefits and risks of cleaning 
and paint removal

### Cleaning

It is the nature of Victorian stucco façades, with their usual composition of classical decorative elements, that exposed flat surfaces become weathered over time and remain relatively clean and free of harmful surface deposits; whereas protected surfaces retain their original finishes, as well as accumulated deposits of dirt and by-products from surrounding and adjoining materials. The implication of this normal pattern of weathering is that some parts should be cleaned to remove the dirt, and other parts may need to have their protective and decorative finishes reinstated. However, the most common response to this situation—and the most potentially damaging over the long term—is to paint the whole façade.

It is time to review common painting practices, and to consider other and possibly more appropriate options, including partial cleaning and partial reinstatement. It is not rational to continue with practices which imperil heritage values and create the ongoing burden of a continuing cycle of painting, which would otherwise be totally unwarranted.

The cultural heritage values of Victorian stucco demand a cautious approach in cleaning and refinishing. There are no simple or universal remedies for a soiled building façade—every case must be considered on its merits. It is important that no change to a stucco surface be made without first considering the long-term results. For example, inappropriate cleaning methods could damage the surface characteristics of the stucco and make it unstable; or the application of new impervious paint finishes could cause dampness to appear on interior surfaces, or harmful salts to accumulate in other areas with very damaging consequences for the building fabric. Therefore, careful assessment and a staged approach to reasonable change are needed.

An assessment of the stucco should be undertaken prior to any cleaning or repairs, to gain a full understanding of the nature of the material, its application, original appearance and current condition before any works are undertaken. Each of these factors could influence the final choice of cleaning method. A clear understanding of the original surface finishes and the intended appearance of the building is an important prerequisite to deciding on the need for cleaning, and the appropriateness of any possible new finishes as well.

Sometimes, colouring of the finished surface of fresh stucco was performed within a few hours of application, to obtain optimum colour retention—this type of finish is integral to the stucco finish and therefore may be resilient to mild cleaning. However, other finishing methods may not be robust enough to withstand even mild cleaning methods. For example, the application of lime and cement-based washes was common, but surviving examples of those finishes are not likely to be resilient 
to some cleaning methods.360

Consideration of cleaning methods must be based on a detailed analysis of the nature of the dirt and the most effective means of dissolving and removing it. The most benign methods, such as clean water washing at low pressure, should be tried before more aggressive methods are considered. Rarely—if ever—should grit abrasive methods be contemplated because these are highly likely to damage the surface of the stucco. Cleaning should be directed at removing the harmful deposits without affecting the stucco or the residual evidence of its colouring. Chemical solvents and detergents, if used, should be completely removed by flushing with clean water—lest they remain in the porous substrate in sufficient concentrations to initiate a new cycle of deterioration.

### Dealing with clear coatings

When clear polyurethane coatings were developed, they soon found many new applications in which traditional varnishes—because of their inherent colour and high gloss levels—could not be used. The polyurethanes could be made water-clear and non-glossy—very desirable characteristics for so-called invisible coatings. However, polyurethane coatings change over time under the effects of ultra violet light—commonly turning yellow and becoming opaque and brittle. The application of clear coatings to finishes such as weathered stucco has been calamitous in the past—with unanticipated results including unsightly milkiness across a façade, uneven weathering, darkening and yellowing, and a bleak prognosis.

The types of clear coatings which were marketed in the past for outdoor use, are not readily soluble in conventional solvents, and therefore cannot be removed economically. Neither can they be re-coated with another clear coating. The only way to deal with them is to remove them entirely and face the high probability of damaging the substrate in the process; or paint over them with an opaque finish which will very likely obliterate the natural characteristics of the stucco substrate.

### Paint removal

The removal of paint can be problematic. Therefore, the first decision must be about the need to do so at all. If paint layers are present in sound condition and with reasonable vapour permeability, they are unlikely to affect the condition of the stucco adversely, and it may be appropriate to clean them but not to remove them. Any decision to remove such paintwork would be based purely on aesthetic considerations.

In some situations, the removal of accumulated layers of relatively modern, moisture entrapping alkyd and acrylic-bound paints would be desirable for other reasons, such as the need to reduce an already unstable accumulation of paint. It would be best achieved by using chemical solvents and super-heated water at low pressure, although some recent developments in cleaning technology have produced promising results with less environmentally damaging materials. Abrasive and high-pressure methods are, as noted above, very damaging to stucco and should be avoided. However, no matter what method is considered, it should not proceed without first testing the proposed method fully to determine its effectiveness and the likely impacts on the underlying stucco substrate.

When considering cleaning and paint removal techniques, a number of key questions need to be answered. Some of them have been raised already but they are repeated here again in their logical sequence as a checklist.

1	Is cleaning necessary for the conservation of the stucco?

2	Has the nature and extent of the original surface appearance been established?

3	How would the original finish withstand cleaning (based on field trials)?

4	How would the original finish appear or be reinstated following cleaning?

5	If water is to be used in the cleaning process, would structural cracks or hairline cracking admit water and cause the internal fabric to become damp or damaged?

6	If structural cracks or hairline cracking are present, what is the best way to deal with these and what is the most suitable finish treatment to apply after cleaning?

7 	If paint removal is considered, what is the least damaging method of removal?

8	How would the paint residue be effectively and safely collected and disposed?

9	How would chemical solvents be removed entirely from the fabric following the paint removal?

10	What, if any, would be an appropriate new finish 
to apply?

In the discussion below, a small range of commonly used finishes is considered for use on stucco today. And, as with the paint removal methods, it is wise to consider the most benign coatings, like water soluble washes before resorting to impervious coatings that would not only impact on the aesthetic values of the stucco, but also be costly to remove in the future should the need arise.

## Today’s options for finishing stucco

When it is determined after careful analysis that a new finish should be applied, the correct choice will be a finish which will replicate the aesthetic and functional characteristics of the original finnish. In addition, although the history of weathering and repair of the structure may militate against the success of a finish that matches the original finish, it should be always considered first: the original finish should be the starting point for selection 
of an appropriate new finish.

### Clear finishes

The coatings industry has conducted a sufficiently exhaustive investigation of clear or invisible finishes (including anti-graffiti coatings) to conclude that there is no product or treatment on the market today that would satisfy the standards of sound conservation practice and reasonable durability for a clear coating on unpainted stucco. All the ‘invisible’ coatings have one or more unwanted features—imparting an unnatural milky or wet look; changing the appearance in some other way; or blocking pores, inhibiting moisture transfer (preventing breathability) and disrupting normal weathering. Accordingly, the application of clear coatings should be avoided: they are not suitable.

### Limewashes

Limewash is a traditional finish that has been in continuous use for many years, although its use in recent times has been limited. It is now enjoying a revival in conservation work, and to some extent in commercial work, because of its inherent benefits and compatibility with porous materials. It is an excellent option for painting or re-painting stucco.361

There are many recipes for traditional limewashes (usually containing animal fats, oils and other additives) and there are now several paint manufacturers who are producing limewash for new work and for conservation—sometimes with fail-safe additives to make it suitable for the home handyman. Some of these new limewashes are modified by adding acrylic emulsions to give them paint-like qualities. This improves their workability and durability but can also interfere with the natural behaviour of porous materials, especially when moisture and salts are present. The acrylic can block pores and reduce vapour permeability in a way that could be detrimental.

Limewash is not paint in the normal sense of the word. Limewash does not harden by the drying of the surface film. Rather, the slaked lime particles of calcium oxide combine with airborne carbon dioxide to form calcite crystals of calcium carbonate. This process requires suitable attendance to ensure that the surfaces remain damp long enough for the reaction to run its course. Some recipes for exterior limewashes indicated that the lime should be slaked and applied hot, which is all that is needed for it to perform satisfactorily—however, recent research indicates that it can perform satisfactorily in its natural form without heat.362 Some recipes call for the addition of various functional additives, with some regional peculiarities and more than a few ‘secret’ ingredients. The additives include salt and alum (to slow down drying and to fix pigments); linseed oil, tallow or milk (to reduce permeability); starch, glue or size (to improve workability and adhesion); and coloured mineral pigments (to improve opacity and colour).

Limewash can be mixed to a traditional recipe for local or site-specific conditions, or it can be obtained in a ready-mixed form with or without acrylic binders. One leading manufacturer has taken the decision to remove the acrylic resin from its product and replace it with a casein binder due to concerns about the pore-blocking effects of acrylic, and to address growing concerns about volatile organic compounds (VOCs) in all forms of paint. 363

### Distempers

The basic ingredients of the class of paints called distempers are powdered chalk or whiting (plaster of Paris) and glue size (cellulose or starch). The calcium carbonate in distempers exists as a powder, (and therefore differs from the calcium carbonate in limewashes, which forms in a reaction with air). As simple water-based finishes, distempers were inexpensive and easy to apply, but their durability was dependent upon the glue binders, and usually limited. Being water soluble they would not survive very long on exposed weather faces. The addition of stabilising substances, such as salicylic acid and cresylic acid (a coal tar by-product), was recommended to improve adhesion and retard decomposition.364 Distempers of greater or lesser durability were used on stucco façades, although it is unlikely that they would have been preferred to the more durable finishes used in the better classes of work. Modern ready-mixed distempers for interior use include small amounts of acrylic and PVA resins, which impart reasonable properties for interior use, but are not recommended for exterior use for the reasons mentioned above. Distempers for external use could be made with a casein binder, which would provide an improved but still modest performance. Their greatest advantage would be their suitability for use on the most significant stucco surfaces where compatibility is a more important consideration than durability.

### Cement paints

Portland cement washes were commonly specified and used on Portland cement stucco surfaces. Early cement washes were based on the same basic constituents as distempers (plaster of Paris and glue size) with the addition of alum and hydrated lime. Better quality cement washes were based on Portland cement, which had the advantage of forming a durable surface by the chemical setting of the cement. Boncote cement paint is a Portland cement-based coating, which has been in use more or less continuously since 1920.365 It was designed for use on unpainted cement, stucco, brick and concrete surfaces. It provided a convenient finish for asbestos cement sheeting when that material was introduced to domestic building, initially in 1915. Boncote is not suitable for use over existing impervious paint coatings, although manufacturer supports its use on previously painted surfaces with appropriate preparation and primers. It is supplied in powder form and once mixed with water366 can be applied to prepared absorbent concrete masonry and stucco surfaces to form a hard, durable, matt, coloured coating.367

### Oil paints

Modern oil paints are based on the principal ingredients of alkyd resins and titanium dioxide base pigments in all the light tints. They do not possess anything like the hardness and durability of traditional white lead and linseed oil paints in the external environment. Alkyd enamels (as they are now called) are considered a good choice for use on sound timber, but not for all porous masonry surfaces. They form a surface film which degrades by chalking when the resins break down under the effect of ultra violet light. They are also susceptible to moisture when it is present in the stucco, and may blister and crack due to inadequate moisture permeability. Nevertheless, they provide a relatively compatible option in some situations.

### Mineral silicate paints

Mineral silicate paints are mineral-based coatings formulated with potassium silicate or sodium silicate, otherwise known as waterglass, as the binder, combined with inorganic, alkaline resistant pigments.368 They are fully inorganic—containing no organic solvents. Mineral paints petrify, by binding to any silicates within the substrate, forming a micro-crystalline structure and a vapour-permeable finish. They are also alkaline and therefore inhibit microbiotic growth, and reduce carbonisation of cementitious materials.369 Modern silicate paints are matt and coarse grained and therefore similar in some respects to the traditional stucco surfaces in appearance. Some brands contain acrylic resin binders and form an impervious finish which may be undesirable in many situations. Silicate paints are understood to have a 
long service life.

### Acrylic resin paints

Acrylic resin paints, known commercially as ‘acrylics’, now dominate the commercial and domestic market. They satisfy many environmental considerations and they have excellent performance properties on new structures—but not on heritage structures. Their main disadvantage is their poor vapour permeability. Paint manufacturers have developed and refined acrylic resin paints in an inexorable progression since World War II and production has probably reached a peak.370 They claim that the very best exterior water-based paints are 100% acrylic.371 Acrylic paints today are promoted in Australia as the most suitable paints for all external applications. Further, they are claimed to have sufficient vapour permeability for use on heritage building fabric—however, the evidence indicates they are unsuitable in many commonly found situations at heritage places. They have the advantage of being readily available in a vast range of colours and finishes, and they are easy to apply. They have the disadvantage of being relatively impervious. They form a thick film with limited vapour permeability, which may trap moisture or, worse, cause salt-laden moisture to accumulate in areas with catastrophic consequences 
for vulnerable stucco decoration.

It can be concluded that the physical characteristics and performance characteristics of acrylic paints are inconsistent with traditional finishes, and that they should not be considered for applications where authenticity and traditional performance characteristics are sought.

### Other paint types

The substantial array of further products on the market which could be suitable for use on stucco in some circumstances are too numerous to mention here. Furthermore, the relentless marketing of new products causes the range to be constantly changing. Paint manufacturers will advocate multi-layer paint systems where a high degree of waterproofing is required and will quote high rates of vapour permeability, which in reality are improbable and unlikely to be achieved. Others will advocate finishes containing fine aggregates (sand) to improve durability and surface texture. However, it should be noted that acrylic resins are a normal constituent of most modern, flexible paint finishes, and acrylic resins have been found in practice to inhibit the movement of moisture and salts, leading to alarming failures in some porous building fabric. For this reason, and for reasons of historical appropriateness, limewashes, cement washes, colour washes and, in some circumstances, silicate paints, are safer and more authentic finishes for use on Victorian stucco today.

## Conclusion

Recent examples of cleaning and re-coating of stucco façades demonstrate that insufficient attention is paid to the authentic nature of the finish and its conservation needs—far too often modern paint coatings are applied because they offer immediate and apparently economical solutions to perceived problems. In other cases, skim coatings of Portland cement-based mixtures are applied in the mistaken belief that they replicate original finishes. Skim coatings have not been covered in this discussion on conventional paint coatings and washes. The impact of the prevailing approach is that significant places have been and are being damaged by poorly considered work, and over the longer term the problems remain and often develop further.

The approach which should be adopted, and possibly even regulated, is to follow correct conservation procedures and make decisions based on the significance of the places and their real needs. Interventions, such as the removal of paint coatings, or the application of new paint coatings, should proceed only after careful consideration and trialling of the best options and with experienced professional input.

CASE STUDIES

Documentation: Peter Lovell

## W W Wardell, ‘English Scottish & Australian Chartered Bank Melbourne’ [specification] (Melbourne 1887)

### Mason & Bricklayer

Lime and Lime Mortar

The lime used is to be the best duck ponds Roche Lime or other approved lime of equal quality, and the lime mortar is to be composed of one part in measured proportions of lime and two parts of well washed clean sharp grit coarse drift sand of approved quality free from salt loam dirt and other impurities and Yan Yean water, the proportions of the lime and sand to be measured in a box before mixing.372

Cement and Cement Mortar

All of the cement used is to be the best London made Portland Cement of approved quality in every respect, and any that may be brought upon the ground which may not be approved on examination shall be removed from the premises, and the Contractor shall provide any tests for the Cement that the Architect may require.373

Where work is specified to be lain in Cement, it is to be taken to mean 
(except where otherwise specified) a mortar composed of the measured proportions of one part of cement and three parts of sand similar to that described for lime mortar, and all well mixed and tempered together with water.

Wardell specifies lime mortar in the footing courses and cement mortar is limited in application to the piers to take the iron columns that support the main banking chamber. He includes two damp proof courses: one set at basement floor level using ‘No. 1 Claridges Asphalte’ and the second set just below the ground floor level using ‘Callender & Sons pure Bitumen Damp Course’.374

The freestone facades to Collins Street 
and Queen Street are specified with both the sandstone ashlar and brickwork behind to be laid in cement mortar. As an alternative option, he indicates that the contractor is also to include in his tender for the walls to be laid in solid sandstone ashlar laid in lime mortar and punched on the internal face to be take a plaster finish.375 The specification goes on to indicate that all arches, and all walls that are in brickwork less than 18 inches thick are to be laid in cement mortar. All other brickwork is to be in lime mortar.

All work above the roof level including parapets, chimneys and copings is specified to be in cement mortar.

### Plasterer

Mortar	The mortar for the plastering is to be of equal parts of well burnt shell lime and clean sharp coarse sand free from salt and other impurities thoroughly mixed and tempered together with a sufficient quantity of good tough hair. The lime is to be run through a sieve and the mortar and fine stuff are to be made up at least three weeks before being used.

## Charles Mayes, The Australian Builders’ Price-Book (Melbourne 1886)

### Advertisements

The 1886 edition includes a number of advertisements including one for Best English Portland Cement; Castle Brand manufactured by Wm. Levett & Co., Ltd., London. The sole agents were MacDonnell & Busch of Bond Street Sydney. The advertisement states, ‘Likewise in Australia it is now the leading brand’, suggesting that it has an established presence in the market. Other cements advertised include those supplied by Petsch, Doehling & Co in Sydney, the Crown A1 Cement, ‘Stern’ or ‘Star’ Cement and ‘Faucus’ English Cement. In Melbourne, the Builders’ Lime and Cement Company advertises that it stocks ‘Portland Cement, ‘various brands’, and Alsen’s Portland Cement is advertised by the sole agents H Haege and Co. of Pitt Street, Sydney.

This edition of Mayes includes information on the tensile strength of various brands of Portland cement, indicating an increased interest in its overall strength and performance. In a more extensive article on Portland cement, Mayes notes that the strength of current cements is at least double the strength of those produced 40 years ago. This is said to be the result of ‘great competition among cement manufacturers.’376

In the section on plasterer’s work Mayes distinguishes between ‘stucco’ and lime plaster for external use and Portland Cement stucco. His pricing of cement renders is based on a one of cement to three of sand in a ¾ inch [19 mm] coat. 
He comments on the need to pre-wet surfaces and the use of a two-coat application. He also comments on the
 need for daily wetting to assist in curing 
for between three to 14 days dependant upon the weather.

In relation to lime plaster, he indicates that other than in Sydney the use of such plasters in external applications has been almost totally superseded by Portland Cement ‘compo’.

‘Callender’s’ pure bitumen damp proof course, the brand specified by Wardell for the E S & A Chartered Bank, is also advertised.

## Reed & Barnes, ‘Melbourne Town Hall Contract & Specification, 1868’

### Mason and Bricklayer

The specification distinguishes between work set in cement and work set in good lime mortar. The cement is specified to be the ‘very best Portland Cement’ mixed in a mortar comprising 1/3 cement and 2/3 sand. Lime mortar is specified to be in ‘fresh well burnt Geelong Roche Lime’ mixed in a mortar comprising 1/3 lime and 2/3 sand, all mixed in a pugmill. Work is generally specified to be in lime mortar, with cement being used in cornices and for dowels. Brickwork to arches is specified in 
cement mortar.

### Plasterer

Generally all internal work is in a lime plaster finished in plaster of Paris and all external work is specified in cement plaster ‘to be comprised of two (2) parts of clean sharp sand and one (1) part of cement, well mixed’. The cement is specified as the ‘best Portland Cement’.

Robert Haddon, in Australian Architecture of 1908, addresses external plastering in a section titled ‘Outside Cementing’. He notes that while such work is sometimes referred to as ‘stucco’, it is more typically referred to as ‘cementing’. His mixes are 1:4 cement and sand for the first or floating coat, and 1:2.5 cement and sand for the finishing coat.

In James Nangle’s Australian Building Practice of 1911, external plasterwork is addressed in his chapter, Plastering. His terminology in this chapter is mixed. In his introductory comments on external plastering, he includes a statement that such work involves ‘the covering of the wall or exterior of the building, with the rendering of cement mortar, called stucco’. Two paragraphs later, he titles a paragraph ‘The proportions of sand and cement for rendering’. Within this paragraph, the words stucco and rendering are used interchangeably, and rendering is the action of applying the stucco and the material itself. His mixes are 1:3 Portland cement to Sand and 1:2 for arises and exposed angles. He comments that rendering is generally done in one coat, but sometimes two.

On the use of ‘lime water’ and lime in 
the mix, he comments that this sometimes occurs to make the mix fat, but comments that this practice is to be condemned 
as ‘lime and cement fail to make a satisfactory mix’.

In the 1925 third edition and the 1944 fourth edition prepared by his son, the 
text on external plastering is unaltered.

## Terry & Oakden, What to Build and How to Build It (Melbourne 1885)

Brick cemented is too well known as a favourite building material amongst us to need much comment; while it has little to recommend it from an art point of view, it is cheap and convenient, and has also the advantage of keeping the walls free from damp. When used, a direct imitation of stone should be avoided, as being in bad taste; the greatest danger is that of over-crowding the ornament, as the material is so pliant there is a great temptation to fall into this, the most vulgar of all errors. The most appropriate system of decoration is surface ornament as opposed to those features more essentially suggestive of stone (in particular, as in many others, architects are subject to the wishes of their clients, and often imitate stone in cement under compulsion). The whole front may be painted in some pleasing tint; such a treatment is observable in many of the Italian towns.377

Peter Lovell is a Director of Lovell Chen. He is a graduate of Melbourne University and qualified with a Bachelor of Building Degree. Over the past 30 years he has established himself as a key participant in the building conservation field and has been involved in many aspects of conservation practice.

Bontharambo tower: Greg Owen

abstract

scope of the project

philosophy of repair

investigation pre-access

post-access (during works)

render

repair types

paint

works as executed

access

render

Repair Type R1

Repair Type R2

Repair Type R3

Repair Type R4

Repair Type R5

Repair Type R6

Repair Type R7

Repair Type R8

Repair Type R9

conclusion

acknowledgements

## Abstract

The third homestead at ‘Bontharambo’ near Wangaratta was designed by Thomas Watts and built between 1857 and 1859 for the Reverend Joseph Docker. This report deals with the preservation and repair work undertaken on the rendered tower in 2007.

Bontharambo is significant for many reasons. The property has been in the Docker family since selection in 1838 and this, the third house, has been the family’s principal residence since 1859. The house contains furniture and effects overlanded from Windsor, near Sydney, from the original expedition. The interiors are relatively undisturbed and there are furnishings from subsequent generations. It exemplifies the wealth created in the colony in a relatively short time in the early pastoral period following on from the effects of the Victorian gold rush. It now seems that it is even more significant due to its early and well considered use of Portland and other cements in its construction in 1859.

Following a number of conservation studies of the property as a whole and of the 1859 house, the tower was determined to be the highest conservation priority and Period Restoration Services Pty Ltd was engaged to finalise the scope and specification, and to carry out the remedial works. Access to the work areas was expensive and difficult, which precluded full investigation in advance of the work. Once access was gained, many unexpected materials, including what are believed to be Roman and Portland cements in a number of different mortars, were found. This paper describes the materials found, as well as the philosophies, methodology and remedial techniques used.

## Scope of the project

The scope of the project was to preserve and repair the tower above eaves gutter level. This work would encompass all trades and fabrics encountered in this part of the building, which included, flat and ruled render,378 run mouldings, precast enrichments, brickwork, timber joinery (spiral stairs etc), timber framing and cladding, roof cladding, rainwater goods and painting. This document discusses only the issues relating to the plaster and its painting.

## Philosophy of repair

The objective of works was to:

- preserve as much extant and early fabric as was reasonably practicable, considering the cost, the expected life of the repair, and the usual Burra Charter considerations including reversibility and appropriateness

- present the tower as it would have been on completion in 1859.

There was no desire to make any change to the building unless it was driven by the building’s current or future preservation needs.

The general philosophies were those of the Burra Charter, but those most commonly used on a day to day basis were:

- ‘DAMANBALAP’—do as much as necessary but as little as possible

- ‘no broke no fix’—if it is not broken, don’t fix it; if it is broken (or not performing well under the circumstances) make changes very cautiously

- match extant trade work, in both methods and finishes.

Having said that, we believe:

- it is inappropriate to replicate faults or previous poor workmanship unless the lack of those faults is going to create a greater interpretation focus than replicating them

- it is inappropriate to rectify faults or poor previous workmanship or materials unless they seriously affect the future performance of the building, see ‘no broke no fix’ above.

## Investigation pre-access

The project was generally prompted by recommendations made by Allom Lovell & Associates who listed ‘investigate and rectify cause of cracking in tower’ as the highest priority for works to the homestead and discussed this.379 A subsequent structural report380 listed ‘tower cracking’ and ‘tower, render delamination’ as structural Issues of an urgency category ‘within 12 months’.

As a result of subsequent inspections and observations the following was prepared by the author and submitted to Heritage Victoria as part of a permit application:

Proposed Interventions 
and Methodology

Due to the access costs involved it is proposed to undertake all required conservation works to the tower to ground level381 but not to other adjacent parts of the building which will be the subject of later works stages.

The works we propose involve:

Structurally

Re-assess vertical cracking once access is available. The most likely repair strategy would be removal of render and insertion of helical S/S reinforcement right around the building at each level of cracking. Investigate other effective methods of repair that will involve less render removal.

Carefully remove severely fretted bricks and replace with matching bricks and mortar.

Repair/replace as necessary flooring and structural timberwork to third floor level roof/floor.

Renderwork

Re-adhere delaminated render wherever practicable by method currently being prepared by Lovell Chen.382

Remove and replace damaged render, not practicable to re-adhere, by traditional methods including insitu run mouldings and using matching materials and details to extant.

Repair where practicable, otherwise replace, enrichments and pressed elements e.g. balusters, urns, finails etc to exactly match extant.

Generally

Replace galvanized steel flashings to third floor level roof/floor. Repair/replace previously replaced roof cladding sections.

Replace all rotten timberwork and repair, tighten and reconstruct stairway (second to third floor levels).

Prepare and repaint all previously painted surfaces with matching materials, colours and finishes, including renderwork and timber.

Repair and make operational cast iron rainwater goods.

Remove concrete grano topping to second floor. Investigate original floor materials and construction. Repair/reconstruct floor to match original.

Replace defective lead flashings to second floor and to main roof box gutter.

## Post-access (during works)

### Render

Once access was available, another assessment of the fabric was made by the author. The undisturbed nature of the fabric was evident and it became obvious that the small amount of intervention that had taken place was limited to easily accessible areas. While there was some significant damage, many areas showed their original relatively unweathered condition. These areas, while showing little paint, showed almost every detail of the original workman’s finish.

The render was coarsely wood float finished and often showed poor workmanship in terms of plumb, level, square and line. A number of different materials also became apparent. Cornices and other weathering areas consisted of a hard mortar, which had cracked as a hard concrete does, with fewer but wider cracks as the work articulated. It was light grey in colour with a relatively fine sharp sand, and had the feel and appearance of an ordinary Portland cement (OPC) based mortar. More weather protected areas were of a softer off-white mortar with a fine sharp sand, which seemed to be lime based.

The parapet finials were of what is in my experience very unusual construction. They had a solid moulded finial, with enrichments planted on, but they were unusual in that this solid finial was built up of quarters in apparently precast pieces mitred at the corners and stuck together to form each level. This was then plastered over to give the desired finish. Even more unusual was that the precast quarters were a very strong brown concrete with a coarse sharp sand. This material was so strong we could not break or chip it manually and had to cut it for examination using a diamond blade. 
The mortar used to stick the pieces together and finish the finials was much softer (of moderate strength).

Where the northeast finial had been struck by lightning, it had broken into all its component precast pieces but none found were broken. The enrichments of the finials were precast, as expected, and were made of a brown fine sand concrete, of moderate strength.

Below the scope of our works, but visible from our access tower was a broken capital moulding of a pilaster, which showed construction similar to that of the finial bodies – precast moulded pieces of very hard brown concrete, mitred at the corners, stuck on to the pilaster and then thinly plastered over in a softer render.

The balusters from the parapet were severely eroded, although they were made from a brown concrete with a fine sharp sand, similar to the parapet finial enrichments (which did not show the erosion). The material was of moderate strength, stronger than I would expected of a lime based mix. The concrete had been weathering for quite some time and had been extensively patched with an OPC mortar. From my experience, the extant concrete had the appearance of a mortar mixed with the addition of gypsum plaster.383

When works to install horizontal reinforcement ring beams in the tower above the arcading began (see more detail below), the first brickwork bed joint to be prepared was the lower one in the rendered frieze and this was, as we expected, a simple task of hand chiselling out the lime mortar of the brickwork. However, the second higher band in the frieze level was totally different. The bed joint mortar was very tough, and could barely be removed with hammer and plugging chisel, the removal rate per hour being probably 5% that of the joint below. The mortar was of 
a light grey colour with fine sharp sand, which seemed to me to be using an OPC binder. Most of the joint was removed by the careful use of diamond blades and hammer and chisel.

All the materials found were assessed by the author for some of their basic physical characteristics, with a view to replacing this fabric with a similarly performing material. Characteristics included colour, strength, aggregate (size grading, shape, composition and cleanliness), porosity and density. Barrie Cooper viewed and tested some materials and gave verbal advice.

In particular we investigated aggregates which might enable reasonable thicknesses (up to 20 mm) of lime mortar to be applied without extensive shrinkage problems. We knew that if we applied such thicknesses using a fine sand similar to that of the extant render and float coats, we would get extensive shrinkage cracking. The existing render had coat thicknesses frequently up to 25 or 30 mm, with overall thicknesses up to 65 mm. Barrie Cooper advised the use of a coarse well graded clean sharp sand to which he had access, known as REL 1 from Lithgow NSW, and guaranteed that it would perform as we wanted in the ratio 12 sand: 4 lime putty: 1 metakaolin (pozzolan). So this mortar was used for all render and float coats to flat work and for coring to mouldings.

The list of defects to be repaired was revised following access and is summarised below

### Repair types

R1 Repair vertical cracking from arcading to top of upper cornice

R2 Repair vertical cracking to cornice other than R1

R3 Removal and replacement of poor previous OPC render repairs

R4 Replacement/patching of flat renderwork

R5 Replacement/patching of run mouldings

R6 Replacement/repair of precast finials, balusters and enrichments

R7 Refixing flat delaminated render

R8 Refixing run mouldings

R9 Repairing eroded brickwork and joints

For each of these repair types, a methodology was investigated and considered bearing in mind the general project objectives, in particular ‘DAMANBALAP’ and ‘no broke, no fix’.

### Mortars

As discussed, the site investigation revealed we now had a number of different extant mortars to consider. These were categorised as the ME series in table 1 below.

For each of these mortars, a replacement mortar, the MR series in table 1 below, was investigated and considered. In accordance with our general project objectives, if a mortar had performed well, considering its situation, then no changes were made to its basic properties. This was the case with all mortars except ME7 and ME9. ME7, the precast baluster mortar, had severely eroded, and ME9 (very hard precast moulding mortar), whilst the mortar had not failed at all, was so much harder than the mortar used to adhere the items together that failure of the jointing mortar was frequent.

Replacement mortars were chosen to roughly match the extant mortar’s engineering properties. As visual investigation revealed that all render had previously been painted with lime wash, the colour of the replacement mortar was considered to be less important.

Over the course of the work, it was revealed that all the brickwork from just below to the top of the cornice, and the render from the drip to the top of the cornice, was the tough [OPC?] mortar. Similarly, it became obvious from remnants of extant work that the top of the parapet and the external moulding, again to about the drip was the tough [OPC?] ME5 and ME6 mortars. The run mouldings below the drip were all in the softer [lime?] ME1 and ME2 mortars.

Further down the tower, the work was predominantly [lime?] ME1 and ME2 mortars except for the capitals at the arcading pillars—these were the most curious of all. The mouldings ran round all four sides of the pillars, with the external run being in the [OPC?] ME5 and ME6 mortars; the side (semi-exposed) runs being in the [lime?] ME1 and ME 2 mortars; and the internal runs and their corners (sheltered) being in gypsum plaster ME11 mortar – making three mortars in the one moulding!

## Paint

The investigation of any coating over the render had been an important part of the overall project from the beginning, but little surviving paint was to be found. Small cracks and crevices revealed what appeared to be a limewash of a mustard colour, but also revealed a brighter orange coating that looked like red lead. Areas of weather protected flat render showed a faint mustard colouring consistent with the traces of limewash traces. The east side of two chimneys (which would be difficult to access, and were weather protected and not easily seen) showed a two colour scheme with the mustard on the flue and a linen colour on the frieze and cornice of the chimney. Microscopic investigation indicated that these were not the first coats, but were close copies of the original coats underneath. Investigation for remnants of the linen-coloured lime wash was undertaken in places likely to coincide with a scheme based on the chimney evidence, but nothing conclusive was found. However, as the colour was so similar to much of the substrate material, we did not consider this surprising, given our limited ability to investigate. Most notable was that we did not find any other colour evidence. There was a widespread deposition of a purple black colour, which I disregarded, having frequently encountered such a deposit on lime render.384

In the owners’ possession is an excellent photograph, believed to date from 1875,385 showing the house from the north-east. This black and white photo shows a light tone on the friezes and cornices generally and a mid tone elsewhere, consistent with the evidence found on the chimney. More of the scheme revealed by the photo was checked for extant evidence to support it and some was found. Many viewers of the photo thought a further shade was present, but this was disregarded for three reasons. First, no physical evidence was found to support it; second, a black and white photo will always show the same colour as different tones under differing lighting conditions; and third, based on advice received it was already unusual to have an Italianate design with two colours (rather than one).386

Such a scheme using ‘mustard’ and ‘linen’ lime washes was used, based on both physical and photographic evidence. No laboratory analysis of the extant coatings was undertaken. Due to the difficulty and expense involved in recoating the lime wash at a later date, a proprietry lime wash was used which has a small proportion of acrylic binder added, Westox lime wash. This choice was a compromise between expected life and permeability.

## Works as executed

### Access

Access was a major element of the works, in terms of both cost and planning. Whilst there are always numerous options, in situ run rendered mouldings need fixed scaffolding to be really successful. Using fixed (modular) scaffolding, two options were then available – scaffolding supported by both the ground and building through slate roof penetrations, or scaffolding supported by steel beams through the tower openings, a relatively common practice for accessing church spires. The latter was chosen because of the lesser risk of roof leaks over significant fabric, and because of the similar engineering complexity (the scaffolding over the house had to be supported by steel beams anyway, as the walls did not coincide with any configuration of scaffold layout we could come up with). The abnormal aspect of this was that the beams had to be located midway up the scaffold so the upper part was supported by the beams in the normal fashion, but the lower part had to hang from them.

Once the scaffold was erected, and a stair access tower was installed beside it, the whole scaffold perimeter was covered with shadecloth and a custom-made tarpaulin was erected over the top to give a relatively controlled environment. This allowed work to proceed in bad weather and also enabled more controlled curing of the lime mortars to be used.

## Render

Our initial work consisted of structural work on the balustraded parapet and the vertical cracking above the arcading and through the upper cornice.

Repair type R1, repair of vertical cracking from the arcading to top of the upper cornice

The vertical cracking from the arcading to the upper cornice on each elevation was restrained by installing bands of reinforcement right around the tower structure, and vertically in the rendered frieze above the arcade keystones. Each band consisted of 2 x 6 mm proprietary twisted stainless steel ribbon (Helibar in this case) grouted in with the manufacturer’s highly cementitious grout (Helibond MM2). This reinforcement was inserted into the brickwork bed joints by chiselling out the bedding mortar , injecting grout into the joint, pushing the reinforcement into the grout, injecting another layer of grout, installing another layer of reinforcement, and then injecting a final layer of grout and pressing it firmly into the joint and reinforcement with a finger trowel. The whole installation was pre-wetted and then kept wet to ensure good curing. Then the last of the bed joint was repointed with a mortar to match the adjacent extant mortar.

It was also proposed to use twisted stainless steel ribbon reinforcement for the cracking on the cornice itself and this was done locally, see repair type R2. However, during the works we discovered that the cornice was hollow. The cornice was started in the usual fashion by corbelling out brickwork and then the projection was created by cantilevering two layers of roofing slate and bricking onto them again. Maybe in an effort to reduce the weight of the cornice, the next two courses were left out internally and then the cavity covered with slate again and brickwork recommenced to form the cornice coping. As a result of this opportunity, we used the cavity to locate a reinforced concrete ring beam in the cornice. A few bricks were removed from the corona of the cornice at each corner and a galvanised reinforcing bar was inserted, already cranked to go around the corner and tie to the next length. Once the reinforcement was suitably held at the correct location, the holes were closed and the cavity filled with a modern mix low alkali concrete and vibrated from holes opened in the coping. The render work was then reinstated.

### Repair Type R2, repair of vertical cracking in cornice, other than type R1

Repairs to the cracking on the corona of the cornice were undertaken using localised crack stitching with twisted stainless steel ribbon and grout otherwise as per R1.

### Repair Type R3, removal and replacement of poor previous OPC render repairs

The internal face of the parapet, being accessible, had been repaired with a very strong OPC mortar, which displayed very poor workmanship. This situation of very strong OPC repair mortars over extant masonry, consisting of underfired bricks and lime bedding mortars, is a common one in our experience, and one that makes it very difficult to achieve a good outcome with minimal disturbance of the brickwork. This case was no exception, with even the most gentle attempts to remove the render causing the removal of the bricks from the wall. Therefore, there was significant removal and reconstruction of the brickwork on two elevations of the parapet.

This reconstruction used primarily the original bricks, supplemented with recycled bricks with similar engineering properties, and a lime mortar MR3 made from local ‘bricklayers sand’, slaked lime and metakaolin (pozzolanic material) in the ratio 12:4:1. In an attempt to meet the important need for lime mortars to cure adequately (which requires, among other things, slow dehydration), and given with the typical extremely high suction of the extant construction (dry old underfired bricks and lime mortar), copious amounts of water were used to pre-wet both the undisturbed brickwork and the bricks to be re-used. The finished work was kept moist with a lesser amount of water, so as not to wash the new mortar away, but on a frequent basis. We often used a pressure washer on low pressure, fan spray setting at a distance of at least 1.5 metres to give a very even mist spray to the work at frequent intervals.

The iron bars spanning the openings in which the balusters are mounted were mechanically cleaned by chipping, wire brushing and so on, and painted with cold galvanising primer.

### Repair Type R4, replacement/patching of flat render

At the level of the pillars in the arcading there was significant loss of render. This was most prominent at the southeast corner below the tower stormwater outlet, rainhead and downpipe. Render had obviously been lost for some time as there was also some significant joint and individual brick erosion. Render that we did not consider could be satisfactorily re-adhered was removed, and all the missing render was replaced. All the work was in three or more coats, depending on the thickness, which ranged up to 65 mm. Thicker work was built up in 20 mm coats. Adhesive bonding agent (acrylic, not PVA) was only used very selectively where OPC mortars were needed to bond to extant OPC mortars. This occurred almost exclusively where the coping of cornices needed to be replaced: here good adhesion and the prevention of cracking were paramount to prevent future water penetration, which is a common cause of cornice failure.

New work was not purposely made to be visually apparent to future viewers, although much would be to a trained eye. While I can understand the desire for this from philosophical principles, in my experience, it is not normal conservation practice in Victoria.

### Repair Type R5, replacement/patching of run mouldings

Once again, mouldings that we did not consider could be satisfactorily re-adhered were removed, and all the missing render replaced with mortars that matched the original mortar’s engineering properties. An adhesive bonding agent was used – more often than for flat work where larger moulding sections were to be bonded to extant work. Where there was a concern in bonding larger sections to extant work or substrate, or where the construction made future cracking more likely, stainless steel threaded rod was installed with polyester adhesive as ‘starter bars’. All mouldings to be replaced were reconstructed by running in situ, using traditional methods.

### Repair Type R6, replacement/repair of precast finials, balusters and enrichments

#### Precast corner finials

As mentioned previously, the extant finials were made up of numerous precast Roman cement (ME9) items stuck together with mortar and then plastered over to a suitable finish. The enrichments were then planted on the body.

This original construction method was not entirely satisfactory, as some of the finials had cracked or come apart where they were stuck together. To reconstruct the required replacement finial by the original method would have been more time-consuming and it would have been likely to fail in a similar manner. Therefore, the replacement finial was produced by a mixture of run moulding and casting. The base and top were run on the bench to match the extant finials, with stainless steel rod protruding from the top of the base section. The base was then placed in position on the top of the tower and bedded into position in ME6 mortar. Formwork was then constructed onto the base slightly smaller than finished dimensions, and cast with modern concrete mix to reproduce the central cube of the finial. This was later finished with a final render coat to final dimension. The top moulded section was then bedded onto the central cube.

[Intermediate finials were in much better condition, probably due to being precast in fewer sections. Only one replacement top section was required, and this was reproduced by moulding on the bench.

#### Enrichments

As is often the case, the decoration on the finials was made up of many precast pieces planted onto the finial body. The originals were made of ME8 [Roman cement?] mortar. The enrichments were examined to locate the join between castings, and the best of each section of enrichment was identified, and if still in position, carefully removed. Each extant piece of enrichment was cleaned, repaired with gypsum plaster where necessary, and mounted on plywood. Thickened silicone moulding rubber was then applied to make a mould, and a plaster mould case was poured over to maintain the mould shape. The extant enrichment was removed and the silicone moulds used to cast numerous new items with a MR8 natural cement mortar. In total, 12 moulds were made, and a total of approximately 64 enrichments precast and planted onto the finials.

#### Balusters

The extant balusters were all very severely weather eroded. Each baluster that showed the original shape and detail in some section or another, was tagged and carefully removed. The baluster profile was reconstructed by measuring each intact section and drawing it in CAD. A full size replica was then reproduced in gypsum plaster by traditional plastering methods using a lathe. From that pattern, a full size silicone rubber mould was cast inside a timber mould case, again to retain its shape. The rubber was cut to allow removal of the pattern and then the mould reassembled. The mould was used to pour multiple castings using a MR7 modern OPC concrete mix. The full mould was propped horizontally and exactly half-filled with casting (gypsum) plaster to form a pattern for a half baluster of which one is required at each end of each balustrade opening. This pattern was mounted on plywood and then covered with thickened moulding silicone, and a plaster mould case and reproduction half balusters recast as per the full items. In total 36 full and 24 half balusters were produced. The new balusters were installed into the preformed balustrade openings and secured by ME2 mortar top and bottom, and then the surrounds were weathered to shed water.

### Repair Type R7, refixing flat delaminated render

Large areas of delaminated render were present in both the pillars and the internal flat work up inside the arcaded level. Most of these delaminated areas were around 30–40 mm thick with some up to 65 mm, so the render was quite strong in itself. We were familiar with the practice of re-glueing internal plaster ceilings back to laths from above using acrylic adhesives, so we investigated and experimented with using this method, eventually with good success. The products used were the Westox RAP adhesives, the only Australian-made products of this type known to me. Normally with these adhesives, the suction of the render is controlled, and the material locally stabilised, by the introduction of a very thin watery sealer, which penetrates and soaks deeply into the material. The adhesive is then introduced (poured, injected etc) into the space, and it penetrates and glues the render to the substrate. Without the sealant, the render suction is likely to be so great that the penetration of the glue will be very poor.

Where the delaminated render had moved away from the substrate leaving a gap (the very hollow drummy sections) this standard adhesive procedure was undertaken using approx 10 mm holes drilled for access. Where the delaminated render was still quite tight against the substrate (drummy, but not hollow by the tap test) we could not get penetration by this method. With experimentation, we found that by pre-wetting the render and substrate with water through the access holes, and then dripping in the adhesive (with no sealant) we could get a fairly consistent minimum of about 50 mm penetration around the hole, giving a 100 mm dot of adhesion. Not all the injections were successful, but these were apparent the following day by the tap test. The result was large areas of render held to the substrate with a matrix of adhesive dots. As it is very important that masonry remains breathable, it is important that the entire surface is not sealed with the acrylic adhesive. The final method gave a compromise between adhesion and permeability.

### Repair Type R8, refixing run mouldings

In a number of locations, the existing run mouldings had lost adhesion to their substrate, or the substrate had become unstable. In severe cases, these mouldings were completely separated from the substrate, while the substrate was rebuilt or stabilised. In other cases, the mouldings were loose or severely drummy by the 
tap test.

Where the moulding was relatively small and with a small projection, acrylic adhesive was used as for flat work repair in R7. We were not confident enough of the strength of the acrylic adhesives to hold a large moulding, where the gluing area is relatively small and the weight high. In these cases, we pinned the mould with stainless steel threaded rods into the substrate and fixed the pins with a commercial two part polyester adhesive, Ramset Chemset 101. Typically, 6 mm pins were used in an 8 or 10 mm hole. Twisted stainless steel ribbon could have been used, but at a greater cost for the materials, and I am also reluctant to use the highly cementitious grouts where I don’t have to.

### Repair Type R9, repairing eroded brickwork and joints

Repairs of this type were quite simple and used common conservation methods. Where the bricks were severely eroded, they were replaced with recycled bricks from another site, which roughly matched the engineering characteristics and size of the better quality extant bricks. Introduced bricks were laid and mortar joints were repointed, in a mortar matching the work in that area (MR3 or MR4).

## Conclusion

Bontharambo needs further materials research, but it seems to be a remarkable example of the pioneering use of materials new to Australia. It seems to have used Roman cement for precast elements – an expensive material imported from England from about the 1820s – but it is its very early use of Portland cement that is so remarkable. The first Portland cement was imported into Melbourne around 1850 (discussed elsewhere in these proceedings), and here we have it used in the construction of a country homestead, albeit an impressive one. The heavy material would have been carted by wagon to Wangaratta. Not only was it used, but it was used appropriately in areas subject to high weathering, where lime would have a much shorter life. In areas where lime could be expected to perform satisfactorily, lime mortars were used.

At the time, with the nearby goldfields of the Ovens and Beechworth areas luring workers, it must have been very difficult to get skilled tradesmen, and even more to get men who could adapt to new materials with poor workability. This is probably why much of the plastering of the tower does not reflect high quality trade skills.

Further investigation of the mortar materials is definitely warranted, but it is expensive to get meaningful results. The standard testing which is routinely undertaken is, in my opinion, usually of questionable benefit. Binder ratio tests, when undertaken to the Australian Standard to determine lime and cement ratios, make some inappropriate assumptions and are often inaccurate. They are also not designed for the alternative binders which we have found on this site. In my experience simple visual (both micro and macroscopic) and tactile analysis by a person familiar with the typical materials is quite reliable and can often only be bettered by very expensive analytical testing.

A review of our industry mortar testing methods is overdue.

It is very common practice for all loose and delaminated render to be replaced with new material during conservation works. There is enormous potential for the greater retention of extant render by the innovative use of adhesives and pinning techniques. Particularly in the case of run mouldings, the re-adhesion processes are often less expensive than the less desirable practice of replacing them.

As I find is so often the case, works such as this highlight more that we don’t know, rather than what we do. How is it in this technological age we don’t know how to replicate the nineteenth century practice of thick coats of fine sand/lime render, which don’t crack up?

Greg Owen is a maintenance engineer by background, having specialised in buildings and services before he formed Period Restoration Services Pty Ltd, a company which undertakes only building conservation work. He has a strong interest in the science and technology of building conservation as well as the maintenance of a wide range of traditional trade skills. He practices trade skills, hands on, in solid plastering and other areas.

## Acknowledgements

John Paul and Mary Paul née Docker (for their significant financial investment in the future of Bontharambo, particularly in these times of poor farming returns, and for their passion for the place); and to the Period Restoration Services team.

Stucco – Malmsbury Town Hall: 
Michael Dempsey

abstract

history

applied finishes

scope of the project

aims and objectives

methodology

philosophy of repair

works as executed

methods

conclusion

## Abstract

A small project to conserve the exterior stucco of Malmsbury Town Hall had two elements—replacing the missing stucco with lime mortar, and stabilising areas of existing stucco with a range of adhesives. The missing sand and cement stucco was replaced with a 3:1 sand and lime putty with 25% pozzolan by volume to lime. This was done in view of the excessive moisture in these areas. Cracks and drummy areas were repaired using the Westox system of adhesives and additives. Neither of these processes was consistent with the materials and techniques of the original stucco, but they have been successful in retaining the original material whilst consolidating the structure and the intact evidence of its original construction.

## History

The Malmsbury Town Hall was built in 1868. It is a bluestone gable-roofed structure, with an impressive pedimented front façade complete with Doric pilasters. The walls are constructed in bluestone. They are divided into bays by grey stuccoed brick pilasters and there is stuccoed brick detailing around the windows. The original front façade, which was fully stuccoed, became unstable, and was demolished in 1947. It was rebuilt in red face brick but the stucco finish was not reinstated, for reasons that are not apparent.

## Applied finishes

The coursed rubble bluestone walls of Malmsbury Town Hall are divided into bays by grey stuccoed brick pilasters and the stuccoed brick detailing around the windows has a smooth finish. The lower parts of the stuccoed pilasters show some evidence of a yellow ochre finish coating, suggesting the colour we see today may not have been the intended final finish. It could be assumed that it was the intention of the original designer to imitate the use of two different stone finishes using the cost-effective sand and cement stucco to carry out the fine imitation dressed stone elements of the front façade. This original façade was rebuilt in red brick without reinstating any of the original decorative stucco, but the majority of the remaining stucco is in sound condition.

The original choice of Portland cement as a binder in the stucco of this modest structure may be significant, as Portland cement was a relatively new material at the time and yet to supplant lime as the preferred binding medium in this type of work in Victoria. However, there were many possible reasons for its use, and care was therefore exercised in the recent work to preserve the original fabric without unnecessary replacement.

## Scope of the project

The extent of the external stucco requiring repairs at Malmsbury Town Hall was small. The work required to reinstate the missing parts and stabilise the drummy areas and repair cracks was not extensive. It was confined mainly to the pilasters where damp had entered and disrupted the fabric, and some other parts where the Portland cement stucco had become detached.

## Aims and objectives

The primary aim was to conserve the existing sand and cement stucco with minimal loss of existing fabric or surface patina. The practical and ethical issues involved in doing this served to highlight the significance of the fabric as it is known, and the potential significance that might be revealed in future research. It aimed to raise the awareness of the vulnerability of cement stucco to unnecessary replacement.

## Methodology

Three potential repair methods were considered.

The first method considered was to remove all loose stucco and replace it with a modern sand and cement stucco. The advantages of that would have been ease of work and a very durable finish. The work would also be legible as repairs. The disadvantage of this method would be that the sand and cement stucco would not allow moisture to escape from the already damp base fabric. Furthermore, the removal of large areas of the original material would have meant the loss of existing fabric and patina.

The second method considered was to remove all loose stucco and replace it with lime-based stucco. This would increase the longevity of the structure by reinstating a durable and porous stucco, which would cope with the moisture in the base fabric. This option would also be clearly legible as a repair when the new material was compared with the original. The disadvantage of this method was the loss of existing fabric and surface patina.

The third method considered, and the one that was proposed and accepted, was to consolidate all loose stucco and to repair missing stucco with a lime stucco matched in colour, tone and texture. The lime stucco would provide increased breathability (moisture transportation) in the areas of loss, whilst sheltering the base fabric from the ingress of further moisture from wind-driven rain. The consolidation would conserve the fabric that had as yet suffered only minimal degradation, thus retaining the patina and the existing fabric. This would minimise the aesthetic change to the place and retain its authentic appearance to the maximum practicable extent. This method proved to be the most advantageous in this instance. Replacing missing stucco with lime stucco provided a vehicle for moisture transportation helped the structure to dry out. By re-adhering the existing loose stucco, we retained the existing surface patina and any remains of original finishes.

## Philosophy of repair

Areas of missing stucco were replaced with lime stucco, which complemented the longevity of the structure. A good colour and texture match was aimed for, so that the aesthetics of the structure were not affected. In relation to the legibility of repair, Brandi suggests that one method is to rebate the surface slightly. This would provide a good aesthetic effect at first glance but still provide evidence that is easily read upon closer inspection.387 These ideals are echoed by the Burra Charter, which holds that that repairs should not be obvious but detectable. In the case of these stucco repairs, it proved more practicable to have the new material slightly raised, due to the need to mask the existing fabric, so as to protect it from smudging from the new stucco.

Earl summarises the debate between the visible and invisible and concludes ‘The general rule that the work of modern hands should be clearly seen, so as not to confuse the historical record or dilute the authenticity of the original fabric, is as reasonable as to invite instant adoption’. However, Earl also cautions against adopting too extreme an approach. ‘Aggressively visible repairs can distract attention from the very qualities that mark out a building for preservation. A little discretion may be no bad thing.’388 Earl and Brandi require a repair to be obvious to the professional, and only apparent to the layperson when it has been pointed out. From this practical perspective, replacement of fabric should be carried out in a manner that is recognisable as a modern intervention but does not detract from the aesthetics of the building.389

The missing stucco was repaired with a tinted lime stucco, which contained sand similar in colour to that of the existing stucco. Trass was used as the pozzolan, and its colour helped in toning down the new lime stucco to match the existing. Lime-based stucco provided breath-ability to areas of the structure that were suffering from moisture issues. The lime stucco could be treated as a poultice, and replaced with a different material later if required, when the areas of the structure were dry.

It was appropriate to re-adhere existing loose stucco to the background. This approach would retain the authenticity of the fabric, the patina, retain existing original finishes and, under closer inspection, it would be apparent that intervention works had been carried out. This style of repair would not align itself with the honest SPAB protocol but it would provide respect for the ‘authenticity in the conservation of the common heritage’.390

## Works as executed

Cracks were repaired in two ways. Minor cracks were edged with masking tape on either side to prevent unsightly smudging during the filling process. The filling material was, 6 sand: 1 cement: 1 lime, the gauge water was a mixture of 3 parts: 1 part Westox RAP adhesive.

Cracks relating to drummy stucco were treated with the Westox re-adhesion system as shown in the figures below. 
The RAP (render and plaster) system contains acrylic binders in four formulations and can be used for re-adhering loose (drummy) render to brick or stone.

### Methods

1.	RAP primer: penetrating primer carried in alcohol, primes the surfaces and provides initial bonding, reduces suction to aid the penetration of the high resin solids adhesive.

2. 	RAP adhesive: high resin solids adhesive (50% resin) acts as an adhesive over the pre-primed surface.

3. 	RAP thickened adhesive: thickened version of the RAP adhesive and used over a pre-primed surface where larger voids are present.391

Initially, all cracks around the surrounding drummy stucco needed to be packed with plasticine to prevent the re-adhesion liquid escaping. A small hole was drilled into the drummy area to provide access for RAP 
primer. When dry, RAP adhesive was used 
in a similar manner.

In method 1 (illustrated) RAP primer was gravity fed, and when dry, RAP adhesive was also fed to re-adhere the stucco. Thickened RAP, which was able to bridge any larger gap between the stucco and brickwork, was also used.

The replacement of the missing stucco was carried out with well-graded washed sand and lime putty (in the ratio 3:1) with the addition of 25% pozzolan by volume to the lime putty. The stucco surrounding the area to be replaced was taped with masking tape to protect it from unsightly smudging, and to provide a very slightly raised surface to make the repair readable. The brickwork was moistened to avoid excessive suction prior to application. The lime mortar was mixed to a workable consistency without using excessive moisture. It was then applied working it into the surface to achieve a good key. The mortar was worked to avoid hairline cracking through hand floating and controlling the level of moisture in the mortar. This lime stucco may be replaced after approximately two years, if required. Two years is a fair amount of time to allow a pilaster in a structure such as this to dry out.

## Conclusion

The work carried out at Malmsbury Town Hall has endeavoured to preserve authenticity and surface patina, whilst also trying to do what is best for the longevity of the building. Three approaches were considered, but it was chosen to consolidate the loose stucco. This case study provided first-hand knowledge of the vulnerability of surface patina, authenticity, original architectural finishes and characteristics of sand and cement stucco.

The sand and cement stucco has proven itself to be a valuable heritage resource. This resource has the ability to retain archaeological data, architectural detail, original finishes, patina, aesthetics, authenticity and meaning. This outweighs the potential for replacing drummy stucco even though the cost of consolidation is higher. Given the importance of the original fabric, it is important to recognise its vulnerability and to guard against loss of fabric where possible.

Michael Dempsey has been working in building restoration for the last 25 years, in Ireland, England and Australia. He served a traditional apprenticeship in Ireland in the craft of plastering, where he was awarded Junior and Senior Craft Certificates. He went on further to gain the London City and Guilds Craft and Advanced Craft Certificate. In 2007, he was awarded his Masters from the University of York, UK, in the Conservation of Historic Buildings. He runs his own conservation business and lives and works in Melbourne.

A sampling of terminology

## Britain

Loudon, Cottage, Farm and Villa Architecture, pp 259-60 [§ 527]. ‘The cements for stuccoing are chiefly the Roman cement, of which there are two kinds common in Britain, Parker’s and Mulgrave’s; the Puzzolano; the tarras; the gypsum; the mastic; Frost’s cement; the metallic cement; and Bailey’s composition’.

Weale, Terms used in Architecture, p 472: ‘Stucco, in architecture, a composition of white marble pulverized and mixed with plaster or lime, but the ingredients vary; it is employed commonly for facing exterior and interior works…’

Donaldson, Handbook of Specifications, p 661, ‘Walls. – Finish with trowel stucco…’ [internal] as distinct from p 662, ‘Portland Cement Work externally’ [string courses, rusticated work, window dressings, cornices, enrichments and walls generally].

Farrow, Specifications for Building Works [no mention of stucco], p 96: ‘External plastering may be carried out in Portland cement, lime stucco, or in rough cast’.

Gwilt, Encyclopædia of Architecture [1881], p 675 [§ 2238], ‘When a wall is to be plastered, it is called rendering’ p 675 [2243-4]—description of bastard stucco and trowelled stucco [both lime-based].

Laxton’s Builder’s Price Book for 1863, p150, ‘Stucco: per yard’, as distinct from p153, ‘Portland Cement’ [refers to the appearance approximating Portland stone]. As distinct in turn from, p153, ‘Roman Cement’ and ‘Johns & Co’s Patent Stucco Cement’; p154 ‘Metallic Cement’, ‘Mastic’; and ‘Atkinson’s Cement’.

Leaning, Building Specifications, [no mention of stucco]; p 500 ‘All the work coloured grey on the elevations to be executed in Portland cement’.

Millar, Plastering Plain and Decorative, [1905], p107: ‘In England stucco is … used loosely for various plastic mixtures in whose composition lime, plaster, or cements enter. Hydraulic lime was formerly used for external stucco. Roman cement … Selenitic lime ... These materials are now entirely superseded by Portland cement.’ Pp109-110, ‘London stuccos’—describes four types, all lime-based. Pp187 ff, ‘Portland cement façades’—at no point referred to as ‘stucco’. P 510: ‘Concrete Dressings. – Architectural works, especially large or plain parts, are generally cast in wood moulds’.

Rea, How to Estimate, [no mention of stucco]; p 331, ‘Rendering with Haired Mortar’ [using lime], as distinct from p 336 ‘Rendering with Portland Cement’.

Sutcliffe, Modern House Construction (new ed, 6 vols, London 1909): II, pp114, 124; VI, p 374: ‘Portland-cement stucco’.

Middleton, Modern Buildings, II (H Y Margary on Plastering): [no mention of stucco]; p 200 ‘Compo or cement rendering is the covering of large surfaces, such as the fronts of houses, with a mixture of Portland cement and sand’.

F W Macey, Specifications in Detail (3rd ed, London 1922), p 444: ‘Lime stucco, whether plain or roughcast, is suitable for external work, but seldom now used, Portland cement stucco having taken its place.’ Reference also to ‘Rough cast lime stucco’, and ‘Rough cast Portland cement stucco’.

W Verrall et al, The Modern Plasterer (2 vols, London, no date [c 1930]): II, p143, ‘By Portland cement stucco is meant something different from, and superior to, an ordinary mixture of cement and sand’.

Young, Spons’ Price Book 1935 [1935]: p186, ‘Bastard stucco, Trowelled Stucco’; as distinct from p187, ‘Rendering’; p 188, ‘Rendering in White Atlas Cement; Rough Cast’.

## Australia

Mayes, Australian Builders Price-Book [1862], p 76, ‘Stucco or External Plastering’ gives prices for bastard or rough stucco, trowelled stucco, &c, very much in the Millar manner, but completely distinct from ‘Portland Cement’, p 77, which includes ‘rough render’, ‘plain faced, on brick, jointed’, &c. This in turn is distinct from ‘Composition enrichments’, p 81, which include capitals, pilasters, trusses, &c.

Mayes, Australian Builders’ Price-Book [1877], p 85: ‘Stucco or lime plaster for external use is now superseded in Sydney and Melbourne by Portland cement compo…’

Australasian Builder and Contractors’ News

23 August 1890, p 123: New Buildings, Camberwell, for the Commercial Bank of Australia … Elevations are in brick with cement facings.

27 September 1890, p 227: We publish a number of designs of plaster and cement castings by G T Cross.

17 March 1894, p 127: Cottage at Harnleigh, New South Wales … ‘The walls are of brick, cemented externally …’.

14 April 1894, p 177: New Offices of the City Mutual Life Assurance Society, Limited, Sydney … ‘The elevations, which are finished in cement…’.

Haddon, Australian Architecture, p 91, ‘The term “stucco” is sometimes applied to cemented surfaces, but it is not of altogether general application, ordinary Portland cement and sand work being generally referred to as “cementing”’.

Nangle, Australian Building Practice (2nd ed, Sydney 1911), p 366, ‘the rendering of cement mortar, called stucco’, however, the diagrams, pp 366, 368, qualify it 
as ‘cement stucco’, and the text has no further reference to stucco but to ‘external plastering’, ‘rendering’ and ‘rough cast’.

Richardson, Ramsay’s Catalogue [1931], § 21d, Australian Cement Manufacturers’ Association: ‘Portland cement stucco’.

Sharp, Australian Methods of Building Construction no mention of the word ‘stucco’ but p 280 ‘A cement mortar is used for plastering the exterior of buildings’; p 281, diagram, ‘cement render’ appears within the drawing and ‘cement rendering’ in the caption.

Department of Labour and National Service, Plastering, p 42: ‘Rendering is the name given to a coating of Portland cement mortar’; p 160 ‘Stucco. An external rendering. The name given to a fine plaster composition’.

Mackey, Gregory’s Modern Building Practice, p 172, ‘Before the development of Portland cement various mixtures were employed for external work with more or less success and the name “stucco” was given to them. To-day the term is applied to all kinds of external rendering. Cement rendering externally is usually carried out …’

Virgo, Australasian Building Knowledge (Volume 2), 
[no mention of stucco]; p 151, ‘External Plaster Work … Portland cement is unquestionably the best material for external plastering.’

Glossary

#### Accelerator

A substance which increases the speed of a chemical reaction, and in plastering, one used to speed up the setting time, such as common salt, alum, borax, Epsom salt (magnesium sulphate) or washing soda.

#### Acrylic

A plastic material used as the basis for quick drying paints and other materials. Acrylic acid is the common name for 2-propenoic acid: CH2=CHCO2H, and other acrylic polymers are formed by polymerising an ester of this acid, such as methyl acrylate.

#### Acrylic paint, see Paint, acrylic

#### Albarium opus

A term used by Vitruvius for pure white lime coat to the surface of which crushed marble was added to give a marble-like external finish, used especially in the Achaean temples of southern Italy.

#### Ashlar

Finely dressed squared stone laid in coursework with regular horizontal and vertical joints, usually thin. The finish is often imitated in plastering, externally by ruling a fine groove and/or marking the purported joint with a pencil or wax crayon; internally more often by marking only, a red line being often favoured.

#### Browning, see Floating.

#### Calcination

Prolonged heating of a material at high temperatures to drive off water and/or carbon dioxide.

#### Cannabic work

A nineteenth century term for plaster reinforced with hemp, based on the English patent taken out by Albano in 1843: essentially an early form of fibrous plaster.

#### Cement, artificial

A cement manufactured by mixing the ingredients, mainly limestone and clay, in optimal proportions before calcining.

#### Cement, natural

A cement manufactured from a raw material containing calcium carbonate and clay in suitable proportions.

#### Cement, Portland

An artificial hydraulic cement, originally made by burning the limestone and clay at a higher temperature than previously, and grinding the product, including the clinker (or partly fused product). It was named from its resemblance to Portland stone when used in stucco or castings, and is referred to in Australia as general purpose Portland cement, Type GP.

#### Cement, Roman

A natural cement, misleadingly named Roman cement in order to promote it, and because of its superiority to existing commercial products. It was manufactured originally by Parker & Wyatt of London from septaria nodules found on the Isle of Sheppey, and tended to be distinctly brown in colour. The cement actually used by the Romans gained its special quality largely from the addition of pozzuolana to common or hydraulic lime.

#### Cement-based paint: see Paint, cement-based.

#### Cement render

Hard-setting mortar covering, made from a mix of Portland cement and sand, with or without the addition of lime, for masonry wall surfaces. See also Stucco.

#### Chunam

An Indian fine plaster of shell lime, jaghery [sugar water], egg white and ghee [clarified butter] in various proportions. Versions of this were used for early flat roofs in Australia, but the term is oddly used in Australia by Mayes for a mixture of lime and ‘thin black oil’, and a similar material was subsequently used to waterproof the Sydney wharves.

#### Compo, see Mortar, compo [composition]

#### Copperas

Iron sulphate, commonly added to stucco as a colourant in the late nineteenth century.

#### Core

The rough shape forming the heart of a mould such as a cornice, made by such means as corbelling bricks out from the wall surface.

#### Cove

A continuous concave moulding at the internal angle between two surfaces, typically within a cornice, but also used of a curved transition between a floor and a wall surface.

#### Controlled setting

That in which over-rapid drying is prevented by applying a fine spray of water or draping the work in damp cloth.

#### Dash coat

A lime or cement-based mix thrown against a wall surface, either as the intended finishing or as pricking-up for subsequent rendering. See also Roughcast, Pebbledash.

#### Distemper

A cheap form of water soluble paint consisting of a white base pigment (usually crushed chalk) and an organic binder in solution (usually animal glue size in water). It was often heavily pigmented and used for internal walls and ceilings. But, distemper made of skimmed milk, quicklime, linseed oil, and a colouring agent such as whiting or ochre was recommended in Australia in 1861 as a means of colouring stucco.

#### Dots, see Screeds

#### Expanded metal

A diamond grid of metal, made by creating a staggered pattern of slits in a sheet, and then pulling it apart laterally. It was invented by the American John F Golding in 1884 and used as lathing, and later used also in reinforced concrete. The Australasian rights were obtained by the Expanded Metal Lathing and Fencing Company Limited, which had a machine at work producing the material at the Centennial International Exhibition, Melbourne, of 1888–89.

#### Fibrous plaster, see Plaster, fibrous

#### Finish coat (plaster), see Plaster coat, finish

#### Finishing, see Setting

#### First coating, see Pricking up

#### Flanking

Filling in plaster between screeds and ruling the work off straight and flush.

#### Float (verb)

To straighten and level a plaster surface or to finish a fresh concrete surface by the use of a float.

#### Float (tool)

A hand tool, usually a flat rectangular plate of steel or timber with a handle, used to finish a surface of concrete, plaster or render. A type with a wooden blade about 270 x 115 mm, is used as a general purpose float on large walls and ceilings. In plasterwork a hand float is used for truing-up and surfacing an undercoat or for providing a rough finish to a finishing coat (off-the-float finish).

#### Floating (and float coat)

In three-coat plaster, the application of the second coat (or second coating) by means of a float to form a true surface for the finishing coat. In two-coat work, the first coat. In Scotland it is called straightening and in the USA browning: laying the second coat of coarse stuff over the first coat.

#### Gauge blocks

Wooden blocks fixed to the surface for guidance, so that the outer faces define the plane of the finished plaster surface.

#### Girth

The surface length of a moulding profile (which can be envisaged as the length of a piece string which would accommodate it) giving some indication of the amount of work and the cost involved in forming it.

#### Gypsum

Hydrated calcium sulphate, CaS04·2H20, found as a soft rock in Australia and elsewhere. If calcined it gives off water and produces the hemihydrate, plaster of Paris: CaS04·2H20 + heat = CaS04·½H20 + 1½H20.

If further calcined it gives off the remaining water to become anhydrous calcium sulphate:

2CaS04·½H20 + heat = CaS04 + ½H20.

#### Gypsum plaster, see Plaster, gypsum

#### Hair

Animal hair used to reinforce plasterwork, usually that of cattle, though texts often refer to horsehair.

Hard finish, see Setting

#### Hawk

A square of aluminium, or traditionally wood, about 
300 mm, with a handle at right angles from the back, 
and which is used to hold a limited quantity of plaster 
of mortar while applying it.

#### Hemihydrate plasters

Retarded plasters such as plaster of Paris, which set hard quickly, and are used for casting. Retarding agents are commonly added to slow setting times for application to large areas.

#### Horse

A running mould or a continuous member along which 
a running mould can be slid.

Howe’s Cement, see Keene’s Cement

Hydrated lime see Lime, hydrated

#### Hydraulic

Used of lime or cement to indicate a capacity to set and cure under water, and to resist erosion by water when used externally.

#### Keating’s cement

In 1846 John Keating obtained a British patent for what later became known as Parian cement (from a purported similarity to Parian marble), which was made in much the same way as Keene’s cement but that borax [sodium borate] was substituted for alum. The material was used in some prominent Australian buildings in the 1850s.

#### Keene’s cement

Anhydrous calcium sulphate plaster obtained by reburning hemihydrate plaster that has been soaked in a solution of alum. It was originally patented in England by J D Greenwood and R W Keene in about 1838. It was made by dissolving alum in water, and in this solution soaking gypsum in small lumps for three hours at 34oC, then letting these dry in the open for about eight days, calcining them at a dull red heat, and grinding and sifting them. If copperas [iron sulphate] was added to the alum solution the resultant plaster would have a fine cream or yellow colour. Keene’s cement sets rapidly and hard, and in Australia came to be much favoured for highly finished plasterwork—especially when it required a marble or other fine finish, or was used in arrises, skirtings or other areas subject to damage. By the end of the twentieth century 
an improved version, Howe’s Improved Keene’s Cement (or just Howe’s Cement) was available.

#### Key (bond)

The roughness of a surface which enables a subsequent layer to bond well to it, or the portion of the plaster which squeezes between laths and spreads slightly behind them, so that the surface plaster cannot fail unless the 
key is physically broken.

#### Keying, see scratching

#### Lath, lathing

Tradition lathing is an arrangement of parallel timber strips or laths [not ‘lathes’], typically about 7 x 32 mm, to provide a base for plastering, their spacing being about 10 mm or sufficient for the base coat to penetrate, spread behind, and form a key. Laths might be sawn or split, and in Australia split laths of local timber were often preferred as being stronger and providing a better bond than sawn laths, which were commonly of oregon and imported from North America.

#### Lath, metal

Metal fabric made by weaving wire or perforating sheet metal (usually mild steel) to create a good key, and used as a base for plaster in place of traditional wooden laths. Wire netting had been used for the purpose, but from about 1890 expanded metal, became popular in place of timber lathing, and subsequently other products such as Hanley’s Patent Corrugated Woven-Wire Lathing, ‘Jhimil’ Patent Metal Lath, Bostwick Patent Fireproof Metal Lath Patent Metal Lathing Sheets, and Helical Metal Lathing were introduced.

#### Lath hammer

A hand tool the head of which has a hammer head in one direction and an axe blade in the other, used for cutting and nailing laths as well as for general work such as cutting plugs and packing pieces.

#### Lime

A word used both for calcium oxide or quicklime (CaO), and for calcium hydroxide or hydrated lime (CaOH2). Quicklime, or unslaked lime, is a white caustic solid prepared by calcining calcium carbonate (in the form of limestone, marble, seashells or coral) to drive off the carbon dioxide. Quicklime is usually slaked, by the addition of water, to produce hydrated lime for use.

#### Lime, hydrated

Calcium hydroxide produced by slaking quicklime (calcium oxide) with water. The exact amount produces a dry powder, while an excess of water produces a putty. Dry hydrated lime is usually factory produced and sold in bags as ‘hydrated lime’.

#### Lime, hydraulic

Lime burnt from a limestone with a clay content sufficient to give the product hydraulic properties (or from a deliberate mixture of limestone and clay).

#### Lime putty

Slaked lime that has been matured in water and sieved to remove coarse particles and achieve a smooth consistency. It is normally used for finishing work. Also called Lime paste and Plasterer’s putty.

#### Lime, quick

The form of lime or CaO produced directly by burning limestone &c, which is corrosive and difficult to handle.

#### Lime, rock

Quicklime produced by calcining limestone.

#### Lime, slaked, see Lime, hydrated

Calcium hydroxide, Ca(OH)2, produced by adding the required quantity of quicklime to water in a chemical reaction giving off heat: Ca0 + H2O Ca(OH)2.

#### Lime wash

A whitewash based upon lime (as opposed to materials such as pipeclay), made according to various recipes, the simplest of which is lime and water. One example consisted of four parts of pounded lime, three of sand, two of pounded wood ashes, and one of ‘scoria of lime’, mixed well and diluted to brushing consistency.

#### Loam

Natural soil containing clay, which when mixed with water forms a plastic material for plastering. This was common in early Sydney mainly for internal work, and often a proportion of lime was added if available.

#### Martin’s cement

One Martin obtained a British patent in 1834 for the manufacture of an imitation marble or cement capable of receiving a high polish, and made by treating powdered chalk or gypsum first with a strong alkali, and then an acid, then in 1840 another patent for mixing the same materials in a solid state. The material was used similarly to Keene’s cement, but was not nearly so popular in Australia.

#### Masonry

Stone laid in courses with mortar joints: sometimes used also of brickwork.

#### Mortar, compo [composition]

A mixture with water of Portland cement, lime and sand, in any one of the following proportions by volume: 1:½:4½; 1:1:6; 1:2:9; or 1:3:12. For floating, it is typically three parts of sand to one part of lime and cement mixture. It is used on internal and external surfaces, is easier to spread than Portland cement mortar, and holds water better.

#### Mortar, lime

A mixture of lime, sand, and water, for floating, typically three parts of sand to one part of lime by volume. For pricking up laths, typically with a little more lime to increase the plasticity, and with cattle hair added.

#### Mortar, Portland cement

A mixture of Portland cement, sand, and water, for floating, varying according to the work from one to four parts of sand to one part of cement.

#### One-coat method

The application to a solid base (brick, concrete or terra cotta) of a single coat of Portland cement mortar or composition mortar, or of a sanded gypsum plaster. Used only where the background is sufficiently true and provides uniform suction.

#### Paint, acrylic

Coating material manufactured with acrylic resins as the main binder.

#### Paint, cement-based.

Paint base in dry powder form, containing Portland cement and other materials, which is mixed with water just before use. Also called Cement paint. Nowadays rarely used.

#### Paint, oil

A paint containing pigments to impart the required colour, white lead or a substitute material to provide body and to conceal the substrate, all of which is ground and mixed with a drying oil (usually linseed oil) as the basic medium, both binder and vehicle.

#### Paint, silicate

Paint based upon water glass, or sodium silicate, introduced in mid nineteenth century Britain by Frederick Ransome and Nicolaus Charles Szerelmey.

#### Papier mâché

A material formed of mashed scrap paper, which is moulded into ornamental forms, then baked and finished, and is lighter and less fragile than cast plaster. It is applied to cornices &c in place of plaster ornament, and may be indistinguishable at a distance.

#### Parian cement, see Keating’s cement

#### Plaster

A mixture of a binder such as lime (possibly combined with gypsum plaster or Portland cement) or Portland cement (but never gypsum plaster and Portland cement) with sand and water, in the form of a paste-like material which can be applied to the surfaces of walls and ceilings and which then sets to form a hard surface. When used externally usually lime-based and referred to as stucco.

#### Plaster, fibrous

Pre-formed work made of plaster of Paris reinforced with fibrous material and sometimes wooden laths. Soluble cutting oils or specially made creams are applied to the mould or surface against which the casting is made, to ensure that it is easily released while preserving a sharp and true profile [or else a gelatin mould is used. The term ‘fibrous plaster’ was used in an English patent of 1856 by the French modeller Léonard Alexandre Desachy, to describe plaster of Paris reinforced with canvas or stiffened with wooden pieces. Until the turn of the twentieth century, most fibrous plaster was similarly based upon canvas or other fabric, but already other types of reinforcement, such as silicate cotton, were being used in some versions. In the twentieth century, loose fibre has been more common (such as jute, sisal, hemp, flax, coir, teased-out old rope, or fibreglass). While originally used mainly for ornamental purposes, in the twentieth century it came to be widely used for plain sheets, and also as a finished surface in its own right rather than as the base for a setting coat. In purpose-made form, it may also include wood lath or metal angle reinforcement for additional stiffness. Also called Fibre-reinforced gypsum plaster.

#### Plaster, gypsum

Calcium sulphate hemihydrate powder (plaster of Paris), made from gypsum, with the addition of water and, if necessary, suitable retarders. This was not used on any extensive scale in Australia until about the time of World War I. Subsequently, the Victor plaster brand dominated the local market, apparently connected in some way with the American Victor Plaster made by the Keystone Plaster Company of Philadelphia, but manufactured from South Australian raw material. Also the slower setting anhydrous calcium sulphate, generally with the addition of accelerators such as Keene’s cement.

#### Plaster coats, see dash, finishing, scratch, setting, skimming &c.

#### Plaster of Paris

Calcium sulphate hemihydrate produced by calcining gypsum, and used in setting coats for internal surfaces, running mouldings, making moulds and casts, and the manufacture of fibrous plaster.

#### Plate, muffle, see running mould

#### Pressed cement

A rather dry mixture of Portland cement and aggregate pressed or rammed into a mould, to create an architectural feature.

#### Pricking up

The London term for scratch coating or the application of a thin surface of mortar to lathing or other substrate material to provide a key for the first layer of plastering, otherwise first coating.

#### Putty coat, see setting

#### Render

Originally the first coat laid onto a brick, stone or concrete wall, such as the first coat in a three-coat plastering system. In modern usage it includes the application of any external finish applied by trowel, including one-coat work in sand and Portland cement.

#### Retarder

A substance used to extend the setting time, such as glue, dextrin or cream of tartar.

#### Roche lime

Rock lime in lump form after burning.

#### Roughcast

An external finish created by throwing onto a wall or other surface a mixture to creamy consistency of gravel, crushed stone toppings or pebbles, with sand and cement, used while in the plastic state. See also pebbledash.

#### Running mould

An implement for forming mouldings by passing it along or over soft plaster, and usually consisting of three main parts, a slipper, a stock and a plate. The slipper is a flat timber plate forming the base of the mould, usually in a horizontal plane. In forming a cornice, one edge of the slipper slides along and is guided by a running rule fixed to wall surface. At right angles on top of the slipper is the wooden stock, of approximately the profile to be formed. Its role is to support the plate fixed on one side of it. The plate establishes the exact finished profile, and is made of zinc, copper, brass, muntz metal or galvanized iron. Commonly the core of the moulding will have been established first, about 5 mm behind the finished surface, by placing an appropriately sized muffle plate over the mould.

#### Scagliola

A form of artificial marble invented in Italy by Guido Sassi in about 1615, and first used in England at the Pantheon, Oxford Street, London, of 1772. Plaster of Paris was sieved and mixed with Flanders glue, isinglass and other materials, and then with the required colour. The various shades were mixed in separate batches, then combined together on the surface to create a marbled effect, and the finished work was smoothed off and highly polished. Later used fine gypsum plaster mixed with cement, pigments and marble or stone chips, and finished with a high polish after it had hardened. It was quite widely used in Australia until at least the 1930s.

#### Scoring, see Scratching

#### Scratch coat

Preparatory layer of mortar or render applied to walls or floors to improve the bonding of a subsequent layer, generally used where one layer of excessive thickness would provide insufficient bond. The surface is left ‘scratched’ to allow a key for the next coat. See also Pricking up.

#### Scratching

Or scoring or keying: scoring the partially hardened coat of plaster of the first coat with a toothed wood or iron scratcher to create a key for the next coat.

#### Screeds

On a wall, dots of plastering material brought to the correct level, as guides for the subsequent flanking work. At the base of the wall, wood grounds provided for fixing skirtings may be used instead. On a floor, usually bands of mortar laid to establish the correct thickness and slope for the layer of mortar that is to be subsequently filled in, but occasionally timber strips for the same purpose.

#### Scrim

Open-meshed jute cloth (or other coarse open fabric, such as hessian, sisal or hemp) used for reinforcing fibrous plaster, and in the past to reinforce the mortar or to strengthen joints in plasterwork generally.

#### Second coating, see Floating

#### Setting, Setting coat

Steel trowelled finishing coat in plastering, 2 to 3 mm thick, of lime putty and/or plaster of Paris. In Scotland, finishing; in the USA hard finish or putty coat: laying and finishing the final coat on the second or floating coat.

#### Shell lime

Lime manufactured by burning shells, which were obtainable in quantity along much of the Australian coastline, particularly in the form of Aboriginal middens. The material was extensively used in Sydney and other locations where limestone was not obtainable.

#### Skimming, skim coat

The application of fast-setting stuff with a trowel as thinly as possible over the floated surface to whiten it (and not designed to modify the existing profile). Fine white sand may be added, and it may be polished to a glazed finish with a sand trowel. Sometimes regarded as an inferior form of setting.

#### Slipper, see running mould

#### Stock, see running mould

#### Stopping, Stopping-up

The filling of blemishes, joints and nail holes, commonly with neat plaster, or plaster and putty, to bring them to an even surface prior to painting.

Straightening, see Floating

#### Stucco

An external lime or cement-based rendered surface, which is in nearly always implicitly or explicitly an imitation of stone. Today the word is occasionally used in Australia for cement surfaces, but ‘cement’ or if applicable ‘cement render’ are better for this. It is also misused for various textured finishes.

The word stucco dates from the Italian Renaissance, for a material principally but not solely for internal modelling, referred to as stuccatura, or stucco duro, and commonly containing marble dust. It has also been used imprecisely by historical writers of any form of plastering in the ancient world (see albarium opus). The usage for exterior surfacing derives ultimately from Palladio, for whom it was still a smooth finish plaster of slaked lime, gypsum and pulverised white marble, used for decorative building parts such as cornices, mouldings or other ornamentation. This was modified by the introduction of so-called Roman cement in late eighteenth century Britain, and subsequently in Australia. This, and still more Portland cement, tends to be referred to as ‘cement’ or, in specific cases as ‘artificial stone’. In the nineteenth century the term ‘stucco’ was not commonly used of Portland cement surfaces or of any heavily moulded work.

#### Stucco wash

A proprietary material for surfacing and colouring stucco, usually containing colourants and one or more of cement, plaster of Paris, or size. Johns’s Patent Stucco Wash, basically stone-coloured, was available in Britain in the 1850s, and in Australia by 1859.

#### Tallow

Rendered animal fat, sometimes added as a plasticiser 
to stucco.

#### Textured finishes

Finishes other than the orthodox floated or trowelled types, usually executed in Portland cement.

#### Three-coat method

The application of three coats, a bond coat, a floating (or flanking) coat, and a finishing coat. usually on laths or rough stonework. The first pricking-up coat is mortar with hair to hold it together, approximately straightened with a laying trowel, and subsequently finished as for the two-coat method.

#### Trowel, gauging

A tapered steel blade, with a handle at the end, used for gauging material and applying it to mouldings.

#### Trowel, laying

A rectangular steel blade, with a handle at the back, used for applying and spreading plaster and for finishing some types of work.

#### Trowel, margin

A small rectangular steel blade, with a handle at the end, used for trowelling in margins or panels.

#### Two-coat method

The application of two coats, a bond coat and a flanking coat, to give a finer and more uniform finish than the one-coat method, using lime plaster, gypsum plaster, or Portland cement. The first coat is applied, usually from the bottom up, plumbed, brought to a straight face, and if necessary scratched. The second coat is generally applied from the top down and is very thin, perhaps 7 mm in the case of Portland cement mortar. Used where the background is not sufficiently true or does not provide uniform suction, or where a more highly finished surface free from grinning or crazing is required.

#### Vermiculation

A finish intended to suggest that is worm-eaten, used especially on quoins, keystones, &c. The surface is created true, then an irregular network of bands drawn onto it, then the surface between the bands is picked out with a small tool to leave the bands standing free, or, almost the reverse, shallow, irregular, and winding or wavy channels or markings resembling worm tracks are pressed or incised into the surface.

#### Wattle and daub

A primitive building method consisting of loam or lime plaster laid on interlaced flexible twigs like basketwork: in Britain commonly hazel, but in Australia commonly acacia [hence called wattle].

Bibliography

overseas primary sources

plastering texts

overseas secondary sources

materials science

conservation principles

Australian primary sources

Australian specifications

Australian secondary sources

conservation studies

## Overseas primary sources

——, Sweet’s Architectural Catalogue (New York 1922).

H Aitken, Stone, preserving; cements; plasters; mortars Patent 11,209 (London 1891).

Ashton & Green, Limited, Ashton & Green, Limited, Slate, Tile, Brick, Cement, Marble, and Iron Manufacturers and Merchants (London 1887).

William Atkinson, Views of Picturesque Cottages, with Plans: selected from a collection of drawings taken in different parts of England, and intended as hints for the improvement of village scenery (London 1805).

P B Butler, Portland Cement, its Manufacture, Testing and Use (London 1899).

A J Downing, The Architecture of Country Houses (New York 1850).

Oscar Faber & H L Childe [eds], The Concrete Year Book 1949 (London 1949)

F R Farrow, Specifications for Building Works (London 1898).

Q A Gillmore, A Practical Treatise on Limes Hydraulic Cements, and Mortars (8th ed, New York 1886).

Joseph Gwilt [ed Wyatt Papworth], An Encyclopaedia of Architecture: Historical, Theoretical and Practical (London 1881 [1842]); also (London 1912 [1842]).

P N Hasluck, Cassell’s House Decoration: A Practical Guide to Painters’ and Decorators’ Work (London 1910).

Bryan Higgins, Experiments and Observations [on] Calcareous Cements (London 1780).

C Kersten [translated N C Ricker], Der Eisonbetonbau (2 vols in 1, Urbana [Illinois] 1916 [from the 10th German edition, 1915, originally 1906] [typescript in the Ricker Library, University of Illinois at Urbana-Champaign].

F W Laxton, Laxton’s Builder’s Price Book for 1863 (43rd ed, London 1863).

John Leaning, Building Specifications (London 1901).

London, Great Exhibition of the Works of Industry of all Nations, 1851, Official Descriptive and Illustrated Catalogue (3 vols, London 1851).

J C Loudon, Encyclopædia of Cottage, Farm and Villa Architecture (London 1846 [1833]).

F W Macey, Specifications in Detail (3rd ed, London 1922).

G A T Middleton [ed], Modern Buildings (6 vols, London, no date [c 1910]).

G Mitchell, Building Construction (12th ed, London 1929).

Richard Neve, The City and Countrey Purchaser, and Builders’ Dictionary: or, Compleat Builders Guide (2nd ed, London1726 [1703])

Wyatt Papworth [ed], The Dictionary of Architecture (6 vols, London 1853-92).

N E Pelouze, Art de Fabriquer en Pierre Factice très-dure et susceptible de recevoir le poli, &c (Paris 1829).

C W Pasley, Observations on Limes, Calcareous Cements, &c (London 1838).

A W N Pugin, The True Principles of Pointed or Christian Architecture (London 1853 [1841]).

J T Rea, How to Estimate (London 1904).

J Singleton-Green, ‘Cements and Concrete’, in F E Drury et al [eds], Architects’, Builders’ and Civil Engineers’ Technical Catalogue (London 1946), pp 34–43.

G L Sutcliffe, The Principles and Practice of Modern House Construction (new ed, 6 vols, London 1909).

Andrew Ure, Dictionary of Arts, Manufactures and Mines (London 1839).

Giorgio Vasari [translated L S Maclehose & edited G B Brown], Vasari on Technique [being the first part of his Lives of the Artists] (New York 1960 [London 1907 (1550)]).

W Verrall et al, The Modern Plasterer (2 vols, London, no date [c 1930]).

L J Vicat [translated J T Smith], A Practical and Scientific Treatise on Calcareous Mortars and Cements (London 1837).

Marcus Vitruvius Pollio [‘Vitruvius’] [translated M H Morgan], The Ten Books on Architecture (New York 1960 [1916]). Also Joseph Gwilt’s translation (London 1867).

John Weale, Rudimentary Dictionary of Terms used in Architecture, &c (London 1860).

John Wood, A Series of Plans for Cottages or Habitations of the Labourer (London 1806 [?1781]).

Clyde Young [ed], Spons’ Architects’ and Builders’ Pocket Price Book 1935 (62nd ed, London 1935).

## Plastering texts

G P Bankart, The Art of the Plasterer (London1908).

Wilfred Kemp, The Practical Plasterer (London1893).

W S Lowndes & D K Boyd, Plastering and Stucco Work (2nd ed, Scranton [Pennsylvania] 1923 [1921]).

William Millar, Plastering Plain and Decorative (London 1897) [reprinted Shaftsbury, 2004] (also 3rd ed, London 1905).

J T Sawyer, Plastering,1951, [reprint Shaftsbury [Dorset] 2007).

W Verrall et al, The Modern Plasterer (2 vols, London, 
no date [c 1930]).

## Overseas secondary sources

A C Davis, A Hundred Years of Portland Cement (London 1924).

Roger Dixon & Stefan Muthesius, Victorian Architecture (London 1978).

Donald Ellsmore, ‘Nineteenth-Century Painted Decorations’ (2 Volumes, D Phil, University of York, 1993).

Claire Gapper, ‘What is Stucco? English Interpretations of an Italian Term’, Architectural History, XL11 (1999), pp 333-334.

S B Hamilton, ‘Building and Civil Engineering’, in Charles Singer et al [eds], A History of Technology, Volume IV: the Industrial Revolution c 1750 to c 1850 (Oxford 1975).

Eileen Harris, British Architectural Books and Writers 1556-1785 (Cambridge 1990.

Hermione Hobhouse & Ann Saunders [eds], Good and Proper Materials; the Fabric of London Since the Great Fire (London 1989).

Lawrence Hurst, ‘The Properties and Uses of Roman Cement’, Construction History, XVIII (2002).

Sara Wermiel, ‘The Development of Fireproof Construction’, Construction History, IX (1993).

John Wilson, AA Book of New Zealand Historic Places (Auckland 1984).

Brian Kearney, Architecture in Natal (Cape Town1973).

R B Lewcock, Early Nineteenth Century Architecture in South Africa (Cape Town 1963).

G C L Lynch, ‘The Colour Washing and Pencilling of Historic English Brickwork’, Journal of Architectural Conservation, XII, 2 (July 2006).

Donald Pilcher, The Regency Style 1800 to 1830 (London 1947).

Thomas Ritchie, Canada Builds 1867-1967 (Toronto 1967). Russell, Watts & Pritchard, ‘Specifications for ... Dwelling houses ... at Elwood… for Joseph Docker’, 13 December 1854, Docker papers, State Library of Victoria.

Witold Rybczynski, The Perfect House (New York 2002).

A W Skempton, ‘Portland Cements, 1843-1887’, in Frank Newby [ed], Early Reinforced Concrete (Aldershot [Hampshire] 2001).

Samuel Smiles, Lives of the Engineers (3 vols, London 1862).

John Stacpoole, William Mason (Auckland 1971).

John Summerson, Georgian London (London 1945).

Geoffrey Thornton, Cast in Concrete (Auckland 1996).

G C Thornton, ‘Early Concrete Structures in New Zealand’, Fourth National Conference on Engineering Heritage 1988, Sydney 5-8 December 1988, Preprint of Papers (Barton [ACT] 1988).

G C Thornton, New Zealand’s Industrial Heritage (Wellington 1982).

John Weiler, ‘Colonial Connections: Royal Engineers and Building Technology Transfer in the Nineteenth Century’, Construction History, XII (1996).

Manfred Wundram & Thomas Pape, Andrea Palladio (Köln, no date).

## Materials science

G Allen et al, Hydraulic Lime Mortar for Stone, Brick 
and Block Masonry (Shaftesbury [Dorset] 2003).

John Ashurst, Mortars, Plasters and Renders in Conservation (London 1983).

John Ashurst & Nicola Ashurst, Practical Building Conservation (5 vols Aldershot [Hampshire] 1988): vol 3, Mortars, Plasters and Renders.

Nicola Ashurst, Cleaning Historic Building, Vol 1 (London 1994).

L Burgio, ‘Dating Alhambra Stuccos’ V& A Conservation Journal Online, Spring 2005, 49, <www.vam.ac.uk/res_cons/conservation/journal/number_49/alhambra_stuccoes/index.html>, accessed 23 May 2009

E B Cliver, ‘Tests for the Analysis of Mortar Samples’, APT Bulletin, VI, 1 (1974) pp 68–73.

Beatriz del Cueto, ‘A Manual on Conservation Methodology for Historic Buildings and Structures. P Puerto Rico and the Virgin Islands’ (1997) [Caribbean Heritage Inc, Guaynabo, Puerto Rico: reproduction supplied by the US National Parks Service 1997].

Barrie Cooper, Westlegate Pty Ltd Product Information (Sydney 2008).

Peter Ellis, ‘The Analysis of Mortar: the Past 20 Years’, Historic Churches (2002), accessed via www.buildingconservation.com, 24 April 2009.

A M Forster, How Hydraulic Lime Binders Work: hydraulicity for beginners and the hydraulic lime family (Edinburgh 2004).

R J Gettens & G L Stout, Painting Materials: a Short Encyclopaedia (New York 1966).

C M Grossi & Peter Brimblecombe, ‘The White Tower and the Perception of Blackening’, Journal of Architectural Conservation, 11, 3 (November 2005).

C Herm, ‘Kalkfarbetechniken: eine Literaturstudie’ [Limewash techniques: a literature review] Arbeitsblätter für Restauratoren, 33, no 2, Gruppe 7 (2000), pp 153-168 [German with English summary]: abstract accessed 13 April 2009.

P C Hewlett, Lea’s Chemistry of Cement and Concrete (4th ed, Oxford 1988).

Elizabeth Hirst, ‘Limewash and Distempers’, The Building Conservation Directory 2002

<www.buildingconservation.com/articles/lwdistempers/lwdistempers.htm>, accessed 15 December 2008.

Getty Conservation Institute & International Institute for Conservation of Historic and Artistic Works, Art and Archaeology Technical Abstracts [AATA Online]: <http://aata.getty.edu/NPS/>

Historic Scotland, External Lime Coatings on Traditional Buildings [Technical Advice Note 15] (Edinburgh 2001).

Historic Scotland, Preparation and use of Lime Mortars [Technical Advice Note 1] Historic Scotland, (revised ed, Edinburgh 2003).

S Holmes & M Wingate, Building with Lime: a practical introduction (revised ed, London 2002).

Paul Holper & Julie Noonan, Urban and Regional Air Pollution Information Sheet (2000) [CSIRO Research]

<www.dar.csiro.au/information/urbanpollution.html> accessed 12 December 2008.

D Hughes, S Swann, & A Gardner, ‘Roman Cement, Part One’, Journal of Architectural Conservation, XIII, 1 (March 2007), & ‘Part Two’, XIII, 3 (November 2007), pp 41–58.

J Hughes & J Válek, Mortars in Historic Buildings: a review of the Conservation, Technical and Scientific Literature (Edinburgh 2003).

Institution of Engineering and Technology, ‘Colour Vision Defects’ (2007), <www.theiet.org/factfiles/health/colourvisiondefects.cfm?type=pdf>, accessed 9 May 2009

International Centre for the Study of the Preservation and Restoration of Cultural Property [ICCROM] Mortars, Cements and Grouts used in the Conservation of Historic Buildings. [proceedings of an ICCROM symposium, 
3–6 November 1981] (Rome 1981).

Ioan Istudor, Anca Dina˘ , Geanina Ros˛u, Doina S˛ecla˘ man and Gheorghe Niculescu, ‘An Alteration Phenomenon of Cinnabar Red Pigment in the Mural Paintings from Sucevita’, e-conservation, Issue 2 (2007), pp 602
<www.e-conservationline.com/content/view/587>, accessed 23 May 2009.

S M Jackson, Tye Botting & Mary Striegel, ‘Durability of Traditional and Modified Limewashes’, APT Bulletin, XXXVIII, 2-3 (2007), pp19-28.

J Jacob & N R Weiss, ‘Laboratory Measurement of Water Vapour Transmission rates of Masonry Mortars and Paints’, APT Bulletin, XXI, 3-4 (1989), pp 62–70.

M Jonsson & E B Cliver, ‘Coloring Historic Stucco: the Revival of a Past Technique in San Juan, Puerto Rico’, APT Bulletin, XXXIII, 4 (2002), pp 31–6.

Sheldon Keck, ‘Some Picture Cleaning Controversies: Past and present’, Journal of the American Institute for Conservation, 23, 2, (1984), article 1, pp 73 to 87,
<http://aic.stanford.edu/jaic/articles/jaic23-02-001.html>, accessed 28 November 2008.

D S Krotzer, ‘Architectural finishes: Research and Analysis’ [Practice Points no 06]. APT Bulletin, XXIX, 2-3 (2008), pp 1–6.

D S Krotzer and J J Walsh, ‘Analyzing Mortars and Stuccos at the College of Charleston: A Comprehensive Approach’, APT Bulletin, XL, 1 (2009), pp 41–8.

M Lawrence, P Walker & D D’Ayala, ‘Non-Hydraulic Lime Mortars’, Journal of Architectural Conservation, XII, 1 (March 2006).

Frank Matero, ‘Loss, Compensation and Authenticity in Architectural Conservation’, Journal of Architectural Conservation,1,12 (March 2006).

F G Matero & J C Snodgrass, ‘Understanding Regional Painting Traditions: The New Orleans Exterior Finishes Study’, APT Bulletin, XXIV, 1/2 (1992), pp 36–52.

Museum of Fine Arts, Boston: Conservation and Art Material Encyclopedia Online [CAMEO]: <http://cameo.mfa.org/>.

Vratislav Nejedlý, [A couple of comments to the surface finish of the sculptural works of art installed in the exterior] Zprávy Památkové Péc ˇ e, 63, no 2 (2003), pp110–117 [Czech with English summary]: abstract accessed 
17 March 2008.

Alan Phenix, ‘Solvent Abuse: some observations on the safe use of Solvents in the Cleaning of Painted and Decorated Surfaces’,

<www.buildingconservation.com/articles/solvent/solvent.htm>, accessed 15 December 2008.

Nigel Seeley, ‘The Use of Lead Paint for Historic Buildings’, Journal of Architectural Conservation, Vol 5, 
2 (July 1999), pp 24–42.

Standards Association of Australia, Lime and Limestones, Part 1: Limes for building, AS:1672.10-1997 
(Sydney 1997).

Standards Association of Australia, Portland and Blended Cements, AS:3972-1997 (Sydney 1997).

Standards Association of Australia, Masonry cement, AS:1316-2003 (Sydney 2003).

J Stewart & J Moore, ‘Chemical Techniques of Historic Mortar Analysis’, APT Bulletin, XIV,1(1982) pp11–16.

J H Stoner, ‘The Impact of Research on the Lining and Cleaning of Easel Paintings’, Journal of the American Institute for Conservation, 1994, 33, 2 (1994), article 5, pp 131–140:

<http://aic.stanford.edu/jaic/articles/jaic33-02-005.html>, accessed 28 November 2008.

G T Suter, M L Thomson & L Fontaine, ‘Mortar Study of mechanical properties for the repointing of the Canadian Parliament buildings’, APT Bulletin, XXIX, 2 (1998) pp 51–8.

J M Teutonico et al, ‘The Smeaton Project: Factors Affecting the Properties of Lime-based Mortars’ APT Bulletin, XXV, 3-4 (1994), pp 32–49.

E T Thompson, A Laboratory Manual of Semi-Micro Inorganic Qualitative Analysis (London 1957).

G Torraca, Porous Building Materials: Materials Science for Architectural Conservation (3rd ed, Rome 1988).

A I Vogel, A Text Book of Qualitative Chemical Analysis (London 1957).

A I Vogel, Elementary Practical Organic Chemistry, 2. Qualitative Organic Analysis (London 1962).

David Young, Salt Attack and Rising Damp: a guide to salt damp in historic and older buildings (Sydney 2008).

## Conservation principles

Australia ICOMOS, The Burra Charter: the Australia ICOMOS Charter for Places of Cultural Significance, 1999 (Melbourne 1999).

Cesare Brandi, Theory of Restoration (Rome 2005 [1963])

I C Bristow, ‘Exterior Renders Designed to Imitate Stone: A Review’, Transactions of the Association for Studies in the Conservation of Historic Buildings, 22 (1977), p 27.

E Burden, Illustrated Dictionary of Architectural Preservation (New York 2003).

J Earl, Building Conservation Philosophy (3rd ed, Shaftsbury [Dorset] 2003 [c 1996]).

International Council on Monuments and Sites, The Nara Document on Authenticity (Nara 1994).

## Australian primary sources

——, Australian Settler’s Handbook: being Practical Hints for the Unexperienced on the most simple and profitable method of cultivating their land: being the result of many years experience in the Colony (Sydney 1861).

——, To Architects, Contractors, &c [trade circular, apparently Melbourne c 1883], in John Beswicke papers, copy kindly supplied by Mr Ken Bethell.

——, ‘To Mix Lime Wash’, Australasian Decorator and Painter, 1 May 1906, p 160.

James Atkinson, An Account of the State of Agriculture and Grazing in New South Wales (London 1826).

Australia, Department of Labour and National Service, Industrial Training Division, Plastering [Technical Publication No 12] (Melbourne 1947 [1946]).

David Burn, A Picture of Van Diemen’s Land (Hobart 1973 [1840–41]).

Michael Cannon [ed], Historical Records of Victoria, III (Melbourne 1984).

David Collins [ed Maria Collins, James Collier], An Account of the English Colony in New South Wales (Christchurch 1910 [1798 & 1802; 1804]).

Peter Cunningham, Two Years in New South Wales (2nd ed, 2 vols, London 1827).

Harriet Daly, Digging, Squatting, and Pioneering Life in the Northern Territory of South Australia (London 1887).

Charles Griffith, The Present State and Prospects of the Port Phillip District of New South Wales (Dublin 1845).

Robert Haddon, Australian Architecture: a technical manual for all those engaged in architectural and building work (Melbourne, no date [c 1908]).

T H James, Six Months in South Australia (London 1838).

G F G Mackey, Gregory’s Modern Building Practice in Australia (Sydney, no date [late 1940s]).

James Moore & Sons Pty. Ltd., Price List 96 August 1913 (Melbourne 1913).

A W Johnson, ‘Goodlet and Smith Ltd. Brickworks, Roofing Tile Manufacturers, Cement Works & “Benedict Stone” Manufacturers. Granville, N.S.W. (1886-1982)’ (3 vols, major project for Historical Archaeology II [University of Sydney] 1982).

Charles Mayes, Victorian Contractors’ and Builders’ Price-Book (Melbourne 1859); also (2nd ed, Melbourne 1862; 3rd ed, Melbourne 1877; 4th ed, Melbourne 1883; and 5th ed, Melbourne 1886).

Melbourne, Intercolonial Exhibition of Australasia, Official Record (Melbourne 1867).

Melbourne International Exhibition, 1880-1881, Official Record (Melbourne 1882), pp 82–94.

[Janet] Millett, An Australian Parsonage (London 1872).

T L Mitchell, ‘Sir Thomas L Mitchell Memoranda Book, 1827-1829’, Mitchell Library, manuscript ML C38, reel CY 1992.

James Nangle, Australian Building Practice, Part 1 (Sydney 1900).

James Nangle, Australian Building Practice (2nd ed, Sydney 1911); also (4th ed, Sydney 1944).

New South Wales Government Gazette, 1833.

New South Wales, Public Works Department, Annual Report (Sydney 1890).

Arthur Phillip, The Voyage of Governor Phillip to Botany Bay (London 1789).

Pittsburgh Plate Glass Company, Architectural Specifications (Milwaukee [Wisconsin] 1935).

W L Richardson [ed], Ramsay’s Architectural Catalogue (Melbourne 1931).

Watson Sharp, Australian Methods of Building Construction (Sydney 1946).

E G Stone, Reinforced Concrete in Australia (no place, 1920).

Sydney, International Exhibition 1879, Official Catalogue 
of the British Section (London 1879).

Terry & Oakden, What to Build and How to Build It (Melbourne 1885).

[James Tucker] ‘Giacomo de Rosenberg’ [ed Colin Roderick], Ralph Rashleigh, or the Life of an Exile (Sydney 1952 [1929]).

C J Virgo, Australasian Building Knowledge (Volume 2) (Brisbane 1955).

F W Ware & W L Richardson [eds], Ramsay’s Architectural and Engineering Catalogue (Melbourne 1949); also ((Melbourne 1954).

W C Wentworth, Statistical, Historical and Political Description of the Colony of New South Wales (London 1819).

John White, Journal of a Voyage to New South Wales (London 1790).

Australian specifications

Beswicke & Hutchins, ‘Specification of Works to be done in painting “Altyre” Barkers Road Kew for James E Cumming Esq.’ (Melbourne 1889) [single page], Ken Bethell collection.

L J Flannagan, ‘Specification… for Shop Additions in Heidelberg Road, Ivanhoe’, July 1907, p 18, Melbourne University Architectural Collection, State Library of Victoria.

Hyndman & Bates, ‘Specification, &c, Villa Residence Tank +c / Camberwell / Arthur J Fuller Esq / Normanby Chambers Chancery Lane’ (Melbourne 1990).

W S Law, ‘Specifications of Residence Drummond St. Carlton for Mrs. L. Abrahams’ (Melbourne 1891).

New South Wales, ‘Schedule of Contract. Plasterer’s Work’. (Sydney 1836). Mitchell Library.

New South Wales, ‘Schedule of Contract. Plasterer’s Work’. (Sydney 1864). Mitchell Library.

Reed & Barnes, ‘Melbourne Town Hall Specification, 1868’. City of Melbourne Archives.

Reed & Barnes, ‘Specification of Work to be done and Materials to be used in the Erection of Banking Premises at “Kooringa S.A.” for the Bank of Australasia’ (Melbourne 1878), State Library of Victoria.

Reed, Henderson & Smart, ‘Specification of Work to be done ... New Premises for the Metropolitan Gas Coy.’ (Melbourne 1890), State Library of Victoria.

W W Wardell, ‘English Scottish & Australian Chartered Bank Melbourne / W.W. Wardell Aust’ [specification] (Melbourne [1883]). ANZ Bank Archives.

Australian secondary sources

James Broadbent, The Australian Colonial House (Sydney 1997).

Philip Cox, Building Norfolk Island (Melbourne 1971).

Peter Cuffley, Australian Houses of the ‘20’s and ‘30’s (Fitzroy [Victoria] 1989)

D A Cumming & G C Moxham, They Built South Australia: Engineers, Technicians, Manufacturers, Contractors and their Work (Adelaide 1986).

Hanut Dodd, ‘Lime and Victorian Buildings’ (MPD, University of Melbourne, 1997).

Barrie Dyster, Servant and Master (Kensington [NSW] 1989).

Ian Evans, The Australian Home (Sydney 1983).

R J Fergusson, Rottnest Island: History and Architecture (Nedlands [Western Australia] 1979).

Warwick Gemmell, And So We Graft from Six to Six 
(North Ryde [New South Wales] 1986.

Jane Harrington, An Archaeological and Historical Overview of Limeburning in Victoria (Melbourne 2000).

Morton Herman, The Early Australian Architects and their Work (Sydney 1954).

Robert Irving, ‘The First Australian Architecture’ (March, University of New South Wales 1975).

Dennis Jeans, ‘The Building Industry: Materials and Styles’, in Judy Birmingham, Dennis Jeans & Ian Jack, Industrial Archaeology in Australia: Rural Industry (Richmond [Victoria])1983.

E & R Jensen, Colonial Architecture in South Australia (Adelaide 1980).

Sarah Johnstone, ‘Australian Cement Industry’ (typescript article for what was said to be a forthcoming publication of the Institution of Engineers, Sydney 1987).

Clem Lack, Newstead House (Brisbane, no date).

Miles Lewis, ‘Tradition and Innovation in Victorian Building 1801 - 1865’ (3 vols, PhD, University of Melbourne, 1972).

Philip McKay, ‘The History of the Cement Industry to 1939; an essay’ (mimeographed report for the Cement & Concrete Association of Australia, no place, 1977).

D C Markey, ‘Pioneer Perth’, in J Gentilli [ed] Western Landscapes (Nedlands [Western Australia]1872).

C J Mitchell, Hunter’s River (Sydney 1973).

Michael Pearson, ‘Archaeological Interpretation and Ethnographic Analogy: the lime industry in Western Australia’, Archaeology in Oceania, XXI, 1 (April 1986).

D W Penn, How Firm the Foundation: a Historical Survey of an Independent Venture that Founded the Portland Cement Industry in Australia (Sydney 1977).

E G Robertson, Early Buildings of Southern Tasmania 
(2 vols, Melbourne 1970).

J G Steel, Brisbane Town in Convict Days 1824–1842 
(St Lucia [Queensland] 1975).

C R Stone & Pamela Tyson, Old Hobart Town (Lilydale [Victoria] 1978).

Donald Watson & Judith McKay, Queensland Architects 
of the 19th Century (Brisbane 1994).

H P Wellings, Benjamin Boyd in Australia (1842-1849) (Bega [New South Wales], no date).

conservation studies

Allom Lovell & Associates, ‘Bontharambo Wangaratta, Conservation Management Plan’ [prepared for Heritage Victoria] (Melbourne 2001).

Allom Lovell Marquis-Kyle, ‘St. Helena Island Measurement and Assessment of Structures Component Reports’ (Brisbane 1989).

P J F Coutts, Corinella: a Forgotten Episode in Victorian History [Records of the Victorian Archaeological Survey No. 15] (Melbourne 1983).

Heather Godfrey et al, ‘Conservation Management Plan: “Romla and Frelin”. 86 and 87 Darlington Road, Darlington, Sydney’ (Sydney 2008).

Howard Tanner and Associates, Architects, ‘Tempe House Restoration and Conservation (Sydney 2004).

Hughes Trueman Pty Ltd [Simon Wiltshier], ‘Bontharambo at Wangaratta, Structural Condition Report’ (Sydney 2004).

Hughes Trueman Ludlow, Evans Shire Council Heritage Study (2 vols, no place, 1987).

Lindy Scripps et al, Willow Court Conservation Management Plan Stage C(i) The Barracks and Bronte 
[for Derwent Valley Council] (Hobart 2006).

Endnotes

1	Bankart,  pp 4–5 ff.

2	Vitruvius, Ten Books on Architecture, pp 204–214.

3	Vitruvius, Ten Books on Architecture, pp 213–4; Papworth, Dictionary of Architecture, sv Stucco.

4	Verrall, The Modern Plasterer, I, p 10.

5	Bankart, Art of the Plasterer, p 7.

6	Papworth, Dictionary of Architecture, sv Stucco.

7	Bankart, Art of the Plasterer, pp 22–36.

8	Vasari, On Technique, pp 170–2.

9	Verrall, The Modern Plasterer, I, p 20, quoting ‘a Marciano manuscript’ in the Library of St Mark, Venice.

10	This was used at Palladio’s villa ‘La Malcontenta’: Rybczynski, The Perfect House, pp 93-4.

11	Rybczynski, The Perfect House, pp 4, 60, 94.

12	Vasari, On Technique, pp 171, 183. This is a translation, but Millar, Plastering Plain and Decorative, p 107, quotes him as using the word stucchi.

13	Bankart, Art of the Plasterer, p 45.

14	Verrall, The Modern Plasterer, I, p 27.

15	Papworth, Dictionary of Architecture, sv Stucco, quoting Wren, Parentalia, folio 1750, p 277.

16	Verrall, The Modern Plasterer, I, p 29.

17	Millar, Plastering Plain and Decorative, pp 109–110.

18	Neve, quoted in Papworth, Dictionary of Architecture, sv Stucco; I have been unable to locate the reference in Neve

19	Millar, Plastering Plain and Decorative, p 107; Verrall, The Modern Plasterer, I, p 34.

20	Summerson, Georgian London, p 111.

21	Summerson, Georgian London, p 111.

22	Verrall, Modern Plasterer, I, p 33.

23	Atkinson, Views of Picturesque Cottages, p 13.

24	Atkinson, Views of Picturesque Cottages, p 13.

25	Atkinson, Views of Picturesque Cottages, p 19.

26	Neve, quoted in Papworth, Dictionary of Architecture, sv Stucco; I have been unable to locate the reference in Neve

27	Millar, Plastering Plain and Decorative, pp 109–110.

28	Millar, Plastering Plain and Decorative, p 186.

29	Millar, Plastering Plain and Decorative, p 188.

30	Verrall, The Modern Plasterer, II, pp 143–7.

31	Verrall, The Modern Plasterer, II, p 20.

32	Lowndes & Boyd, Plastering and Stucco Work, pp 63, 70.

33	Wood, Cottages of the Labourer, p 7.

34	Smiles, Lives of the Engineers, II, p 37.

35	Higgins, Experiments on Calcareous Cement, passim, especially pp 182 ff.

36	British patent no 1207, to Bryan Higgins, 23 April 1779, reproduced in Davis, A Hundred Years of Portland Cement, pp 227-231.

37	Higgins, Experiments on Calcareous Cements (London 1780), passim, especially pp 182 ff.

38	Summerson, Georgian London, p 111.

39	A-J Loriot, Mémoire sur une Découverte dans l’Art de Bâtir, - la Méthode de Composer un Ciment ou Mortier Propre à une Infinité d’Ouvrage, tant pour la Construction que pour la Décoration (Paris 1774) ref Papworth, Dictionary of Architecture, sv ‘(Antoine Joseph) Loriot’.

40	Harris, British Architectural Books and Writers, p 301.

41	Papworth, Dictionary of Architecture, sv ‘(Antoine Joseph) Loriot’. Harris interprets it as a single recipe using both quick and slaked lime.

42	Higgins, Experiments on Calcareous Cements, pp 228-9.

43	British patent no 2120 to James Parker, 27 July 1796, reproduced in Davis, A Hundred Years of Portland Cement, pp 233-5. See also Repertory of Arts, second series, XVIII, 108 (May 1811), pp 330-332.

44	Gillmore, Practical Treatise on Limes &c, p 62.

45	Hurst, ‘ Roman Cement’, p 27: he incorrectly gives ‘Mulgrove’s’ for ‘Mulgrave’.

46	Pugin, True Principles (1853), p 48.

47	A C Davis, A Hundred Years of Portland Cement (London 1924), pp 26–7.

48	Ure, Dictionary of Arts, sv Mortar.

49	Skempton, ‘Portland Cements’, p 131.

50	Pelouze, Pierre Factice, pp 32-40

51	Skempton, ‘Portland Cements’, p 75.

52	British patent no 4,679 to James Frost, 10 August 1822, reproduced in Davis, A Hundred Years, pp 234–5. See also Pasley, Observations on Cements, 
appendix pp 13–16.

53	Pasley, Observations on Cements, appendix pp 13–16.

54	Skempton, ‘Portland Cements’, p 75.

55	Davis, A Hundred Years, p x.

56	Pasley, Observations on Cements, pp 13–16.

57	Great Exhibition, Official Catalogue, I, p 134; also an illustration of their test beam, facing p 104. See also Davis, A Hundred Years, pp xviii-xix, 31, 33.

58	Builder (London), XI, 529 (26 March 1853), p 208.

59	Allegedly referred to as B White & Co: Ritchie, Canada Builds, p 31.

60	Sydney Exhibition 1879, Official Catalogue of the British Section, pp 51, 50.

61	Davis, A Hundred Years, pp x, xviii.

62	William Aspdin, in Builder, VI, 292 (9 September 1848), p 443; Butler, Portland Cement, pp 1–3.

63	Butler, Portland Cement, p 1. He attributes the tunnel to Isambard Brunel, but at this stage Brunel junior had only recently entered his father’s office. Pasley refers to the use of cement here, but says nothing of its origins. In 1839, however, Isambard Brunel wrote that he himself had used Francis’s cement for the greater part of the tunnel: Davis, A Hundred Years, p 73.

64	Pasley, Observations on Cements, Preface, unpaginated, and p 157.

65	Butler, Portland Cement, p 1.

66	Davis, A Hundred Years, pp xix, 49–53.

67	Skempton, ‘Portland Cements’, p 117.

68	Hamilton, ‘Building and Civil Engineering’, p 117.

69	James Pulham, in the Builder, III, 113 (15 April 1845), p 160.

70	See Pasley, Observations on Cements.

71	Skempton, ‘Portland Cements’, pp 129–130, citing a circular issued by Maude & Co late in 1843.

72	Australasian Builder & Contractor’s News, 12 October 1889, p 346.

73	James Pulham, in the Builder, III, 113 (15 April 1845), p 160.

74	Robins, Aspdin & Co of Northfleet showed their Portland cement at the Great Exhibition of 1851: Great Exhibition, 1851,  Catalogue, I, p 113; Australasian Builder & Contractor’s News, 12 October 1889, p 346, gives it as Robins, Aspdin & Co.

75	Builder (London), XI, 529 (26 March 1853), p 208.

76	Skempton, ‘Portland Cements’, p 129.

77	Builder (London), XI, 529 (26 March 1853), p 208.

78	Kersten, Der Eisonbetonbau.

79	Skempton, ‘Portland Cements’, pp 82-3, 89.

80	Mechanic’s Magazine, XXXVI, 975 (15 April 1842), pp 310–11.

81	Wermiel, ‘The Development of Fireproof Construction’, p 19.

82	Thornton, Cast in Concrete, p 16.

83	Millar, Plastering Plain and Decorative, pp 186-229.

84	Verrall, Modern Plasterer, II, p 20.

85	Lowndes & Boyd, Plastering and Stucco Work, pp 63, 70.

86	AONSW. Schedule of Government Contracts in the Colony of New South Wales, 1836; this uses the expressions ‘render, float and stucco on brick’  and ‘lath, plaster, float, and stucco’. The AONSW. Schedule of Government Contracts in the Colony of New South Wales, 1864 required that  ‘The whole of the plastering and stucco to be made up with sharp pit or fresh water sand or road drift and the stucco be not less than ¾ inch thick’.

87	Sydney Morning Herald, 18 February 1850, p 2, ‘the back wall of the King Street Court House [is being] stuccoed about half way up‘.

88	Millar, Plastering, Plain and Decorative, p 103

89	Millar, Plastering, Plain and Decorative, p 101

90	Mitchell, Building Construction, p 75.

91	Nangle, Australian Building Practice [1944], p 395.

92	Dixon & Muthesius, Victorian Architecture, p 16.

93	Morris-Nunn, Rich and Chaste, p45

94	 Hobhouse and Saunders eds, Good and Proper Materials – the Fabric of London Since the Great Fire, p 18.

95	 Downing, Architecture of Country Houses, p 63. Downing considered stucco to be a cheaper, warmer and drier material than ordinary masonry.

96	 Burden, Illustrated Dictionary of Architectural Preservation, p 247. The full definition is ‘an exterior fine plaster finish composed of Portland cement,  lime, and sand, mixed with water, used for decorative work or mouldings, and usually textured’.

97	 Millar, Plastering, Plain and Decorative, p 183.

98	 Nangle, Australian Building Practice [1944], p 366

99	John Gwynn, London and Westminster Improved (London 1766), quoted in Summerson, Georgian London, p 111.

100	Roman cement was imported in casks in the 1830s by James Bowman for use in finishing his villa ‘Lyndhurst’ on the shores of Sydney Harbour. The villa was built in the Regency style and finished with external stucco, decorated with architraves and cornices run in Roman cement. The Docker house ‘Bontharambo’ near Wangaratta, built in the early 1850s with mainly imported materials, appears to have both Roman and Portland cement elements.

101	In the early 1980s, the plasters and mortars used in the construction of the two end wings of the Rum Hospital in Sydney were examined closely during conservation works. They comprised mainly clay and sand, with small quantities of shell lime and small quantities of both cow hair and chopped grasses to provide some tensile strength and to overcome the shrinkage of the clay during drying. The internal plasters were applied in layers up to 35 mm thick. The setting coats were mixtures of pure lime and sand.

102	Loudon, Cottage, Farm and Villa Architecture, pp 259–60 [§ 527].

103	Loudon, Cottage, Farm and Villa Architecture, cl 527

104	Gwilt, The Encyclopaedia of Architecture [1912], p 709

105	Millar, Plastering Plain and Decorative, p 104.

106	Millar, Plastering Plain and Decorative, p 181.

107	 Mitchell, Building Construction, p 76

108	The house, ‘Osborne’, was built between 1845 and 1851 for Queen Victoria and Prince Albert by the builder Thomas Cubitt, whose company also built the main façade of Buckingham Palace and many London terraces. Prince Albert was the designer. The architecture is based on palaces of the Italian Renaissance and has two campanile-like towers. The brick building was faced with Portland cement and its interiors were richly plastered. The house was always the favourite of Victoria, who spent many summer months there.

109	Millar, Plastering Plain and Decorative, p 91.

110	Mitchell, Building Construction, p 75.

111	Millar, Plastering Plain and Decorative, p 103.

112	Millar, Plastering Plain and Decorative, p 104.

113	Millar, Plastering Plain and Decorative, p 104.

114	Millar, Plastering Plain and Decorative, p 104.

115	Millar, Plastering Plain and Decorative, p 104.

116	 	Lawrence et al, ‘Non-Hydraulic Lime Mortars’, p 26.

117	 	Lawrence et al, ‘Non-Hydraulic Lime Mortars’, p 26.

118	 	Mitchell, Building Construction, p 76.

119	 	Loudon, Cottage, Farm & Villa Architecture, § 528, p 260,

120	 	Lewis, ‘Australian Stucco’.

121	 	Millar, Plastering Plain and Decorative, p 190.

122	Millar, Plastering Plain and Decorative, p 190.

123	The Handyman’, unidentified newspaper [probably the Daily Mirror], Sydney, c 1960.

124	Argus, 10 February 1882, p 1.

125	Keim History, retrieved 9 April 2007, http://www.keimsystems.com/history.html In 1878 A W Keim was granted a royal patent for his liquid silicate paint combining a potassium silicate binder with inorganic fillers and natural earth oxide color pigments, and it has been used successfully since then.

126	Great Britain, patent no 517 to J B Orr, 10 February 1874, for a white pigment of barium sulphide and zinc sulphide.

127	Annual Report by the Government Architect in New South Wales Public Works Annual Report, 1891.

128	The Bendigo Post Office and Law Courts group at 51-71 Pall Mall was built between 1883 and 1896. It is finished with cement which has been coloured with a mid brown wash.

129	Neve, quoted in Papworth, Dictionary of Architecture, sv Stucco; I have been unable to locate the reference in Neve

130	Haddon, Australian Architecture, p 489.

131	Haddon, Australian Architecture, p 491.

132	Phillip, The Voyage of Governor Phillip, p 145.

133	Specifically oyster shells in the case of the New England and Chesapeake Bay colonies: A H Ameri, ‘Housing Ideologies in the New England and Chesapeake Bay Colonies, 1650-1700’, Journal of the Society of Architectural Historians, LVI, 1 (March 1997), p 10. An early example of the use of oyster shell lime mortar was the Apyucxet Trading Post at Bourne, Massachusetts, of 1627: Hugh Morrison, Early American Architecture from the First Colonial Settlements to the National Period (New York 1952), p 90.

134	R B Lewcock, Early Nineteenth Century Architecture in South Africa (Cape Town 1963), p 278; Brian Kearney, Architecture in Natal (Cape Town 1973), p 66.

135	White, Journal of a Voyage to New South Wales, pp 133-4. For a detailed analysis of the building see Helen Proudfoot, ‘The first Government House, Sydney’ (mimeographed typescript report to the Premier’s Department, NSW, 1983), p 15.

136	Dodd, ‘Lime and Victorian Buildings’, p 54.

137	Cannon, Historical Records of Victoria, III, p 271.

138	Dodd, ‘Lime and Victorian Buildings’, p 58.

139	Jeans, ‘The Building Industry’, p 105.

140	Gemmell, And So We Graft from Six to Six, p 5.

141	Wentworth, Statistical Description of New South Wales, p 56.

142	Windross & Ralston, Historical Records of Newcastle, 1797–1897 (Newcastle 1897), cited in Tucker], Ralph Rashleigh, p 242.  See also Mitchell, Hunter’s River, pp 7–8.

143	Wellings, Benjamin Boyd, p 14.

144	Intercolonial Exhibition, Official Record, p 61.

145	Cannon, Historical Records of Victoria, III, pp 270–279.

146	Steel, Brisbane Town in Convict Days, pp 54, 73.

147	Intercolonial Exhibition, Official Record, p 74.

148	Stacpoole, William Mason, p 30.

149	Lack, Newstead House, p 5.

150	Allom Lovell Marquis-Kyle, ‘St. Helena Island’, no M514.

151	Australasian Builder & Contractor’s News, 8 September 1887, p 358. See also Daly, Digging, Squatting, and Pioneering Life, p 110.

152	Collins, The English Colony in New South Wales, p 177.

153	Robertson, Early Buildings of Southern Tasmania, I, p 15.

154	Charles Jeffreys, Van Diemen’s Land (London 1820), quoted in Stone & Tyson, Old Hobart Town, p 58.

155	Hobart Town Gazette, I, 3 (15 June 1816), p 2.

156	Irving, ‘The First Australian Architecture’, p 149, citing Herman, p 134; Freeland, p 68; Bigge Enquiry C.O. 201/122, p 58. Irving claims the same for Van Diemen’s Land, but this is contradicted by the Hobart Town Gazette report, supra.

157	Herman, The Early Australian Architects, p 98, quoting Henry Kitchen to Commissioner Bigge, 1821, Bigge Appendix, box 27, 6449.

158	R I Jack in Hughes Trueman Ludlow, Evans Shire Council Heritage Study, I [no page] theme 6.

159	Atkinson, Agriculture and Grazing in New South Wales, p 97.

160	Atkinson, Agriculture and Grazing in New South Wales, p 97.

161	Gemmell, And So We Graft, p 5.

162	Mayes, Australian Builders’ Price-Book (1877), p 44.

163	Gemmell, And So We Graft, p 5.

164	Burn, Picture of Van Diemen’s Land, p 89.

165	Report by Major Lockyer, Historical Records of Australia, 3/6, pp 481, 485, 489, quoted in Coutts, Corinella, p 146.

166	Pearson, ‘The lime industry in Western Australia’, p 94.

167	Fergusson, Rottnest Island, p 21.

168	Markey, ‘Pioneer Perth’, p 56.

169	Millett, An Australian Parsonage, p 71.

170	Griffith, The Port Phillip District, pp 4-5.

171	Henry Kitchen to Commissioner J T Bigge, 13 August 1823, J.T. Bigge Report - Appendix, Bonwick Transcripts, Mitchell Library, box 27, p 6449,  cited in Broadbent, The Australian Colonial House, p 95.

172	Australian, 5 April 1826, quoted in Dyster, Servant and Master, p 105

173	Sydney Herald, 23 November 1835, reproduced in Evans, The Australian Home, p 59.

174	Geelong Advertiser, 28 July 1856.

175	South Australian Register, 6 October 1858, quoted in Jensen, Colonial Architecture in South Australia, p181.

176	Hyndman & Bates, ‘Villa Residence Camberwell’, p 2.

177	Reed, Henderson & Smart, ‘Premises for the Metropolitan Gas Coy’, p 4.

178	Harrington, Limeburning in Victoria, p 9, pp 38-9, ref C Johnston, ‘Conservation Analysis: Coimadai Lime Kilns’ (report to the Rural Water Commission 1986); Melbourne’s Living Museum of the West, ‘An Oral History of the Coimadai Kilns’ (report to the Rural Water Commission 1986).

179	‘Mitchell Memoranda Book, 1827-1829’.

180	J[ames] Thompson, letter of 10 August 1833, in Architectural Magazine, I (December 1834), p 377.

181	James, Six Months in South Australia, p 28.

182	Colonial Secretary’s correspondence C 53/9930. See also Mayes’s advertisement in the Argus, 3 October 1853, p [?3].

183	Australasian Builder & Contractor’s News, 16 March 1889, p 249.

184	Pasley, Limes, Calcareous Cements, &c, appendix pp 114–5. Pasley does not name Cotton, but see John Weiler, ‘Colonial Connections: Royal Engineers and Building Technology Transfer in the Nineteenth Century’, Construction History, XII (1996), pp 4–5, ref A T Cotton, ‘Magnesia Cement’, Professional Papers of the Madras Engineers, I (1845), p 28.

185	Weiler, ‘Colonial Connections’, p 4, ref J M Brown, ‘Contributions of the British to Irrigation Engineering in Upper India in the Nineteenth Century’, Transactions of the Newcomen Society, LV (1983-4), pp 85–112.

186	Pasley, Limes, Calcareous Cements, &c, p 28.

187	Gillmore, Hydraulic Cements and Mortars, pp 304–5. See also pp 48, 49, 51 & 53 for the Rosendale companies.

188	Lewis, ‘Tradition and Innovation’, II, p 310–13.

189	Hughan was later to obtain a British patent for the use of Portland, Roman and other cements in deodorizing works: Great Britain, patent no 2893 to  W H Hughan, 19 September 1868. Also related patents, no 67, 8 January 1879; no 3060, 30 November 1871; no 2700, 20 August 1873; and no 1959,  5 June 1874.

190	For example at Adelaide in 1851: Colonial Architecture in South Australia, p 107.

191	Melbourne Prices Current and Shipping List, 14 April 1857, quoted Dodd, ‘Lime and Victorian Buildings’, p 37.

192	Australian Builder and Practical Mechanic. 25 September 1856, p 236.

193	Dodd, ‘Lime and Victorian Buildings’, p 37.

194	Dodd, ‘Lime and Victorian Buildings’, p 73.

195	Mayes, Australian Builders’ Price-Book (1862), p viii.

196	Information from Irene Wynne, 7 September 2004.

197	Dodd, ‘Lime and Victorian Buildings’, p 33.

198	Australian Engineering and Building News, 1 May 1881, p 216.

199	Australasian Builder & Contractor’s News, 22 December 1888, p 582.

200	Ashton & Green, Limited, p 20.

201	Said to have been established in 1850: Building News, 20 April 1888, p xxvii.

202	Building News, 20 April 1888, p xxviii.

203	Building News, 20 April 1888, p xxviii.

204	Flannagan, ‘ Shop Additions in Heidelberg Road, Ivanhoe’, p 18.

205	Stone, Reinforced Concrete in Australia, p 11.

206	James Moore & Sons, Price List 96, p 5.

207	Davis, Portland Cement, p 1.

208	Reed & Barnes, ‘ Banking Premises at “Kooringa S.A.”’, p 48.

209	Victorian patent no 1548 to William Henry Malyon, 29 August 1871.

210	Victorian patent no 1725, 1725A to James Moeller Robertson, 29 January 1873.

211	McKay, ‘The Cement Industry to 1939’, p 1.

212	Penn, How Firm the Foundation, passim.

213	McKay, ‘Cement Industry to 1939’, p 6.

214	The company was apparently established at Portland in Western Victoria, but leased land at Fyanstown near Geelong, with limestone available not far away at Batesford. It did not come into production until well into 1890. Australasian Builder & Contractor’s News, 7 December 1889, p 152.

215	McKay, ‘Cement Industry to 1939’, pp 2–4; Johnstone, ‘Australian Cement Industry’, pp 2–3.

216	Goodlet & Smith commenced production of Australian Portland cement at their Granville works in 1893 under the ‘Rock’ brand. The cement was burnt from limestone brought by rail from Mudgee, where the company owned large deposits, using patent kilns and, from 1901, rotary furnaces. Johnson, ‘Goodlet and Smith’, pp 2, 6.

217	Cunningham, Two Years in New South Wales, II, p 162.

218	Australian Settler’s Handbook, p 11.

219	Loudon, Cottage, Farm and Villa Architecture, § 527, p 259.

220	Builder, XII, 585 (21 April 1854), p 207.

221	Loudon, Cottage, Farm, and Villa Architecture, § 830, p 421.

222	Russell, Watts & Pritchard, ‘Dwelling houses at Elwood’, p 19.

223	Australian Builder, 24 December 1859, p 409, quoting the St Kilda Chronicle.

224	Australasian Builder & Contractor’s News, 3 September 1887, p 267.

225	Town and Country Journal, 3 March 1877, p 348.

226	Mayes, Australian Builders’ Price-Book (1877), p 85.

227	Smith’s note in Vicat, Calcareous Mortars and Cements, p 136.

228	Mayes, Australian Builders’ Price-Book (1877), p 97.

229	Law, ‘Specifications ... for Mrs. L. Abrahams’, p 44.

230	Haddon, Australian Architecture, pp 490–1.

231	Nangle, Australian Building Practice, p 397.

232	Russell, Watts & Pritchard, ‘Dwelling houses at Elwood’, p 19.

233	Scripps et al, Willow Court Conservation Management Plan, p 33.

234	Australian Settler’s Handbook, p 11.

235	Beswicke & Hutchins, ‘Painting “Altyre”’.

236	Haddon, Australian Architecture, p 498.

237	Hasluck, Cassell’s House Decoration, pp 159–60.

238	Builder [UK], XI, 539 (4 June 1853), p 367: it came in a stone colour, but could be tinted to different colours, and was recommended as an improvement over common lime wash or water colour.

239	Mayes, Victorian Contractors’ Price-Book (1859).

240	Australasian Builder & Contractor’s News, 11 June 1887, p 72.

241	Argus, 10 February 1882, p 1.

242	Haddon, Australian Architecture, p 491.

243	Millar, Plastering Plain and Decorative, p 187. Millar does refer on p 25 to the impressed plaster of the 12th–13th centuries, but it appears to be literally impressed, rather than incised, presumably with moulded forms rather than sharp edges.

244	Cornwall Chronicle, 22 October 1864, p 4.

245	The material seems to be unconnected with the ‘Victoria Stone’ patented in England in 1868, which was made of granite chippings and Portland cement cast in moulds, then steeped in ‘a solution of silica’: Papworth, Dictionary of Architecture, sv Victoria Stone.

246	Argus, 5 August 1881, p 3.

247	Argus, 2 October 1883, p 9.

248	Argus, 3 October 1883.

249	To Architects, Contractors, &c.

250	Argus, 2 September 1882, p 9; 12 December 1882, p 10.

251	Argus, 20 October 1884, p 6

252	Argus, 20 March 1884, p 5.

253	Argus, 18 October 1884, p 10.

254	Reported by Helen McCarthy, 1999.

255	Haddon, Australian Architecture, pp 491–2.

256	Law, ‘Residence for Mrs. L. Abrahams’, p 46.

257	Law, ‘Residence for Mrs. L. Abrahams’, pp 46–9.

258	Ware & Richardson, Ramsay’s Catalogue [1949], § 5/1; Ware & Richardson, Ramsay’s Catalogue [1954], § 5/1.

259	Nangle, Australian Building Practice, p 367.

260	Richardson, Ramsay’s Catalogue [1931], § 25, pp 207, 210.

261	Haddon, Australian Architecture, p 497.

262	Richardson, Ramsay’s Catalogue [1931], § 25, p 202.

263	Richardson, Ramsay’s Catalogue [1931], § 25, p 221.

264	Green, ‘Cements and Concrete’, p 42.

265	Sold by the Cement Marketing Co Ltd of Westminster: Faber & Childe, Concrete Year Book 1949, p 574. It was a waterproof cement paint supplied in white, cream, pink and silver grey.

266	Pittsburgh Plate Glass Company, Architectural Specifications (Milwaukee [Wisconsin] 1935), pp 25-6.

267	One would assume that this was made or sold by the Cement Marketing Co, makers of Cullamix: Faber & Childe, Concrete Year Book 1949, p 307. Hoeverthesaoheel out

268	Faber & Childe, Concrete Year Book 1949, p 586.

269	Sweet’s Architectural Catalogue (New York 1922), p 79. This formed ‘in and on the surface, a tough, flat pigment film, which does not flake,  blister or peel, and which is absolutely waterproof.’

270	Richardson, Ramsay’s Catalogue [1931], § 21d, pp 191-2.

271	The normal sand and lime plastering would be carried out using a render and float coat of 3 parts sand to 1 part slaked lime. The set coat is a reverse mix and contained 3 parts lime to 1 part sand, which could vary slightly depending on the sand to a 5 parts lime to 2 parts sand mix. However, the lime being used would be the normal non hydraulic fat lime, and would rely on compression of the top coat created by working the surface with a wooden float several times to close the surface and to stop the cracking, before finishing with a steel trowel. On internal work, plastering with fat limes is fine but externally they fail very quickly—because it is just a 3 to 4 mm thick coating of sand and lime without any additives that is relying carbonation to achieve any real resistance to the weather.

272	Kemp The Practical Plasterer, p 25.

273	Kemp The Practical Plasterer, p 25.

274	NSW, ‘Schedule of Contract: Plasterer’s Work’, 1836 and 1864.

275	 Tanner, Tempe House.

276	 Elastosil M4503, Wacker Chemie. AG.

277	 Godfrey, ‘Romla and Frelin’.

278	 Vitruvius, Ten Books of Architecture, book VII, chapter III, p 207.

279	 Kemp, Practical Plasterer, p 114.

280	 Kemp, Practical Plasterer, p 115,

281	 Kemp, Practical Plasterer, p, 115.

282	 Kemp, Practical Plasterer, p 116.

283	Hughes & Válek, Mortars in historic Buildings, passim.

284	Nangle, Australian Building Practice [1911], p 366.

285	Young, Salt Attack and Rising Damp, passim.

286	Hughes & Válek, Mortars in historic Buildings, passim.

287	APT Bulletin; The Journal of Preservation Technology, Association of Preservation Technology International, USA. See index at www.apti.org

288	See especially Stewart & Moore, ’Chemical Techniques of Historic Mortar Analysis’.

289	See Jacob & Weiss, ‘Laboratory measurement of water Vapour Transmission Rates’.

290	See Suter et al, ‘Mortar study of Mechanical Properties’.

291	See Suter et al, ‘Mortar study of Mechanical Properties’.

292	 Seeley, ‘Lead Paint for Historic Buildings’, pp 24–42.

293	Krotzer, ‘Architectural finishes’, pp 1–6.

294	 Ellis, ‘The Analysis of Mortar’.

295	 Herm, ‘Kalkfarbetechniken’.

296	Matero & Snodgrass, ‘Understanding Regional Painting Traditions’, pp 36–52.

297	Burgio, ‘Dating Alhambra Stuccoes’.

298	Istudor et al ‘An Alteration Phenomenon of Cinnabar Red Pigment in the Mural Paintings from Sucevita’, p 602.

299	Jonsson & Cliver, ‘Coloring Historic Stucco’, pp 31–6.

300	 Getty Trust, AATA Art and Archaeology Technical Abstracts online, search for ‘paint‘.

301	Museum of Fine Arts, Boston, CAMEO: Conservation & Art Material Encyclopedia Online, at <http://cameo.mfa.org/>, definition found  using search for ‘distemper’.

302	Hirst, ‘Limewash and Distempers, the Building Conservation Directory’.

303	Museum of Fine Arts, Boston, CAMEO.

304	Gettens and Stout, Painting Materials, p 175.

305	Vratislav, ‘Zprávy Památkové Péc˘ e’, pp 110–17.

306	Aitken, accessed via Getty Trust, AATA Art and Archaeology Technical Abstracts online

307	Museum of Fine Arts, Boston, CAMEO: Conservation & Art Material Encyclopedia Online, at <http://cameo.mfa.org/>, definition found using search for ‘Dirt’.

Gettens and Stout, Painting Materials, p 175.

308	Holper & Noonan, ‘Air Pollution Information Sheet’.

309	As a result, the conversion of lime (calcium hydroxide) to more voluminous gypsum (calcium sulphate) by the action of acid rain (containing sulphur dioxide and similar materials) is not common, but in theory could be found near industrial areas. Little research has been done on whether this form of deterioration is present on Australian historic buildings.

310	Del Cueto, ‘Manual on Conservation Methodology ‘, p A.4.4.

311	Institution of Engineering and Technology, ‘Colour Vision Defects’,

<www.theiet.org/factfiles/health/colourvisiondefects.cfm?type=pdf> accessed 9 May 2009.

312	David Tilbrooke, is a conservation scientist with many years experience in the technical analysis of museum, art and architectural materials.  He is the director of Museum Environment and Conservation Services, based in South Australia.

313	 Vogel, Qualitative Chemical Analysis.

314	 Vogel, Qualitative Organic Analysis.

315	Thompson, Semi-Micro Inorganic Qualitative Analysis.

316	End of Tilbrooke contribution.

317	Stoner, ‘Lining and Cleaning of Easel Paintings’. The debate over cleaning of paintings started over 300 years ago with heated public discussions regarding the advisability of removing yellowed varnish from paintings. These varnishes had yellowed to such an extent that the original colours could no longer be seen or were greatly distorted (a yellowed varnish over a blue area will make it appear green etc). However, others felt that the removal of the ‘golden glow’ of age was akin to vandalism.

318	Keck, ‘Some Picture Cleaning Controversies’.

319	Matero, ‘Loss, Compensation and Authenticity’.

320	Grossi & Brimblecombe, ‘The White Tower and the Perception of Blackening’.

321	Personal communication.

322	 Gettens & Stout, Painting Materials.

323	Personal communication with Porter’s Paints representative, in relation to Porter’s Original Lime Wash.

324	Jonsson & Cliver, ‘Coloring Historic Stucco’, pp 31—36.

325	Personal communication with Kiem® Mineral Paints representative, in relation to Keim® Concretal System and Keim® Royalan Paint.

326	Hughes, Swann & Gardner, ‘Roman Cement. Part 2’. p 56.

327	Hughes, Swann & Gardner, ‘Roman Cement. Part 2’, p 56.

328	 Matero, Loss, Compensation and Authenticity’.

329	 Heritage Victoria statement of significance.

330	Millar, Plastering Plain and Decorative, p 104, describes trowelled stucco, which was ‘used for work that that has to be subsequently painted’. In addition, Schedules of Contract of Plasterer’s work for the service of the Honourable Board of Ordinance at Sydney (1836, 1838, and 1864) two types of stucco were scheduled. They were ‘Render, float and stucco on brick’ and ‘Render, float, and trowel, stucco on brick’.

331	Millar, Plastering Plain and Decorative, p 104, describes ‘common stucco’ which was finished with a hand float, ‘rough stucco’ which was coloured to imitate stone, and ‘bastard stucco’ which was trowelled off and brushed.

332	Mitchell, Building Construction, p 75.

333	Pilcher, Regency Style, pp 49-50, quoting C A Busby, Designs for Villas and Country Houses, (1808).

334	Mitchell, Building Construction, p 76. A product called Cullacrete, composed of white ferrocrete mixed with a wide range of pigments  and selected sands, properly graded, was supplied by the Associated Portland Cements Ltd for use as a finishing coat in stucco work.

335	Bristow, ‘Exterior Renders Designed to Imitate Stone’, p 27.

336	Loudon, Cottage, Farm and Villa Architecture, p 260 [§ 528].

337	Schedule of Contract of Plasterer’s work for the service of the Honourable Board of Ordinance at Sydney [1836] p 8.

338	Although the reserves of limestone (calcium carbonate) for the production of lime (calcium oxide and calcium hydroxide) were limited in the first years of colonisation, other sources, including estuarine shells, were plentiful in the vicinity of the early port settlements, and new sources of limestone were located and exploited as the colonies expanded inland.

339	Chalk or plaster of Paris and glue size were the base ingredients of distempers. Most forms of glue size were soluble in water.

340	Loudon, Cottage, Farm and Villa Architecture, p 260 [§ 528].

341	Millar, Plastering Plain and Decorative, p 190.

342	Bristow, ‘Exterior Renders Designed to Imitate Stone’, p 27.

343	The author has sampled many stuccoed façades over the past 25 years and found loose bound pigments of the type used to make washes below the oil bound paint finishes. Even allowing for the extreme chalking of poor quality oil paints, it must be concluded that water-based colours were applied in most cases before the oil-bound paints were applied.

344	Raddle is a variety of red ochre that gave its name to the application of red or sometimes yellow or black to brickwork to intensify the brick colouring and contrast with the white or black pointing.

345	Long standing traditional bricklaying craft practices included methods of applying colour washes over brickwork to enhance the uniformity of the brickwork, and redefine the joint lines by the application of thin contrasting coloured lines in a process called ‘pencilling’. See Lynch, ‘The Colour Washing and Pencilling’, passim.

346	Loudon, Cottage, Farm and Villa Architecture, p 260 [§ 528].

347	‘To Mix Lime Wash’, Australasian Decorator and Painter, 1 May 1906, p 160.

348	Examples include the Church of the Sacred Heart, Carlton (1897) which is a brick neo-Baroque building with Portland cement dressings coloured with  a distinctive golden tint. This colouring has weathered off the exposed surfaces but is clearly visible on the protected cement stucco.

349	New South Wales Government Gazette, 1833, p24. Commissariat Office, Sydney, Store Branch, 7th January 1833, articles for sale included, copperas, white and green.

350	Lewis, elsewhere in this volume, refers to the best-known brand, Johns’s Patent Stucco Wash, which was marketed in Melbourne by Dickson, Williams & Co.

351	Keim History, retrieved 9 April 2007, <www.keimsystems.com/history.html> One of the first was marketed by Keim Mineral Paints in Bavaria. It was claimed to be the nineteenth century equivalent of traditional fresco paint. In 1878, A W Keim was granted a Royal Patent for his liquid silicate paint.

352	It is not known whether the specification of ‘silicate paint’ on the cement stuccoed parts of railway buildings in New South Wales in the early twentieth century was the Keim type or a washable distemper produced by the Silicate Paint Co.

353	Australasian Decorator and Painter, 1 July 1 1906.

354	Charlton white was a sulphide zinc white made by combining the two pigments, sulphide of zinc and sulphate of barium. It was patented by the British manufacturer J B Orr.

355	Duresco Washable Water Paint was employed with such success in New South Wales that the Government Architect reported in 1890 that it was in use on the interior and exterior of all public buildings.

356	Cement particles provide the base pigment of cement washes.

357	Hasluck, House Decoration, p159.

358	The West Coast Kalsomine Co produced Wesco Cement Bonding Paint, suitable for porous surfaces including stucco. Boncote Cement Paint has been available since 1920. It is now manufactured by Porters.

359	Taubman’s Cement-Proof Paint was a solvent-based paint that was curiously incompatible with linseed oil. Majora Anti-Cement Oil Paint was marketed specifically for concrete, cement, stucco, plaster, stone and Monier pipe. Berger’s Cement and Waterproof Paint was an oil paint that dried to a dull velvety finish without gloss. It was available in the colours of light stone, slate and ivory.

360	Testing of paint removal methods in December 2008 at Albert Hall in Canberra (built 1927), where the original finish was cement wash on Portland cement-based stucco, included trialling an abrasive method using calcium carbonate aggregate that was considered to be ‘soft’. It successfully removed accumulated layers of oil-based and modern emulsion paints, but it also damaged the surface of the stucco as soon as it was exposed to the abrasive. This example is but one of many that highlights the risks of abrasive cleaning methods on even the most robust types of Portland cement-based stuccos.

361	Although the terms ‘paint’ and ‘painting’ are used throughout this discussion, strictly speaking the washes and distempers are not paints. In earlier times, washes were applied by plasterers (or bricklayers) and not by painters. But today they would be applied by painters.

362	Jackson, Botting & Striegel, ‘Durability of Traditional and Modified Limewashes’, pp 19-28.

363	Porter’s Paints was lobbied by the NSW Heritage Branch Technical Advisory Group to remove the potentially harmful acrylic resin from its limewash.  The choice of casein as an alternative binder is based on traditional practice.

364	Hasluck, Cassell’s House Decoration, p 159.

365	Wesco Bonding Cement Paint was first produced by the West Coast Kalsomine Co. (Australia) Ltd at Parramatta, NSW in 1920.

366	Porters recommend a conditioner should be used in mixing Boncote—this conditioner is an acrylic resin emulsion.

367	It is sometimes recommended that cement paint should be applied with acrylic conditioner over lime-proof undercoats. The use of acrylic-based materials on porous stucco may compound problems of damp and salts.

368	The difference between the use of sodium silicate and potassium silicate as a binder is mainly geographic. The western hemisphere mainly produces sodium silicate, whereas Europe produces potassium silicate.

369	Silicate Mineral Paint, Wikipedia, retrieved 9 April 2007, <http://en.wikipedia.org/wiki/Silicate_mineral_paint>.

370	History of Acrylic paint retrieved 10 April 2007, <www.watercolorpainting.com/acrylics.htm>. The first synthetic acrylic resin were made in 1901 by Dr Otto Röhm and brought into American commercial production in the 1930s by Röhm & Haas. The acrylic resin was particularly useful for making cast plastic sheeting (Perspex) as well as polymerized emulsions for making paint. After World War II, the first acrylic paints were put onto the market. They were sold in solution form dissolved with turpentine and could be mixed with oil paints. By 1953, Röhm & Haas introduced the first true acrylic paints as interior wall paints.

371	Wikipedia, Acrylic paint, retrieved 10 April 2007, <http://en.wikipedia.org/Wiki/Acrylic.paint>. Water-based acrylic paints were subsequently sold as ‘latex’ house paints, although acrylic dispersion uses no latex derived from a rubber tree. Interior ‘latex’ house paints tend to be a combination of binder (sometimes acrylic, vinyl, or pva), filler, pigment and water. Exterior ‘latex’ house paints may also be a ‘co-polymer’ blend, but the very best exterior water-based paints are 100% acrylic. Soon after the water-based acrylic binders were introduced as house paints, artists (the first of whom were Mexican muralists) and manufacturers alike began to explore the potential of the new binders. Water soluble artist quality acrylic paints became commercially available in the early 1960s, offered by Liquitex.

372	Wardell, ‘the English Scottish & Australian Chartered Bank’, p 18.

373	Wardell, ‘the English Scottish & Australian Chartered Bank’, p 19.

374	Wardell, ‘the English Scottish & Australian Chartered Bank’, pp 21–2.

375	Wardell, ‘the English Scottish & Australian Chartered Bank’, pp 28–9.

376	Mayes, Australian Builders’ Price Book [1886], p 95.

377	Terry & Oakden, What to Build and How to Build It, p 7.

378	Contrary to other parts of this publication, this case study uses terminology as experienced, by the author, in the trade conservation industry in the twenty-first century, whether I agree with it or not. This includes use of the term render for all external ‘plasterwork’ including mouldings. The term ‘stucco’ is not used for the same reason. Whilst I welcome other more traditional terms in professional publications such as this, I encourage heritage professionals to be familiar with currently used trade terms in an attempt to bridge the chasm that so often exists between the two groups

379	Allom Lovell & Associates, ‘Bontharambo, Wangaratta, CMP’, pp 262, 263.

380	Simon Wiltshier, ‘Bontharambo, Structural Report’, pp 2, 3.

381	A permit was sought for the full height of the tower, though Stage 1 works being limited to the upper portion.

382	Lovell Chen was originally engaged to provide technical support for the project.

383	Gypsum plaster is not stable in damp or exposed exterior situations.

384	I have always believed the deposit to be some sort of organic compound because it occurs only in locations with prolonged moisture (exposed to weather but not hot sun) and the unlikelihood that such a colour would be found so widely on rendered nineteenth century buildings.

385	So dated in the Allom Lovell conservation management plan.

386	Comments by Peter Lovell and Janet Beeston, 2006.

387	Brandi, Theory of Restoration, p 72.

388	Earl, Building Conservation Philosophy, p 108.

389	Australia ICOMOS, The Burra Charter.

390	ICOMOS, The Nara Document on Authenticity (Nara 1994), Appendix 1.5.

391	Barrie Cooper, Westlegate Pty Ltd Product Information (Sydney 2008).

Index

(types)

(types) artificial, 6, 8, 9, 10, 11, 12, 15, 23, 26, 27, 28, 44, 45

acrylic, 20, 56, 57, 65, 66, 71, 75, 77, 78, 79, 80, 90, 91, 95, 99, 103

albarium opus, 6, 106

analysis

chemical, 62, 68

technical, 54, 55, 56, 57, 59, 62

ashlar, 6, 7, 18, 23, 28, 29, 30, 33, 74, 81

Australian standards, 43, 44, 48, 92

binder (see also casein, glue size), 14, 15, 43, 44, 46, 47, 51, 52, 56, 58, 63, 68, 69, 70, 72, 78, 79, 87, 93, 100, 103, 104

Boom Style, 33

brands (of lime, cement), 9, 26, 27, 79, 82

Burra Charter, 47, 66, 85, 94, 112

carbonation, 14, 42, 43, 45, 55, 56

casein, 33, 35, 56, 57, 58, 68, 69, 70, 73, 78, 79

casting (see also moulds, ornamentation, enrichments), 15, 23, 27, 28, 31, 32, 33, 38, 91, 101, 104

cement (types)

hydraulic, 5, 7, 8, 9, 26, 27, 28, 51, 99

natural, 6, 8, 9, 11, 12, 14, 23, 26, 32, 51, 99

Parian, 101, 104

Portland (see also mortar, stucco, casting), 5, 8, 9, 10, 11, 13, 14, 15, 16, 17, 18, 19, 20, 21, 23, 26, 27, 28, 29, 30, 31, 32, 33, 34, 35, 44, 45, 48, 51, 56, 64, 71, 72, 73, 75, 79, 80, 82, 84, 92, 93, 94, 97, 98, 99, 103, 104, 106

Roman, 5, 8, 9, 14, 15, 16, 19, 23, 25, 26, 28, 29, 35, 56, 72, 73, 90, 92, 97, 99, 106

cement render (see also stucco, roughcast, pebbledash), 5, 10, 17, 82, 97, 98, 106

cement wash, 20, 72, 73, 74, 75, 79, 80

chalk (calcium carbonate - see also whiting), 6, 9, 10, 16, 18, 24, 33, 56, 58, 66, 68, 69, 70, 73, 74, 78, 100, 103

chromatography, 54, 63

chunam, 29

cleaning, 64, 71, 72, 75, 76, 77, 80

coatings, 12, 20, 21, 31, 45, 54, 55, 56, 57, 59, 65, 66, 72, 75, 77, 78, 79, 80, 88

clear, 71, 75, 77, 78

maintenance, 54, 55, 56, 58

colour washes (see also limewash, colourants), 20, 21, 73, 74, 80

colourants (see also stucco wash, copperas, pigments, ochres), 54, 55, 56, 65, 66, 106

compatibility (of repair materials), 47, 48, 52, 66, 78, 79

compo (see also composition mortar), 5, 28, 29, 82, 98, 100, 103

consolidation, 94, 96

copperas (iron sulphate - see also colourants), 19, 30, 57, 66, 73, 74, 101

delamination, 50, 52, 66, 85

differential thermal analysis (DTA), 52

distemper, 20, 30, 57, 62, 68, 69, 74, 100

drumminess, 49, 50

electron microscopy, 51, 54, 63

enrichments (see also ornamentation), 32, 35, 38, 85, 86, 87, 90, 97, 98

expanded metal, 102

Federation style (see also roughcast, pebbledash), 14, 21, 75

finishes (see also paint, distemper, limewash, stucco wash, cement wash, whitewash, varnish, pigments, colourants, colour wash), 5, 12, 13, 14, 16, 17, 18, 20, 21, 22, 23, 30, 33, 35, 48, 49, 50, 51, 55, 56, 64, 71, 72, 73, 74, 75, 76, 77, 78, 79, 80, 85, 86, 93, 94, 95, 96, 106, 111

clear, 71, 78

glue size, 74, 78, 79, 100

Haddon, Robert, 23, 29, 30, 31, 32, 33, 82, 98, 113

hair, 7, 18, 28, 33, 77, 81, 95, 101, 103, 106

hydration, 43, 45

importation (of cement), 26, 27

incised decoration, 6, 31, 74, 107

infra-red thermography, 49, 50

intervention, 54, 55, 64, 86, 94, 95

Italian Renaissance, 5, 6, 32, 35, 106

Italianate style, 13, 16, 17, 88

Italy

Rome, <0091>Porta Maggiore<0092>, 6

lath, 18, 29, 104

lathing, 100, 102, 104

lead white (lead carbonate), 57, 66, 69, 70

lime (types - see also limewash, stucco)

hydrated (calcium hydroxide), 10, 43, 44, 56, 68, 69, 79, 102

hydraulic, 5, 7, 8, 9, 11, 14, 15, 17, 18, 25, 26, 28, 35, 43, 44, 45, 56, 72, 99, 111

lias, 8

lime (types - see also limewash, stucco) non-hydraulic, 43, 44, 72

lime (types - see also limewash, stucco) pozzolanic, 56

lime (types - see also limewash, stucco) putty, 8, 13, 16, 18, 19, 43, 56, 93, 95, 105

lime (types - see also limewash, stucco) quicklime (calcium oxide), 7, 8, 30, 43, 100, 102

lime (types - see also limewash, stucco) roche, 16, 25

lime (types - see also limewash, stucco) rock (calcium oxide - see also quicklime), 8, 19, 23, 24, 25

lime (types - see also limewash, stucco) shell, 24, 25, 27, 29, 81, 100

lime (types - see also limewash, stucco) slaked, 6, 7, 8, 19, 43, 78, 106

magnesian, 23, 26

lime burning, 6, 8, 10, 24, 25, 28, 29, 43, 44, 56, 81, 82, 102

lime mortar, 81, 82, 87, 89, 90, 92, 93, 95

limewash (see also whitewash, colour washes), 55, 56, 58, 65, 66, 74, 78

linseed oil, 20, 30, 33, 57, 69, 73, 75, 78, 79, 100, 103

loam, 24, 25, 81, 107

Loudon, J C, 15, 19, 73, 74, 97, 108

materials identification, 54, 55, 59

moisture barrier, 66

mortar, 8, 13, 24, 25, 32, 38, 43, 45, 46, 47, 52, 68, 81, 82, 85, 86, 87, 90, 91, 92, 95, 98, 99, 101, 103, 104, 105, 106

composition, 87, 90, 103

Portland cement, 87, 98, 103, 106

mouldings (see also running mould), 13, 14, 15, 29, 31, 32, 35, 38, 66, 68, 85, 86, 87, 91, 92, 105, 106

moulds

plaster, 38

silicone rubber, 91

timber, 91

wax, 38

NSW

Ashfield, Vine Street, 28

Darlington, <0091>Romla<0092> and <0091>Frelin<0092>, 115

Glebe, <0091>Lyndhurst House<0092>, 35

NSW Goulburn, <0091>Noorilim<0092>, 30

NSW Hill End, cottage, 28

NSW Paramatta, Old Government House, 30

ochres, 18, 20

ornamentation (see also enrichments), 106

paint, 18, 20, 21, 30, 31, 33, 51, 55, 57, 61, 62, 63, 65, 66, 69, 70, 71, 72, 73, 74, 75, 76, 77, 78, 79, 80, 84, 86, 88, 99, 100, 103

acrylic, 65, 75, 80

cement, 33, 71, 74, 79

mineral, 65

oil, 20, 21, 33, 55, 57, 64, 70, 71, 73, 74, 75, 79

silicate, 20, 66, 71, 73, 74, 79, 80

water-based, 20, 79

paint removal, 71, 76, 77

Pasley, Charles, 10, 26, 109

patina, 58, 65, 94, 95, 96

pebbledash (see also roughcast), 105

pigments (see also colourants, whiting, lead white, zinc white, titanium dioxide, ochres), 19, 21, 29, 56, 57, 63, 64, 65, 72, 75, 78, 79, 103, 105

mineral, 19, 20, 57, 72, 73, 74, 78

plaster (see also stucco, cement render)

fibrous, 99, 104, 105

gypsum (calcium sulphate), 28, 38, 56, 87, 103, 104, 105, 106

hard, 30

lime, 7, 20, 29, 82, 98, 106, 107

plaster of Paris (see also gypsum plaster), 20, 30, 32, 74, 78, 79, 82, 91, 101, 104, 105, 106

plastering (see also rendering), 5, 6, 7, 8, 12, 13, 14, 15, 16, 17, 18, 20, 23, 24, 25, 28, 29, 64, 81, 82, 83, 92, 96, 97, 98, 99, 102, 103, 104, 105, 106, 108, 109

dash coat, 7

finish coat, 35, 51, 93

flanking, 105, 106

floating, 13, 17, 30, 82, 95, 103, 105, 106

gauging, 32, 106

one-coat method, 106

pricking up, 103

scratch coat, 17, 104

setting coat, 13, 16, 18, 27, 104

skim coat, 80, 105

three-coat method, 17

two-coat method, 106

poisons (used to destroy biological growth), 58

pozzolan (pozzuolan, pozzuolana), 43, 44, 87, 93, 95

pressed cement, 32

Queen Anne style (see also roughcast, pebbledash), 21, 75

refixing (mouldings etc), 91

Regency style, 9, 13

render (see also plaster, stucco), 7, 11, 17, 20, 27, 29, 31, 38, 45, 46, 47, 48, 56, 60, 84, 85, 86, 87, 88, 89, 90, 91, 98, 99, 100, 105

rendering, 6, 13, 16, 17, 18, 30, 82, 97, 98, 100

repair method, 94

resin, 56, 57, 61, 63, 66, 68, 71, 75, 78, 79, 95

rosin (pine resin), 56, 68

roughcast (see also pebbledash), 35, 97

running mould, 13, 90, 101, 104, 106

sample, 52, 54, 58, 59, 60, 61, 62, 63, 64

sampling, 17, 49, 50, 51, 54, 59, 60

sands, 15, 19, 29, 45, 46, 72

impurities, 45, 46, 52, 81

lime, 45

mineralogy, 45

quartz, 45

void ratio, 45, 46, 47

screeds, 100

septaria, 8, 15, 99

sgraffito, 18

significance, 47, 55, 58, 65, 80, 94

slipper, 105

SPAB (Society for the Preservation of Ancient Buildings), 95

specifications/instructions, original by

Charles Mayes, 26, 81, 113

Reed & Barnes, 82, 114

Terry & Oakden, 32, 83, 114

W W Wardell, 81, 114

spectroscopy, 52, 54, 63

stucco (types - see also plaster, cement render)

cement, 5, 13, 20, 23, 33, 72, 93, 94, 95, 96, 97, 98

common, 18

lime, 8, 18, 23, 73, 94, 95, 97

local, 23, 28

modern, 6, 8, 66

Portland cement, 5, 8, 19, 34, 79, 94, 97, 98

stucco terminology, 5, 27, 82

surface deposits, 54, 55, 58, 76

Syria, tomb at Palmyra, 6

tallow, 19, 30, 78

Tasmania

<0091>Mountford<0092>, 30

Launceston, Wesleyan Chapel, 29

New Norfolk, <0091>Willow Court<0092>, 115

testing

chemical, 49, 52

visual, 49, 51

textured finishes (see also roughcast, pebbledash), 5, 18, 106

titanium dioxide, 65, 66, 79

UK

Isle of Wight, <0091>Osborne House<0092>, 16, 17

Kent, <0091>Mereworth Castle<0092>, 7

varnish, 56, 62, 63, 69, 70

vermiculation, 32

Victoria

Carlton, <0091>Benvenuta<0092> (<0091>Medley Hall<0092>), 29, 30, 32, 33, 34, 54, 55, 56, 58, 61, 68

Carlton, <0091>Walkham House<0092>, 32

Doncaster, <0091>Pontville<0092>, 30

East Melbourne, Greek Orthodox Church, 31

Fitzroy, Gore Street, 27, 30, 114

Inverleigh, <0091>Lullote<0092>, 26

Malmsbury Town Hall, 93, 94

Port Albert, <0091>Hawthorn Bank<0092>, 28

Port Fairy, Volunteer Arms Hotel, 30

South Melbourne Town Hall, 5

Victoria St Kilda, 30 Burnett Street, 29, 32

Wangaratta district, <0091>Bontharambo<0092>, 84, 92, 115

visual inspection, 49

Waschatz, Otto, 32

wattle and daub, 28

Westox system of adhesives and additives, 91, 93, 95

whitewash (see also limewash), 55, 57, 58, 65, 66, 69, 70, 103

whiting (calcium carbonate - see also chalk), 8, 30, 56, 68, 69, 78, 100

zinc white (zinc carbonate), 66